Mechanisms and adsorption capacities of natural and eco-friendly nanoparticles for heavy metals and phosphate ions from water using DSD approach

Autors: Jovana Jokić Govedaricaa, Dragana Tomašević Pilipovića*, Vesna Gvoićb, Đurđa Kerkeza, Anita Leovac Maćeraka, Nataša Slijepčevića, Milena Bečelić-Tomina

a University of Novi Sad, Faculty of Sciences, Department of Chemistry, Biochemistry and Environmental Protection, Trg Dositeja Obradovića 3, 21000, Novi Sad, Serbia

b University of Novi Sad, Faculty of  Technical Sciences, Department of Graphic Engineering and Design, Trg Dositeja Obradovića 6, 21000, Novi Sad, Serbia

*Corresponding author: Dragana Tomašević Pilipović, Phone: +381 21 485 27 34; Fax: +381 21 454 065; e-mail address: dragana.tomasevic@dh.uns.ac.rs; Postal address: Trg Dositeja Obradovica 3, 21000 Novi Sad, Serbia

List of Figure Captions

Figure S1. Diagnostic plots: a) cadmium - Actual vs Predicted; b) cadmium - Residual by Predicted; c) phosphate - Actual vs Predicted; d) phosphate - Residual by Predicted

Figure S2: Pareto chart for: a) cadmium removal; b) phosphate removal

Figure S3. Diagnostic plots: a) nickel - Actual vs Predicted; b) nickel - Residual by Predicted; c) phosphate - Actual vs Predicted; d) phosphate - Residual by Predicted

Figure S4: Pareto chart for: a) nickel removal; b) phosphate removal

Figure 5. a) effect of reaction time on adsorption of Cd (II) and Ni (II) in the presence of phosphate on oak-nZVI b) kinetic model pseudo-first-order c) kinetic model pseudo-second-order

Figure S1. Diagnostic plots: a) cadmium - Actual vs Predicted; b) cadmium - Residual by Predicted; c) phosphate - Actual vs Predicted; d) phosphate - Residual by Predicted

Figure S2: Pareto chart for: a) cadmium removal; b) phosphate removal

Figure S3. Diagnostic plots: a) nickel - Actual vs Predicted; b) nickel - Residual by Predicted; c) phosphate - Actual vs Predicted; d) phosphate - Residual by Predicted

Figure S4: Pareto chart for: a) nickel removal; b) phosphate removal

Figure S5: a) effect of reaction time on adsorption of Cd (II) and Ni (II) in the presence of phosphate on oak-nZVI b) kinetic model pseudo-first-order c) kinetic model pseudo-second-order

List of Tables

Table S1. Process variables with experimental levels

Table S2. DSD experimental design layout

Table S3. Adsorption efficiency (%) for the removal of cadmium and phosphate

Table S4. Standard selection criteria for the regression models (cadmium and phosphate)

Table S5. ANOVA and "Lack of fit "test (cadmium and phosphate)

Table S6. Experimental verification of optimized processes for cadmium and phosphate removal

Table S7. Adsorption efficiency (%) for the removal of nickel and phosphate

Table S8. Standard selection criteria for the regression models (nickel and phosphate)

Table S9. ANOVA and "Lack of fit"test – nickel and phosphate removal

Table S10. Experimental verification of optimized processes

Table S11. Parameters of kinetic models for describing the adsorption of cadmium and nickel in the presence of phosphate on oak-nZVI

Table S1. Process variables with experimental levels

| Variables | Unit | Symbol coded | Levels |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | -1 | 0 | +1 |
| Metal concentration | mgL-1 | X1 | 1 | 5 | 9 |
| Ion concentation | mgL-1 | X2 | 1 | 5 | 9 |
| pH | - | X3 | 2 | 6 | 10 |
| oak-nZVI concentration | ml | X4 | 2 | 9 | 16 |

Table S2. DSD experimental design layout

| Run | Metal concentration | Ion concentration | pH | oak-nZVI concentration |
| --- | --- | --- | --- | --- |
| 1 | 9 | 9 | 10 | 9 |
| 2 | 1 | 1 | 2 | 9 |
| 3 | 1 | 5 | 10 | 16 |
| 4 | 9 | 5 | 2 | 2 |
| 5 | 5 | 1 | 2 | 16 |
| 6 | 5 | 9 | 10 | 2 |
| 7 | 1 | 9 | 6 | 16 |
| 8 | 9 | 1 | 6 | 2 |
| 9 | 9 | 9 | 2 | 16 |
| 10 | 1 | 1 | 10 | 2 |
| 11 | 9 | 1 | 10 | 16 |
| 12 | 1 | 9 | 2 | 2 |
| 13 | 5 | 5 | 6 | 9 |
| 14 | 9 | 9 | 10 | 9 |
| 15 | 1 | 1 | 2 | 9 |
| 16 | 1 | 5 | 10 | 16 |
| 17 | 9 | 5 | 2 | 2 |
| 18 | 5 | 1 | 2 | 16 |
| 19 | 5 | 9 | 10 | 2 |
| 20 | 1 | 9 | 6 | 16 |
| 21 | 9 | 1 | 6 | 2 |
| 22 | 9 | 9 | 2 | 16 |
| 23 | 1 | 1 | 10 | 2 |
| 24 | 9 | 1 | 10 | 16 |
| 25 | 1 | 9 | 2 | 2 |
| 26 | 5 | 5 | 6 | 9 |
| 27 | 5 | 5 | 6 | 9 |
| 28 | 5 | 5 | 6 | 9 |

Table S3. Adsorption efficiency (%) for the removal of cadmium and phosphate

| Run | Cadmium | Phosphate |
| --- | --- | --- |
| 1 | 91.06 | 64.67 |
| 2 | 90.02 | 82.00 |
| 3 | 96.63 | 29.00 |
| 4 | 85.94 | 71.56 |
| 5 | 57.54 | 75.00 |
| 6 | 95.86 | 81.40 |
| 7 | 98.96 | 73.00 |
| 8 | 26.02 | 76.22 |
| 9 | 91.90 | 66.89 |
| 10 | 15.44 | 97.00 |
| 11 | 24.85 | 81.00 |
| 12 | 99.01 | 69.00 |
| 13 | 89.61 | 83.20 |
| 14 | 92.59 | 64.22 |
| 15 | 90.47 | 87.00 |
| 16 | 96.71 | 34.00 |
| 17 | 86.09 | 71.89 |
| 18 | 59.56 | 76.40 |
| 19 | 95.64 | 79.80 |
| 20 | 98.91 | 69.00 |
| 21 | 39.83 | 76.89 |
| 22 | 91.90 | 66.33 |
| 23 | 91.13 | 91.00 |
| 24 | 33.14 | 79.00 |
| 25 | 98.87 | 65.00 |
| 26 | 91.95 | 81.80 |
| 27 | 91.47 | 82.60 |
| 28 | 92.19 | 82.20 |

Table S4. Standard selection criteria for the regression models (cadmium and phosphate)

| Descriptive factor | Cadmium | Phosphate |
| --- | --- | --- |
| R2 | 0.823 | 0.737 |
| R2 adj | 0.761 | 0.626 |
| AIC | 241.184 | 223.199 |
| BIC | 243.174 | 223.580 |
| RMSE | 12.886 | 8.779 |

Table S6. ANOVA and "Lack of fit "test (cadmium and phosphate)

| Source | aDF | bSS | cMS | F parameter |
| --- | --- | --- | --- | --- |
|  | Cadmium |  |  |  |
| Model | 7 | 15480.632 | 2211.520 | 13.318 |
| Error | 20 | 3321.069 | 166.050 | Prob>F |
| C. Total | 27 | 18801.701 | - | <0.0001 |
| Lack of Fit | 5 | 319.399 | 63.880 | 0.319 |
| Pure Error | 15 | 3001.669 | 200.111 | Prob>F |
| Total Error | 20 | 3321.069 | - | 0.894 |
|  | Phosphate |  |  |  |
| Model | 8 | 4107. 143 | 513.393 | 6.661 |
| Error | 19 | 1464.501 | 77.079 | Prob>F |
| C. Total | 27 | 5571.644 | - | 0.0003 |
| Lack of Fit | 4 | 1399.634 | 349.908 | 80.9137 |
| Pure Error | 15 | 64.867 | 4.324 | Prob>F |
| Total Error | 19 | 1464.501 | - | 0.966 |

aDegrees of freedom;bThe sum of square; cVariance (mean of square)

Table S6. Experimental verification of optimized processes for cadmium and phosphate removal

| Run | Cadmium | Phosphate |
| --- | --- | --- |
| 1 | 98.90 | 89.28 |
| 2 | 99.66 | 87.38 |
| 3 | 98.98 | 87.42 |
| 4 | 98.77 | 87.92 |
| 5 | 98.93 | 88.02 |
| 6 | 99.08 | 87.16 |
| 7 | 99.09 | 87.66 |
| 8 | 98.99 | 87.44 |
| 95% confidence interval | 98.83 - 99.27% | 87.29 - 87.86% |

Table S7. Adsorption efficiency (%) for the removal of nickel and phosphate

| Run | Nickel | Phosphate |
| --- | --- | --- |
| 1 | 92.08 | 95.76 |
| 2 | 13.96 | 49.40 |
| 3 | 91.35 | 58.00 |
| 4 | 91.59 | 95.99 |
| 5 | 67.39 | 75.20 |
| 6 | 85.98 | 63.02 |
| 7 | 87.59 | 71.90 |
| 8 | 60.31 | 97.70 |
| 9 | 76.55 | 80.84 |
| 10 | 76.32 | 75.50 |
| 11 | 65.18 | 90.34 |
| 12 | 76.16 | 13.10 |
| 13 | 93.69 | 83.58 |
| 14 | 85.39 | 95.73 |
| 15 | 87.09 | 48.70 |
| 16 | 89.03 | 56.10 |
| 17 | 93.05 | 95.93 |
| 18 | 90.50 | 74.14 |
| 19 | 87.01 | 63.86 |
| 20 | 88.93 | 71.20 |
| 21 | 66.93 | 97.66 |
| 22 | 79.99 | 80.74 |
| 23 | 97.38 | 80.30 |
| 24 | 71.32 | 90.82 |
| 25 | 79.69 | 13.30 |
| 26 | 94.69 | 83.52 |
| 27 | 95.11 | 83.50 |
| 28 | 94.86 | 83.28 |

Table S8. Standard selection criteria for the regression models (nickel and phosphate)

| Descriptive factor | Nickel | Phosphate |
| --- | --- | --- |
| R2 | 0.715 | 0.910 |
| R2 adj | 0.546 | 0.872 |
| AIC | 246.007 | 218.047 |
| BIC | 241.194 | 218.428 |
| RMSE | 11.286 | 8.008 |

Table S9. ANOVA and "Lack of fit"test – nickel and phosphate removal

| Source | DF | SS | MS | F parameter |
| --- | --- | --- | --- | --- |
|  | Nickel |  |  |  |
| Model | 10 | 5421.248 | 542.125 | 4.256 |
| Error | 17 | 2165.324 | 127.372 | Prob>F |
| C. Total | 27 | 7586.574 | - | 0.0044 |
| Lack of Fit | 15 | 2165.235 | 144.39 | 3234.107 |
| Pure Error | 2 | 0.089 | 0.045 | Prob>F |
| Total Error | 17 | 2165.324 | - | 0.906 |
|  | Phosphate |  |  |  |
| Model | 8 | 12307.914 | 1538.49 | 23.993 |
| Error | 19 | 1218.335 | 64.12 | Prob>F |
| C. Total | 27 | 13526.249 | - | <0.0001 |
| Lack of Fit | 17 | 1218.299 | 71.665 | 4041.240 |
| Pure Error | 2 | 0.0355 | 0.018 | Prob>F |
| Total Error | 19 | 1218.3347 | - | 0.925 |

Table S10. Experimental verification of optimized processes

| Run | Nickel | Phosphate |
| --- | --- | --- |
| 1 | 93.77 | 96.20 |
| 2 | 94.85 | 96.92 |
| 3 | 95.14 | 96.82 |
| 4 | 94.65 | 96.75 |
| 5 | 93.73 | 97.12 |
| 6 | 94.02 | 97.06 |
| 7 | 94.56 | 97.03 |
| 8 | 94.45 | 96.41 |
| 95% confidence interval | 93.97 - 94.83% | 96.51-97.06% |

Table S11. Parameters of kinetic models for describing the adsorption of cadmium and nickel in the presence of phosphate on oak-nZVI

| Pseudo-first order |  |  |  |  |
| --- | --- | --- | --- | --- |
| Metal | R2 | qe (mg/g) exp | k1 (min−1) | qe (mg/g) cal1 |
| Cd | 0.815 | 53 | 0.96 | 43.3 |
| Ni | 0.839 | 47 | 0.977 | 18.6 |
| Pseudo-second order |  |  |  |  |
| Metal | R2 | qe (mg/g) exp | k2 ·10-3 (q mg−1 min−1) | qe (mg/g) cal2 |
| Cd | 0.957 | 53 | 1.89 | 55.1 |
| Ni | 0.996 | 47 | 6.48 | 47.7 |