Supplementary Materials

Preparative and catalytic properties of MoVI mononuclear and metallosupramolecular coordination assemblies bearing hydrazonato ligands

Mirna Mandarić, Edi Topić, Dominique Agustin*, Jana Pisk*, Višnja Vrdoljak*

Contents

Scheme	2

Single-crystal X-ray diffraction	3

NMR spectroscopy	21

Imaginary frequency (cm−1) of the calculated transition states shown in Table S14.	29

DFT Coordinates of all species.	29

# Scheme

Scheme S1. Hydrazidato and hydrazonato tautomeric forms.

# Single-crystal X-ray diffraction

(a)

(b)

(c)

(d)

(e)

(f)

Figure S1. Molecular structure and enumeration scheme for (a) H2L3, (b) H2L4, (c) 1a, (d) 2a, (e) 3a, (f) 3. Non-hydrogen atoms are shown as thermal ellipsoids at 30% probability. The second symmetrically inequivalent molecule in (b) is omitted for clarity. In (f), only symmetrically unique molecular fragment is shown.

(a)

(b)

(c)

(d)

(e)

(f)

Figure S2. Packing of molecules in the crystal structure of (a) H2L3, (b) H2L4, (c) 1a, (d) 2a, (e) 3a, (f) 3, shown along c-axis for ligands (a) and (b) and along b-axis for complexes (c)-(f).

(a)

(b)

Figure S3. Supramolecular environment of ligand molecules in (a) H2L3 and (b) H2L4. In (a), ligand molecules form supramolecular chains through hydrazide N–H∙∙∙Oar hydrogen bond. In (b), symmetrically inequivalent molecules (shown as green and blue) form a complicated hydrogen bond network.

(a)

(b)

(c)

(d)

Figure S4. Supramolecular environment of complex molecules in (a) 1a, (b) 2a, (c) 3a and (d) 3. All complexes have few available hydrogen bond donors (methanol OH moiety or NH2 moiety on the aromatic ring), therefore observed supramolecular networks are relatively simple. In (a) and (b) supramolecular chains are formed between methanol OH group and pyridyl nitrogen atom. In (c), supramolecular dimers are established through methanol OH and amine nitrogen atom, which are further connected in chains through N-H∙∙∙Oeq=Mo hydrogen bond. Finally, in (d), only the similar situation is found as in (c), except that dimers are formed through coordination of amine to the MoO2 core.

Table S1. Experimental and crystallographic data for ligands H2L3 and H2L4.

| Identifier | H2L3 | H2L4 |
| --- | --- | --- |
| Empirical formula | C15H15N3O3 | C15H15N3O3 |
| Mr | 285.30 | 285.30 |
| T/K | 150.00 | 150.00 |
| Crystal system | orthorhombic, yellow block | triclinic, yellow prism |
| Space group | P n a 21 | P –1 |
| a/Å | 19.964(2) | 9.6923(6) |
| b/Å | 11.2493(9) | 11.4322(6) |
| c/Å | 6.1009(8) | 12.8069(7) |
| α/° | 90 | 95.232(4) |
| β/° | 90 | 93.942(5) |
| γ/° | 90 | 95.427(4) |
| V/Å3 | 1370.1(3) | 1402.52(14) |
| Z | 4 | 4 |
| ρcalc/g cm–3 | 1.383 | 1.351 |
| μ/mm–1 | 0.099 | 0.096 |
| F(000) | 600 | 600 |
| Crystal size/mm3 | 0.7×0.2×0.02 | 0.4×0.2×0.2 |
| Radiation | MoKα (λ = 0.71073Å) | MoKα (λ = 0.71073Å) |
| 2Θ range/° | 8.628 to 51.982 | 8.284 to 51.998 |
| Index ranges | –24 ≤ h ≤ 24, –13 ≤ k ≤ 13, –7 ≤ l ≤ 7 | –7 ≤ h ≤ 11, –14 ≤ k ≤ 14, –15 ≤ l ≤ 15 |
| Reflections collected | 12063 | 12837 |
| Independent reflections | 2645 [Rint = 6.2%, Rsigma = 6.71 %] | 5486 [Rint = 5.3%, Rsigma = 3.11 %] |
| Data/restraints/parameters | 2645/-/203 | 5486/-/405 |
| g1, g2 in wa | 0.0313, 0 | 0.0546, 0 |
| Goodness–of–fit on F2, Sb | 1.069 | 1.008 |
| Final R and wRc values [I≥2σ(I)] | R1 = 5.29%, wR2 = 8.4% | R1 = 4.92%, wR2 = 10.86% |
| Final R and wRc values [all data] | R1 = 7.08%, wR2 = 8.95% | R1 = 8.0%, wR2 = 12.55% |
| Largest diff. peak/hole / e Å–3 | 0.147/–0.155 | 0.206/–0.211 |
| Flack parameter | 0.1(10) | / |

aw = 1/[σFo2 + (g1P)2 + g2P] where P = (Fo2 + 2Fc2)/3
bS = {Σ[w(Fo2 – Fc2)2]/(Nr – Np)}1/2 where Nr = number of independent reflections, Np = number of refined parameters.
cR = Σ||Fo| – |Fc|/Σ|Fo|; wR = {Σ[w(Fo2 – Fc2)2]/Σ[w(Fo2)2]}1/2

Table S2. Selected bond lengths in the crystal structures of ligands H2L3 and H2L4.

| H2L3 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Atoms | Bond length/Å | Atoms | Bond length/Å | Atoms | Bond length/Å |
| C4–C5 | 1.382(5) | C11–C12 | 1.386(5) | N3–H3B | 0.85(3) |
| C5–C6 | 1.394(6) | N1–C1 | 1.290(4) | O1–C14 | 1.378(4) |
| C6–C7 | 1.373(5) | N1–N2 | 1.375(4) | O1–H1 | 0.83(4) |
| C7–C8 | 1.408(5) | N2–C2 | 1.374(4) | O2–C2 | 1.233(4) |
| C9–C10 | 1.398(5) | N2–H2 | 0.88(2) | O3–C11 | 1.384(4) |
| C9–C14 | 1.410(5) | N3–C8 | 1.371(5) | O3–C15 | 1.420(5) |
| C10–C11 | 1.381(5) | N3–H3A | 0.89(4) |  |  |
| H2L4 |  |  |  |  |  |
| Atoms | Bond length/Å | Atoms | Bond length/Å | Atoms | Bond length/Å |
| C4–C5 | 1.376(3) | C25–C26 | 1.388(2) | N6–H6A | 0.87(2) |
| C5–C6 | 1.394(3) | C26–C27 | 1.386(3) | N6–H6B | 0.859(18) |
| C6–C7 | 1.394(3) | N1–C1 | 1.279(2) | O1–C14 | 1.365(2) |
| C7–C8 | 1.376(3) | N1–N2 | 1.378(2) | O1–H1 | 0.904(19) |
| C9–C10 | 1.393(2) | N2–C2 | 1.370(2) | O2–C2 | 1.231(2) |
| C9–C14 | 1.406(3) | N2–H2 | 0.906(19) | O3–C11 | 1.376(2) |
| C10–C11 | 1.383(3) | N3–C6 | 1.381(2) | O3–C15 | 1.397(2) |
| C11–C12 | 1.389(3) | N3–H3A | 0.872(19) | O4–C29 | 1.374(2) |
| C19–C20 | 1.381(3) | N3–H3B | 0.89(2) | O4–H4 | 0.849(19) |
| C20–C21 | 1.394(3) | N4–C16 | 1.282(2) | O5–C17 | 1.238(2) |
| C21–C22 | 1.395(3) | N4–N5 | 1.375(2) | O6–C26 | 1.370(2) |
| C22–C23 | 1.375(2) | N5–C17 | 1.367(2) | O6–C30 | 1.426(2) |
| C24–C25 | 1.392(2) | N5–H5 | 0.847(17) |  |  |

Table S3. Selected bond angles in the crystal structures of ligands H2L3 and H2L4.

| H2L3 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Atoms | Bond angle/° | Atoms | Bond angle/° | Atoms | Bond angle/° |
| N1–C1–C9 | 120.6(3) | N3–C8–C3 | 121.7(3) | N2–N1–C1 | 117.5(2) |
| N2–C2–C3 | 114.4(3) | N3–C8–C7 | 119.9(3) | C2–N2–H2 | 121(3) |
| O2–C2–C3 | 123.9(3) | C1–C9–C10 | 118.6(3) | N1–N2–C2 | 119.4(2) |
| O2–C2–N2 | 121.7(3) | C1–C9–C14 | 122.5(3) | N1–N2–H2 | 119(3) |
| C2–C3–C4 | 120.2(3) | C10–C9–C14 | 118.9(3) | C8–N3–H3A | 120(2) |
| C2–C3–C8 | 120.4(3) | C9–C10–C11 | 121.0(3) | C8–N3–H3B | 114(2) |
| C4–C3–C8 | 119.2(3) | C10–C11–C12 | 120.0(3) | H3A–N3–H3B | 121(3) |
| C3–C4–C5 | 121.3(3) | O3–C11–C10 | 116.0(3) | C14–O1–H1 | 106(2) |
| C4–C5–C6 | 119.3(3) | O3–C11–C12 | 124.0(3) | C11–O3–C15 | 117.5(3) |
| C5–C6–C7 | 120.6(3) | C11–C12–C13 | 119.7(3) |  |  |
| C6–C7–C8 | 121.1(4) | C12–C13–C14 | 121.0(3) |  |  |
| C3–C8–C7 | 118.3(3) | O1–C14–C9 | 122.9(3) |  |  |
| H2L4 |  |  |  |  |  |
| Atoms | Bond angle/° | Atoms | Bond angle/° | Atoms | Bond angle/° |
| N1–C1–C9 | 120.61(16) | O1–C14–C9 | 121.99(16) | C27–C28–C29 | 121.25(18) |
| N2–C2–C3 | 117.03(16) | N4–C16–C24 | 120.02(17) | O4–C29–C24 | 121.88(15) |
| O2–C2–C3 | 122.84(16) | N5–C17–C18 | 116.57(17) | N2–N1–C1 | 117.30(15) |
| O2–C2–N2 | 120.10(16) | O5–C17–C18 | 123.06(16) | C2–N2–H2 | 122.8(13) |
| C2–C3–C4 | 124.96(16) | O5–C17–N5 | 120.37(16) | N1–N2–C2 | 117.91(15) |
| C2–C3–C8 | 117.16(16) | C17–C18–C19 | 125.24(16) | N1–N2–H2 | 118.7(13) |
| C4–C3–C8 | 117.85(16) | C17–C18–C23 | 117.18(17) | C6–N3–H3A | 115.7(13) |
| C3–C4–C5 | 121.17(17) | C19–C18–C23 | 117.58(16) | C6–N3–H3B | 116.0(14) |
| C4–C5–C6 | 120.65(17) | C18–C19–C20 | 121.09(17) | H3A–N3–H3B | 120.5(19) |
| C5–C6–C7 | 118.61(16) | C19–C20–C21 | 120.93(18) | N5–N4–C16 | 118.08(16) |
| N3–C6–C5 | 121.34(17) | C20–C21–C22 | 118.18(17) | C17–N5–H5 | 124.7(15) |
| N3–C6–C7 | 120.02(16) | N6–C21–C20 | 121.51(18) | N4–N5–C17 | 118.30(16) |
| C6–C7–C8 | 120.51(16) | N6–C21–C22 | 120.30(18) | N4–N5–H5 | 117.0(15) |
| C3–C8–C7 | 121.21(17) | C21–C22–C23 | 120.81(17) | C21–N6–H6A | 118.0(13) |
| C1–C9–C10 | 118.40(16) | C18–C23–C22 | 121.41(18) | C21–N6–H6B | 120.7(14) |
| C1–C9–C14 | 122.64(15) | C16–C24–C25 | 119.18(17) | H6A–N6–H6B | 121.3(19) |
| C10–C9–C14 | 118.92(16) | C16–C24–C29 | 121.90(16) | C14–O1–H1 | 108.2(13) |
| C9–C10–C11 | 121.13(17) | C25–C24–C29 | 118.92(16) | C11–O3–C15 | 118.37(15) |
| C10–C11–C12 | 119.73(16) | C24–C25–C26 | 121.32(17) | C29–O4–H4 | 106.4(13) |
| O3–C11–C10 | 115.64(16) | C25–C26–C27 | 119.42(17) | C26–O6–C30 | 117.01(15) |
| O3–C11–C12 | 124.62(16) | O6–C26–C25 | 115.71(17) |  |  |

Table S4. Hydrogen bond parameters in the crystal structure of H2L3 and H2L4

| H2L3 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| D–H···A | D-H | H···A | D···A | ∠D–H···A | Symmetry code |
| N2–H2···O1 | 0.88(2) | 2.19(2) | 3.069(3) | 174(4) | –3/2–x, –1/2+y, –1/2+z |
| C10–H10···O2 | 0.95 | 2.47 | 3.404(4) | 167 | –3/2–x, –1/2+y, 1/2+z |
| H2L4 |  |  |  |  |  |
| D–H···A | D-H | H···A | D···A | ∠D–H···A | Symmetry code |
| N2–H2···O4 | 0.906(19) | 2.077(19) | 2.930(2) | 156.4(18) | –1+x, y, z |
| N3–H3A···O3 | 0.872(19) | 2.586(19) | 3.160(2) | 124.2(16) | –x, 1–y, 1–z |
| N3–H3B···O5 | 0.89(2) | 2.208(19) | 3.075(2) | 166.0(18) | 1–x, 1–y, 2–z |
| N5–H5···O2 | 0.847(17) | 2.014(17) | 2.823(2) | 159(2) | x, y, z |
| N6–H6A···O1 | 0.87(2) | 2.30(2) | 3.121(2) | 157.1(18) | 1–x, 2–y, 2–z |
| C4–H4A···O4 | 0.95 | 2.59 | 3.445(2) | 150 | –1+x, y, z |
| C15–H15B···O5 | 0.98 | 2.40 | 3.310(3) | 154 | 1–x, 2–y, 1–z |
| C15–H15C···O2 | 0.98 | 2.59 | 3.476(3) | 151 | –x, 2–y, 1–z |
| C16–H16···O2 | 0.95 | 2.52 | 3.238(2) | 133 | x, y, z |
| C19–H19···O2 | 0.95 | 2.55 | 3.444(2) | 158 | x, y, z |

Table S5. Experimental and crystallographic data for dioxomolybdenum(VI) complexes 1a, 2a, 3a and 3.

| Identifier | 1a | 2a | 3a | 3 |
| --- | --- | --- | --- | --- |
| Empirical formula | C15H15MoN3O6 | C15H15MoN3O6 | C16H17MoN3O6 | C30H26Mo2N6O10 |
| Mr | 429.24 | 429.24 | 443.26 | 822.45 |
| T/K | 169.98(10) | 169.99(10) | 169.99(10) | 170.00(10) |
| Crystal system | monoclinic, orange needle | monoclinic, orange plate | triclinic, orange plate | monoclinic, red block |
| Space group | P 1 21/c 1 | P 1 21 1 | P –1 | P 1 21/c 1 |
| a/Å | 17.7236(4) | 7.9094(3) | 8.1385(3) | 8.06221(12) |
| b/Å | 12.4615(2) | 12.4768(4) | 9.7144(3) | 9.71973(14) |
| c/Å | 7.32534(17) | 8.2941(2) | 10.9563(4) | 18.7390(3) |
| α/° | 90 | 90 | 78.178(3) | 90 |
| β/° | 99.127(2) | 95.092(3) | 88.831(3) | 93.5334(14) |
| γ/° | 90 | 90 | 85.144(3) | 90 |
| V/Å3 | 1597.41(6) | 815.26(5) | 844.79(5) | 1465.64(4) |
| Z | 4 | 2 | 2 | 2 |
| ρcalc/g cm–3 | 1.785 | 1.749 | 1.743 | 1.864 |
| μ/mm–1 | 7.087 | 6.943 | 6.722 | 7.641 |
| F(000) | 864 | 432 | 448 | 824 |
| Crystal size/mm3 | 0.15×0.1×0.05 | 0.48×0.14×0.06 | 0.12×0.08×0.03 | 0.15×0.12×0.1 |
| Radiation | CuKα (λ = 1.54184Å) |  |  |  |
| 2Θ range/° | 8.712 to 155.574 | 10.708 to 154.896 | 8.244 to 156.32 | 9.458 to 155.358 |
| Index ranges | –22 ≤ h ≤ 22, –13 ≤ k ≤ 15, –8 ≤ l ≤ 9 | –9 ≤ h ≤ 10, –15 ≤ k ≤ 15, –8 ≤ l ≤ 10 | –10 ≤ h ≤ 10, –11 ≤ k ≤ 12, –13 ≤ l ≤ 13 | –10 ≤ h ≤ 10, –11 ≤ k ≤ 12, –23 ≤ l ≤ 23 |
| Reflections collected | 17049 | 6361 | 13040 | 15002 |
| Independent reflections | 3395 [Rint = 5.45%, Rsigma = 7.58 %] | 2812 [Rint = 5.71%, Rsigma = 5.9 %] | 3517 [Rint = 6.81%, Rsigma = 7.14 %] | 3095 [Rint = 4.61%, Rsigma = 7.69 %] |
| Data/restraints/parameters | 3395/-/232 | 2812/-/231 | 3517/-/246 | 3095/-/219 |
| g1, g2 in wa | 0.0855, 0 | 0.1140, 0 | 0.0001, 7.1347 | 0.0822, 0.3951 |
| Goodness–of–fit on F2, Sb | 1.086 | 1.113 | 1.099 | 1.078 |
| Final R and wRc values [I≥2σ(I)] | R1 = 4.22%, wR2 = 11.35% | R1 = 5.51%, wR2 = 14.78% | R1 = 5.5%, wR2 = 13.71% | R1 = 4.1%, wR2 = 11.38% |
| Final R and wRc values [all data] | R1 = 4.77%, wR2 = 12.32% | R1 = 5.64%, wR2 = 15.22% | R1 = 5.89%, wR2 = 13.88% | R1 = 4.18%, wR2 = 11.52% |
| Largest diff. peak/hole / e Å–3 | 1.227/–1.461 | 1.821/–1.786 | 1.413/–1.063 | 1.384/–1.229 |
| Flack parameter | / | 0.00(2) | / | / |

aw = 1/[σFo2 + (g1P)2 + g2P] where P = (Fo2 + 2Fc2)/3
bS = {Σ[w(Fo2 – Fc2)2]/(Nr – Np)}1/2 where Nr = number of independent reflections, Np = number of refined parameters.
cR = Σ||Fo| – |Fc|/Σ|Fo|; wR = {Σ[w(Fo2 – Fc2)2]/Σ[w(Fo2)2]}1/2

Table S6. Selected bond lengths in the crystal structures of 1a, 2a, 3a and 3.

| 1a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Atoms | Bond length/Å | Atoms | Bond length/Å | Atoms | Bond length/Å |
| C4–C5 | 1.373(5) | Mo1–O1 | 1.916(2) | N3–C6 | 1.334(5) |
| C6–C7 | 1.392(5) | Mo1–O2 | 2.038(2) | O1–C9 | 1.351(4) |
| C8–C9 | 1.421(4) | Mo1–O4 | 1.704(2) | O2–C2 | 1.323(3) |
| C8–C13 | 1.392(4) | Mo1–O5 | 1.706(2) | O3–C12 | 1.364(4) |
| C9–C10 | 1.392(5) | Mo1–O6 | 2.313(2) | O3–C14 | 1.425(4) |
| C10–C11 | 1.384(5) | N1–C1 | 1.281(4) | O6–C15 | 1.419(4) |
| C11–C12 | 1.399(4) | N1–N2 | 1.398(4) | O6–H6 | 0.88(3) |
| C12–C13 | 1.385(4) | N2–C2 | 1.289(4) |  |  |
| Mo1–N1 | 2.244(2) | N3–C5 | 1.335(5) |  |  |
| 2a |  |  |  |  |  |
| Atoms | Bond length/Å | Atoms | Bond length/Å | Atoms | Bond length/Å |
| C5–C6 | 1.381(14) | Mo1–O1 | 2.024(6) | N3–C5 | 1.327(14) |
| C6–C7 | 1.395(14) | Mo1–O2 | 1.918(5) | O1–C2 | 1.308(12) |
| C8–C9 | 1.402(13) | Mo1–O4 | 1.707(7) | O2–C9 | 1.349(12) |
| C8–C13 | 1.408(12) | Mo1–O5 | 1.704(9) | O3–C12 | 1.371(12) |
| C9–C10 | 1.399(12) | Mo1–O6 | 2.295(7) | O3–C14 | 1.432(12) |
| C10–C11 | 1.404(13) | N1–C1 | 1.286(12) | O6–C15 | 1.413(13) |
| C11–C12 | 1.405(14) | N1–N2 | 1.409(10) | O6–H6 | 0.88(11) |
| C12–C13 | 1.391(12) | N2–C2 | 1.287(11) |  |  |
| Mo1–N1 | 2.226(8) | N3–C4 | 1.343(12) |  |  |
| 3a |  |  |  |  |  |
| Atoms | Bond length/Å | Atoms | Bond length/Å | Atoms | Bond length/Å |
| C5–C6 | 1.376(9) | Mo1–N1 | 2.243(4) | N3–H3B | 0.88(5) |
| C6–C7 | 1.396(9) | Mo1–O1 | 1.919(4) | O1–C10 | 1.355(7) |
| C7–C8 | 1.386(9) | Mo1–O2 | 2.001(4) | O2–C2 | 1.338(6) |
| C9–C10 | 1.404(8) | Mo1–O4 | 1.700(5) | O3–C13 | 1.369(8) |
| C9–C14 | 1.414(8) | Mo1–O5 | 1.711(4) | O3–C15 | 1.422(8) |
| C10–C11 | 1.392(8) | Mo1–O6 | 2.287(4) | O6–C00O | 1.425(9) |
| C11–C12 | 1.379(9) | N1–N2 | 1.389(6) | O6–H6 | 0.872(16) |
| C12–C13 | 1.383(8) | N3–H3A | 0.85(4) |  |  |
| 3 |  |  |  |  |  |
| Atoms | Bond length/Å | Atoms | Bond length/Å | Atoms | Bond length/Å |
| C3–C4 | 1.410(4) | C11–C12 | 1.385(4) | N1–C2 | 1.291(3) |
| C3–C8 | 1.395(4) | C12–C13 | 1.386(4) | N1–N2 | 1.391(3) |
| C4–C5 | 1.389(4) | C13–C14 | 1.383(4) | O1–C4 | 1.351(4) |
| C5–C6 | 1.390(4) | Mo1–N1 | 2.238(2) | O2–C1 | 1.329(3) |
| C6–C7 | 1.396(4) | Mo1–N3_a | 2.536(2) | O3–C7 | 1.364(3) |
| C7–C8 | 1.388(4) | Mo1–O1 | 1.912(2) | O3–C15 | 1.411(4) |
| C9–C10 | 1.409(4) | Mo1–O2 | 2.0197(18) |  |  |
| C9–C14 | 1.402(4) | Mo1–O4 | 1.705(3) |  |  |
| C10–C11 | 1.393(4) | Mo1–O5 | 1.714(2) |  |  |

Table S7. Selected bond angles in the crystal structure of 1a, 2a, 3a and 3.

| 1a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Atoms | Bond angle/° | Atoms | Bond angle/° | Atoms | Bond angle/° |
| N1–C1–C8 | 123.6(2) | O1–C9–C10 | 118.6(2) | O4–Mo1–O6 | 168.65(10) |
| N2–C2–C3 | 117.3(3) | C9–C10–C11 | 121.2(3) | O5–Mo1–N1 | 160.79(11) |
| O2–C2–C3 | 117.5(3) | C10–C11–C12 | 120.2(3) | O5–Mo1–O6 | 85.17(10) |
| O2–C2–N2 | 125.3(3) | O3–C12–C11 | 125.3(3) | O6–Mo1–N1 | 77.73(9) |
| C2–C3–C4 | 119.7(3) | O3–C12–C13 | 115.4(3) | Mo1–N1–C1 | 128.5(2) |
| C2–C3–C7 | 122.0(3) | O1–Mo1–N1 | 81.64(9) | Mo1–N1–N2 | 115.35(17) |
| C4–C3–C7 | 118.3(3) | O1–Mo1–O2 | 149.36(9) | N2–N1–C1 | 115.8(2) |
| C3–C4–C5 | 118.7(3) | O1–Mo1–O4 | 98.87(11) | N1–N2–C2 | 109.2(2) |
| N3–C5–C4 | 123.8(4) | O1–Mo1–O5 | 104.62(10) | C5–N3–C6 | 117.6(3) |
| N3–C6–C7 | 122.9(3) | O1–Mo1–O6 | 81.58(9) | Mo1–O1–C9 | 134.36(19) |
| C3–C7–C6 | 118.8(3) | O2–Mo1–N1 | 72.05(9) | Mo1–O2–C2 | 117.62(19) |
| C1–C8–C9 | 122.7(3) | O2–Mo1–O4 | 97.09(10) | C12–O3–C14 | 117.9(2) |
| C1–C8–C13 | 117.9(3) | O2–Mo1–O5 | 95.99(10) | C15–O6–H6 | 107.6(15) |
| C9–C8–C13 | 119.4(3) | O2–Mo1–O6 | 77.78(8) | Mo1–O6–C15 | 127.8(2) |
| C8–C9–C10 | 118.6(3) | O4–Mo1–N1 | 91.09(10) | Mo1–O6–H6 | 118.4(15) |
| O1–C9–C8 | 122.8(3) | O4–Mo1–O5 | 105.57(11) |  |  |
| 2a |  |  |  |  |  |
| Atoms | Bond angle/° | Atoms | Bond angle/° | Atoms | Bond angle/° |
| N1–C1–C8 | 123.2(9) | O2–C9–C10 | 116.9(9) | O4–Mo1–O6 | 169.1(3) |
| N2–C2–C3 | 118.2(9) | C9–C10–C11 | 120.1(8) | O5–Mo1–N1 | 160.8(3) |
| O1–C2–C3 | 116.9(7) | C10–C11–C12 | 119.6(8) | O5–Mo1–O6 | 85.3(3) |
| O1–C2–N2 | 124.9(8) | O3–C12–C11 | 124.3(8) | O6–Mo1–N1 | 77.6(3) |
| C2–C3–C4 | 118.9(9) | O3–C12–C13 | 115.0(9) | Mo1–N1–C1 | 128.3(6) |
| C2–C3–C7 | 123.3(8) | O1–Mo1–N1 | 71.9(3) | Mo1–N1–N2 | 115.4(5) |
| C4–C3–C7 | 117.8(8) | O1–Mo1–O2 | 149.4(3) | N2–N1–C1 | 115.8(7) |
| N3–C4–C3 | 122.2(9) | O1–Mo1–O4 | 96.6(3) | N1–N2–C2 | 108.7(7) |
| N3–C5–C6 | 123.3(8) | O1–Mo1–O5 | 96.8(3) | C4–N3–C5 | 118.7(8) |
| C5–C6–C7 | 118.6(10) | O1–Mo1–O6 | 80.0(3) | Mo1–O1–C2 | 118.6(5) |
| C3–C7–C6 | 119.4(9) | O2–Mo1–N1 | 81.8(4) | Mo1–O2–C9 | 134.1(6) |
| C1–C8–C9 | 122.8(8) | O2–Mo1–O4 | 99.5(3) | C12–O3–C14 | 117.4(9) |
| C1–C8–C13 | 116.9(8) | O2–Mo1–O5 | 103.6(4) | C15–O6–H6 | 110(2) |
| C9–C8–C13 | 120.3(8) | O2–Mo1–O6 | 79.2(2) | Mo1–O6–C15 | 129.4(7) |
| C8–C9–C10 | 119.9(8) | O4–Mo1–N1 | 91.5(3) | Mo1–O6–H6 | 121(2) |
| O2–C9–C8 | 123.1(8) | O4–Mo1–O5 | 105.5(4) |  |  |
| 3a |  |  |  |  |  |
| Atoms | Bond angle/° | Atoms | Bond angle/° | Atoms | Bond angle/° |
| N1–C1–C9 | 123.5(5) | O1–C10–C9 | 122.9(5) | O4–Mo1–O6 | 170.5(2) |
| N2–C2–C3 | 123.1(5) | O1–C10–C11 | 117.8(5) | O5–Mo1–N1 | 159.37(19) |
| O2–C2–C3 | 114.7(5) | C10–C11–C12 | 120.7(5) | O5–Mo1–O6 | 83.73(18) |
| O2–C2–N2 | 122.2(5) | C11–C12–C13 | 121.0(6) | O6–Mo1–N1 | 77.55(17) |
| C2–C3–C4 | 123.2(5) | C12–C13–C14 | 119.6(6) | Mo1–N1–C1 | 127.9(4) |
| C2–C3–C8 | 118.4(5) | O3–C13–C12 | 115.7(5) | Mo1–N1–N2 | 115.5(3) |
| C4–C3–C8 | 118.4(5) | O3–C13–C14 | 124.7(6) | N2–N1–C1 | 116.5(4) |
| C3–C4–C5 | 118.7(6) | O1–Mo1–N1 | 81.21(16) | N1–N2–C2 | 110.2(4) |
| N3–C4–C3 | 121.9(5) | O1–Mo1–O2 | 147.99(17) | C4–N3–H3B | 116(5) |
| N3–C4–C5 | 119.4(5) | O1–Mo1–O4 | 99.4(2) | C4–N3–H3A | 119(6) |
| C4–C5–C6 | 121.8(6) | O1–Mo1–O5 | 103.99(19) | H3A–N3–H3B | 97(8) |
| C5–C6–C7 | 120.4(6) | O1–Mo1–O6 | 79.55(16) | Mo1–O1–C10 | 134.2(4) |
| C6–C7–C8 | 118.2(6) | O2–Mo1–N1 | 71.65(16) | Mo1–O2–C2 | 120.5(4) |
| C3–C8–C7 | 122.5(6) | O2–Mo1–O4 | 98.6(2) | C13–O3–C15 | 117.4(5) |
| C1–C9–C10 | 122.7(5) | O2–Mo1–O5 | 96.28(18) | C00O–O6–H6 | 109(2) |
| C1–C9–C14 | 117.6(5) | O2–Mo1–O6 | 78.32(17) | Mo1–O6–C00O | 125.0(4) |
| C10–C9–C14 | 119.6(5) | O4–Mo1–N1 | 93.0(2) | Mo1–O6–H6 | 127(2) |
| C9–C10–C11 | 119.2(5) | O4–Mo1–O5 | 105.6(2) |  |  |
| 3 |  |  |  |  |  |
| Atoms | Bond angle/° | Atoms | Bond angle/° | Atoms | Bond angle/° |
| N2–C1–C9 | 120.5(3) | C1–C9–C14 | 118.1(3) | O2–Mo1–O5 | 96.85(9) |
| O2–C1–C9 | 117.0(2) | C10–C9–C14 | 118.9(3) | O4–Mo1–N1 | 94.60(9) |
| O2–C1–N2 | 122.4(2) | C9–C10–C11 | 118.9(3) | O4–Mo1–N3_a | 172.18(8) |
| N1–C2–C3 | 123.9(3) | N3–C10–C9 | 122.6(2) | O4–Mo1–O5 | 106.45(10) |
| C2–C3–C4 | 122.6(2) | N3–C10–C11 | 118.3(2) | O5–Mo1–N1 | 156.83(10) |
| C2–C3–C8 | 117.1(3) | C10–C11–C12 | 121.2(3) | O5–Mo1–N3_a | 79.87(9) |
| C4–C3–C8 | 120.2(3) | C11–C12–C13 | 120.4(3) | Mo1–N1–C2 | 129.44(18) |
| C3–C4–C5 | 118.9(3) | C12–C13–C14 | 119.0(3) | Mo1–N1–N2 | 115.41(15) |
| O1–C4–C3 | 122.5(3) | N1–Mo1–N3_a | 78.43(8) | N2–N1–C2 | 115.0(2) |
| O1–C4–C5 | 118.6(3) | O1–Mo1–N1 | 81.32(8) | N1–N2–C1 | 110.0(2) |
| C4–C5–C6 | 120.5(3) | O1–Mo1–N3_a | 82.28(8) | C10–N3–Mo1_a | 118.94(18) |
| C5–C6–C7 | 120.6(3) | O1–Mo1–O2 | 149.92(8) | Mo1–O1–C4 | 139.10(18) |
| C6–C7–C8 | 119.2(3) | O1–Mo1–O4 | 100.31(10) | Mo1–O2–C1 | 119.55(15) |
| O3–C7–C6 | 124.6(3) | O1–Mo1–O5 | 103.74(9) | C7–O3–C15 | 117.8(2) |
| O3–C7–C8 | 116.2(3) | O2–Mo1–N1 | 71.45(8) |  |  |
| C3–C8–C7 | 120.5(3) | O2–Mo1–N3_a | 80.00(7) |  |  |
| C1–C9–C10 | 123.0(2) | O2–Mo1–O4 | 94.49(9) |  |  |

Table S8. Hydrogen bond parameters in the crystal structure of 1a, 2a, 3a and 3.

| 1a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| D–H···A | D-H | H···A | D···A | ∠D–H···A | Symmetry code |
| O6–H6···N3 | 0.88(3) | 1.82(3) | 2.677(4) | 163(3) | –x, 1/2+y, 1/2–z |
| C1–H1···O4 | 0.95 | 2.37 | 3.307(4) | 170 | x, 1/2–y, 1/2+z |
| C6–H6A···O5 | 0.95 | 2.50 | 3.409(4) | 159 | –x, 1–y, –z |
| C10–H10···O3 | 0.95 | 2.41 | 3.319(3) | 161 | 1–x, 1/2+y, 3/2–z |
| 2a |  |  |  |  |  |
| D–H···A | D-H | H···A | D···A | ∠D–H···A | Symmetry code |
| O6–H6···N3 | 0.88(11) | 1.82(11) | 2.684(11) | 168(9) | x, y, –1+z |
| C1–H1···O4 | 0.95 | 2.41 | 3.319(12) | 160 | 1–x, 1/2+y, 1–z |
| C5–H5···O5 | 0.95 | 2.35 | 3.225(12) | 153 | –x, 1/2+y, 2–z |
| C11–H11···O4 | 0.95 | 2.55 | 3.303(11) | 136 | x, y, –1+z |
| C14–H14C···O5 | 0.98 | 2.55 | 3.358(12) | 140 | 1–x, 1/2+y, –z |
| 3a |  |  |  |  |  |
| D–H···A | D-H | H···A | D···A | ∠D–H···A | Symmetry code |
| O6–H6···N3 | 0.88(3) | 1.82(3) | 2.677(4) | 163(3) | –x, 1/2+y, 1/2–z |
| C1–H1···O4 | 0.95 | 2.37 | 3.307(4) | 170 | x, 1/2–y, 1/2+z |
| C6–H6A···O5 | 0.95 | 2.50 | 3.409(4) | 159 | –x, 1–y, –z |
| C10–H10···O3 | 0.95 | 2.41 | 3.319(3) | 161 | 1–x, 1/2+y, 3/2–z |
| 3 |  |  |  |  |  |
| D–H···A | D-H | H···A | D···A | ∠D–H···A | Symmetry code |
| N3–H3A···O5 | 0.91 | 2.22 | 3.129(3) | 177 | x, 1+y, z |
| C11–H11···O3 | 0.95 | 2.55 | 3.307(4) | 137 | –1+x, 3/2–y, –1/2+z |
| C15–H15B···O4 | 0.98 | 2.56 | 3.363(4) | 139 | x, 1/2–y, 1/2+z |

# NMR spectroscopy

Table S9 1H and 13C chemical shifts (ppm) of H2L1 and 1.

| Atom | H2L1 |  | 1 |  |
| --- | --- | --- | --- | --- |
|  | δ / ppm (1H) | δ / ppm (13C) | δ / ppm (1H) | δ / ppm (13C) |
| 1 | 8.75 | 148.07 | 8.98 | 156.73 |
| 4 | − | 160.94 | − | 166.63 |
| 5 | − | 139.53 | − | 136.90 |
| 6 | 7.92 | 121.06 | 7.88 | 120.94 |
| 7 | 8.85 | 149.83 | 8.77 | 149.96 |
| 8 | − | − | − | − |
| 9 | 8.85 | 149.83 | 8.77 | 149.96 |
| 10 | 7.92 | 121.98 | 7.88 | 120.94 |
| 11 | − | 118.41 | − | 119.57 |
| 12 | − | 151.17 | − | 153.36 |
| 13 | 6.94 | 116.87 | 6.93 | 118.78 |
| 14 | 6.97 | 118.15 | 7.18 | 121.54 |
| 15 | − | 151.71 | − | 153.02 |
| 16 | 7.22 | 111.50 | 7.39 | 116.51 |
| OH | 10.66 | − | − | − |
| NH | 12.37 | − | − | − |
| OMe | 3.77 | 54.94 | 3.78 | 55.14 |

H

C

N

N

C

N

O

H

O

H

1

1

1

2

1

3

1

4

1

5

1

2

3

4

5

6

7

9

1

0

1

6

8

CH3O

Scheme S2. The structural formula of H2L1 with the NMR numbering scheme

Table S10 1H and 13C chemical shifts (ppm) of H2L2 and 2.

| Atom | H2L2 |  | 2 |  |
| --- | --- | --- | --- | --- |
|  | δ / ppm (1H) | δ / ppm (13C) | δ / ppm (1H) | δ / ppm (13C) |
| 1 | 8.73 | 147.66 | 8.95 | 156.94 |
| 4 | − | 161.06 | − | 167.80 |
| 5 | − | 128.25 | − | 126.64 |
| 6 | 9.19 | 148.21 | 9.15 | 149.24 |
| 7 | − | − | − | − |
| 8 | 8.83 | 151.90 | 8.76 | 152.86 |
| 9 | 7.61 | 123.07 | 7.57 | 124.44 |
| 10 | 8.36 | 134.98 | 8.31 | 135.90 |
| 11 | − | 118.40 | − | 120.72 |
| 12 | − | 151.70 | − | 154.30 |
| 13 | 6.94 | 116.84 | 6.92 | 119.79 |
| 14 | 6.97 | 117.98 | 7.16 | 122.31 |
| 15 | − | 151.13 | − | 154.08 |
| 16 | 7.21 | 111.66 | 7.38 | 117.48 |
| OH | 10.72 | − | − | − |
| NH | 12.33 | − | − | − |
| OMe | 3.77 | 54.94 | 3.78 | 56.20 |

H

C

N

N

C

O

H

O

H

1

1

1

2

1

3

1

4

1

5

1

2

3

4

1

6

CH3O

N

5

6

7

8

9

1

0

Scheme S4. The structural formula of H2L2 with the NMR numbering scheme

Table S11 1H and 13C chemical shifts (ppm) of H2L3 and 3.

| Atom | H2L3 |  | 3 |  |
| --- | --- | --- | --- | --- |
|  | δ / ppm (1H) | δ / ppm (13C) | δ / ppm (1H) | δ / ppm (13C) |
| 1 | 8.63 | 146.73 | 8.93 | 154.04 |
| 4 | − | 164.59 | − | 169.14 |
| 5 | − | 112.09 | − | 108.85 |
| 6 | − | 149.79 | − | 148.89 |
| 7 | 6.84 | 116.03 | 6.79 | 115.40 |
| 8 | 7.25 | 132.06 | 7.20 | 132.06 |
| 9 | 6.63 | 114.17 | 6.57 | 114.31 |
| 10 | 7.67 | 127.81 | 7.69 | 129.38 |
| 11 | − | 118.37 | − | 119.83 |
| 12 | − | 151.04 | − | 153.06 |
| 13 | 6.92 | 116.73 | 6.90 | 118.67 |
| 14 | 6.92 | 117.37 | 7.13 | 120.66 |
| 15 | − | 151.59 | − | 152.83 |
| 16 | 7.12 | 112.23 | 7.27 | 115.91 |
| OH | 11.02 | − | − | − |
| NH | 11.96 | − | − | − |
| OMe | 3.74 | 54.90 | 3.77 | 55.05 |
| NH2 | 6.54 | − | 7.00 | − |

N

H

2

5

6

7

8

9

1

0

H

C

N

N

C

O

H

O

H

1

1

1

2

1

3

1

4

1

5

1

2

3

4

1

6

CH3O

Scheme S4. The structural formula of H2L3 with the NMR numbering scheme

Table S12 1H and 13C chemical shifts (ppm) of H2L4 and 4.

| Atom | H2L4 |  | 4 |  |
| --- | --- | --- | --- | --- |
|  | δ / ppm (1H) | δ / ppm (13C) | δ / ppm (1H) | δ / ppm (13C) |
| 1 | 8.64 | 145.95 | 8.73 | 152.14 |
| 4 | − | 162.45 | − | 169.04 |
| 5 | − | 118.33 | − | 115.14 |
| 6 | 6.71 | 112.25 | 6.60 | 112.49 |
| 7 | 7.80 | 128.98 | 7.68 | 129.30 |
| 8 | − | 152.03 | − | 152.09 |
| 9 | 7.80 | 128.98 | 7.68 | 129.30 |
| 10 | 6.71 | 112.25 | 6.60 | 112.49 |
| 11 | − | 118.51 | − | 120.13 |
| 12 | − | 150.91 | − | 152.87 |
| 13 | 6.91 | 116.69 | 6.86 | 118.47 |
| 14 | 6.91 | 117.18 | 7.08 | 120.02 |
| 15 |  | 151.57 | − | 152.79 |
| 16 | 7.12 | 112.10 | 7.28 | 115.79 |
| OH | 11.03 | − | − | − |
| NH | 11.88 | − | − | − |
| OMe | 3.73 | 54.89 | 3.76 | 55.08 |
| NH2 | 5.89 | − | 5.93 | − |

N

H

2

5

6

7

8

9

1

0

H

C

N

N

C

O

H

O

H

1

1

1

2

1

3

1

4

1

5

1

2

3

4

1

6

CH3O

Scheme S5. The structural formula of H2L4 with the NMR numbering scheme

Figure S5. A portion of the 1H NMR spectra in dmso-d6 of: [MoO2(L1)]n (1) - blue line; H2L1 - red line, [MoO2(L1)]n (2) – green line , H2L2 – purple line

Figure S6. A portion of the 13C NMR spectra in dmso-d6 of: [MoO2(L1)]n (1) - blue line; H2L1 - red line, [MoO2(L1)]n (2) – green line , H2L2 – purple line

Figure S7. A portion of the 1H NMR spectra in dmso-d6 of: [MoO2(L3)]2 (3) - blue line; H2L3 - red line, [MoO2(L4)]2 (4) – green line, H2L4 – purple line

Figure S8. A portion of the 13C NMR spectra in dmso-d6 of: [MoO2(L3)]2 (3) - blue line; H2L3 - red line, [MoO2(L4)]2 (4) – green line, H2L4 – purple line

# Table S13. Imaginary frequency (cm−1) of the calculated transition states shown in Table S14.

|  | L1 | L2 | L3 | L4 |
| --- | --- | --- | --- | --- |
| TS | 471i | 470i | 473i | 476i |

# Table S14. DFT Coordinates of all species.

A -  DFT coordinates of organic molecules

A0-MeOH

8       -0.748606000     -0.122482000      0.000001000

6        0.661940000      0.019648000      0.000035000

1        1.036807000      0.543842000      0.893075000

1        1.036822000      0.543722000     -0.893232000

1        1.079608000     -0.990888000     -0.000013000

1       -1.136031000      0.765290000     -0.000051000

A1 – C2H4

6        0.000000000      0.665616000      0.000000000

1        0.923789000      1.239603000      0.000000000

1       -0.923751000      1.239647000      0.000000000

6        0.000000000     -0.665616000      0.000000000

1       -0.923789000     -1.239603000      0.000000000

1        0.923751000     -1.239647000      0.000000000

A2– epo

6        0.000000000      0.823033000      0.000000000

6        0.663277000     -0.487998000      0.000000000

1       -0.044284000      1.406100000      0.920513000

1        1.105429000     -0.869573000      0.920803000

8       -0.762744000     -0.385408000      0.000000000

1       -0.044284000      1.406100000     -0.920513000

1        1.105429000     -0.869573000     -0.920803000

A3 – TBHP

6        0.386063000      0.000211000      0.035516000

8       -0.724877000     -0.051131000     -0.892876000

8       -1.972121000      0.107335000     -0.155683000

6        1.585594000     -0.148364000     -0.908710000

6        0.308477000     -1.169459000      1.023961000

6        0.408392000      1.352799000      0.755437000

1       -2.332288000     -0.792908000     -0.245178000

1        1.280879000      1.423828000      1.414956000

1        1.184972000     -1.179544000      1.681110000

1        2.518340000     -0.109351000     -0.336278000

1       -0.583795000     -1.085739000      1.651566000

1        0.273436000     -2.124477000      0.486863000

1        1.545636000     -1.103632000     -1.442442000

1        1.596327000      0.660559000     -1.645981000

1        0.455220000      2.169404000      0.027401000

1       -0.493901000      1.481099000      1.359235000

A4 – tBuOH

6       -0.005589000     -0.000026000      0.014420000

8        0.015118000     -0.000431000      1.451985000

1        0.945639000      0.001902000      1.728630000

6       -1.490947000     -0.005338000     -0.356041000

6        0.694937000     -1.262772000     -0.510972000

6        0.685524000      1.268259000     -0.510112000

1        0.646742000      1.325318000     -1.604317000

1        0.656167000     -1.319650000     -1.605180000

1       -1.623187000     -0.004815000     -1.443350000

1        1.752964000     -1.271531000     -0.216357000

1        0.219546000     -2.158915000     -0.098630000

1       -1.981082000     -0.894002000      0.055230000

1       -1.987701000      0.878867000      0.056897000

1        0.203120000      2.160551000     -0.097564000

1        1.743307000      1.284985000     -0.215007000

B- DFT coordinates for TBHP as oxidant – Gas phase

B1 - With Ligand L1

MoO2L1(MeOH)

42       0.287666000     -1.514676000     -0.504120000

8        2.144014000     -0.752365000     -0.294954000

8       -1.565353000     -1.411090000      0.082883000

8        0.645363000     -1.424014000      2.021257000

1        1.022133000     -2.319978000      2.057454000

8       -5.624978000      2.342528000     -0.094947000

8        0.108712000     -1.406015000     -2.185325000

8        0.703090000     -3.125229000     -0.109334000

7        0.142879000      0.712702000     -0.023676000

7        6.385133000      1.929815000      0.010732000

7        1.345001000      1.380290000      0.076735000

6        3.724151000      1.024081000     -0.060427000

6       -2.272172000      0.906463000      0.014416000

6       -2.539511000     -0.488793000     -0.007227000

6       -4.921762000     -0.010062000     -0.100932000

1       -5.937399000     -0.385934000     -0.149143000

6       -4.666595000      1.371263000     -0.070131000

6        2.328295000      0.539090000     -0.096256000

6       -3.867804000     -0.921211000     -0.066366000

1       -4.060855000     -1.988940000     -0.081053000

6        4.790253000      0.138240000     -0.253309000

1        4.603904000     -0.914183000     -0.434553000

6       -3.346895000      1.813422000     -0.007801000

1       -3.157402000      2.882601000      0.012215000

6        4.018770000      2.375365000      0.167166000

1        3.219202000      3.091178000      0.319357000

6       -0.931308000      1.434271000      0.079755000

1       -0.800238000      2.509051000      0.212184000

6        6.090244000      0.642697000     -0.208336000

1        6.938353000     -0.023687000     -0.356031000

6        5.354420000      2.768014000      0.193007000

1        5.612969000      3.810804000      0.368842000

6       -6.984409000      1.943800000     -0.175304000

1       -7.184752000      1.374025000     -1.092380000

1       -7.565691000      2.867247000     -0.191324000

1       -7.282326000      1.344269000      0.695383000

6       -0.414593000     -1.326707000      2.981485000

1       -1.206470000     -2.056779000      2.782677000

1       -0.825328000     -0.320143000      2.892063000

1       -0.022459000     -1.462911000      3.995748000

MoO2L1

42       0.300712000      1.662152000      0.087558000

8        2.131126000      0.868342000     -0.157018000

8       -1.543841000      1.455504000     -0.481142000

8       -5.630245000     -2.209257000      0.156519000

8        0.225834000      1.990496000      1.749401000

8        0.669789000      3.074243000     -0.778435000

7        0.145197000     -0.600811000     -0.069358000

7        6.392482000     -1.800863000     -0.007601000

7        1.342419000     -1.288922000     -0.067994000

6        3.727298000     -0.912974000     -0.059047000

6       -2.270159000     -0.815108000     -0.092462000

6       -2.530092000      0.566999000     -0.284022000

6       -4.911996000      0.114421000     -0.177960000

1       -5.926944000      0.493371000     -0.212643000

6       -4.664984000     -1.258787000      0.006929000

6        2.330083000     -0.438522000     -0.086999000

6       -3.855864000      1.009770000     -0.324720000

1       -4.042961000      2.067151000     -0.479305000

6        4.788157000     -0.000879000     -0.095367000

1        4.596485000      1.064921000     -0.144699000

6       -3.348662000     -1.710094000      0.042008000

1       -3.163758000     -2.770657000      0.183887000

6        4.028122000     -2.280661000      0.003791000

1        3.232849000     -3.016664000      0.033977000

6       -0.932089000     -1.334077000     -0.063664000

1       -0.790437000     -2.414537000     -0.028710000

6        6.091498000     -0.498081000     -0.066703000

1        6.936485000      0.187537000     -0.093181000

6        5.366646000     -2.663593000      0.026201000

1        5.631457000     -3.718319000      0.074453000

6       -6.990511000     -1.802689000      0.126139000

1       -7.220071000     -1.099047000      0.937103000

1       -7.575795000     -2.713181000      0.263920000

1       -7.253897000     -1.345764000     -0.836904000

MoO2L1(TBHP)

42      -0.200539000      0.318714000      1.597070000

8       -2.024500000     -0.201903000      0.966892000

8        1.608686000      0.708141000      1.024988000

8        5.803066000     -2.129558000     -1.192853000

8        0.041564000     -0.744004000      2.890367000

8       -0.669602000      1.848953000      2.211773000

7       -0.013600000     -1.090092000     -0.170877000

7       -6.229456000     -2.188571000     -0.943908000

7       -1.197745000     -1.590814000     -0.669697000

6       -3.584013000     -1.467361000     -0.331038000

6        2.403221000     -1.113035000     -0.353952000

6        2.624092000     -0.012739000      0.515019000

6        5.019590000     -0.312918000      0.259861000

1        6.022983000      0.010651000      0.511591000

6        4.811631000     -1.400696000     -0.606453000

6       -2.197538000     -1.081243000     -0.005342000

6        3.935696000      0.370678000      0.806967000

1        4.091723000      1.217242000      1.467378000

6       -4.662057000     -0.870418000      0.332002000

1       -4.490959000     -0.114728000      1.089856000

6        3.507130000     -1.784758000     -0.909567000

1        3.353729000     -2.624875000     -1.580252000

6       -3.857347000     -2.433641000     -1.308963000

1       -3.047878000     -2.917216000     -1.843669000

6        1.077558000     -1.543009000     -0.714226000

1        0.966198000     -2.300338000     -1.490558000

6       -5.954430000     -1.266983000     -0.012965000

1       -6.812487000     -0.819200000      0.485038000

6       -5.187156000     -2.751683000     -1.571865000

1       -5.430702000     -3.498357000     -2.325648000

6        7.151290000     -1.782421000     -0.914035000

1        7.379881000     -1.878801000      0.155530000

1        7.762936000     -2.488655000     -1.477697000

1        7.381652000     -0.760722000     -1.243916000

1       -1.608235000      2.793260000      0.905892000

8       -1.969909000      2.861220000     -0.006449000

8       -0.978379000      2.057130000     -0.708141000

6       -0.224636000      2.926920000     -1.606441000

6       -1.194558000      3.604470000     -2.580376000

1       -1.771308000      2.852762000     -3.129558000

1       -1.892277000      4.251078000     -2.043607000

1       -0.639555000      4.213424000     -3.302930000

1       -0.085268000      4.592289000     -0.219613000

6        0.582107000      3.947216000     -0.797521000

6        0.689837000      1.944232000     -2.344124000

1        0.098899000      1.170252000     -2.844729000

1        1.268678000      2.481437000     -3.103008000

1        1.391556000      1.465065000     -1.655898000

1        1.174608000      4.581387000     -1.466535000

1        1.264143000      3.438893000     -0.107737000

TS

42       0.442669000      1.041296000      1.399288000

8       -1.297058000      0.222217000      0.762924000

8        2.262441000      1.562163000      0.968882000

8        0.823365000     -0.103332000      2.587051000

8       -0.265388000      2.377284000      2.246976000

7       -0.213692000     -1.109378000     -0.784762000

6       -2.606265000     -1.262673000     -0.573088000

6        4.608964000      1.336513000      1.037660000

1        4.643792000      2.243597000      1.632155000

6        4.492533000     -0.972672000     -0.510705000

1        4.462302000     -1.873645000     -1.116291000

7        0.882208000     -0.471353000     -0.246799000

6        3.358701000      0.854101000      0.639821000

8        6.821893000     -1.204704000     -0.505143000

6        3.296795000     -0.328428000     -0.148220000

6       -4.986441000     -1.447360000     -0.304802000

6        2.050737000     -0.887780000     -0.620818000

1        2.088540000     -1.719204000     -1.325891000

7       -5.104317000     -2.335884000     -1.298898000

6       -3.976699000     -2.692807000     -1.930935000

1       -4.090186000     -3.416930000     -2.735913000

6       -1.297445000     -0.691919000     -0.185850000

6        8.107435000     -0.751035000     -0.113122000

1        8.319942000      0.251977000     -0.507035000

1        8.217006000     -0.740544000      0.979589000

1        8.817666000     -1.462082000     -0.538671000

6        5.784395000      0.677881000      0.681299000

1        6.733272000      1.082213000      1.014725000

6       -3.775440000     -0.883048000      0.095606000

1       -3.732266000     -0.169194000      0.910130000

6       -2.715238000     -2.195964000     -1.612891000

1       -1.831916000     -2.517190000     -2.152629000

6        5.732862000     -0.487931000     -0.099831000

1       -1.040647000      3.265236000      1.071115000

8       -1.471127000      3.520047000      0.206803000

8       -0.114032000      2.395103000     -0.494736000

1        2.002054000      4.048337000     -0.298402000

6        1.226805000      4.363867000     -1.004057000

6        0.480970000      3.138795000     -1.557296000

6       -0.616658000      3.560768000     -2.550804000

1       -0.177164000      4.056566000     -3.424403000

1       -1.171912000      2.681278000     -2.894007000

1       -1.320022000      4.251900000     -2.079638000

1        0.529640000      5.024249000     -0.479242000

1        1.701931000      4.934702000     -1.811085000

6        1.464223000      2.201559000     -2.289119000

1        2.293474000      1.910033000     -1.642160000

1        0.948163000      1.300933000     -2.635751000

1        1.880153000      2.718628000     -3.162021000

1       -2.248779000      5.059022000      2.283639000

6       -2.671760000      4.974449000      1.287686000

1       -2.642405000      5.853075000      0.653307000

6       -3.172748000      3.775675000      0.824385000

1       -3.316919000      2.936361000      1.497123000

1       -3.710342000      3.725682000     -0.115929000

1       -5.910399000     -1.170967000      0.200777000

MoO(OR)(OH)L1

42       0.186435000      0.907250000     -1.131216000

8        2.016452000      0.090270000     -0.896490000

8       -1.662138000      1.091154000     -0.580431000

8       -5.779218000     -2.366780000      0.691713000

8       -0.240146000     -0.092879000     -2.437374000

8        0.731849000      2.373588000     -2.215740000

7        0.014876000     -0.913235000      0.187339000

7        6.192126000     -2.427989000      0.329053000

7        1.201857000     -1.534986000      0.515042000

6        3.565384000     -1.467964000      0.039680000

6       -2.408186000     -1.031837000      0.282622000

6       -2.655587000      0.226622000     -0.327243000

6       -5.040132000     -0.233480000     -0.274131000

1       -6.048430000      0.091682000     -0.503548000

6       -4.806801000     -1.476606000      0.336563000

6        2.188009000     -0.953915000     -0.114115000

6       -3.973898000      0.605252000     -0.594932000

1       -4.151223000      1.571066000     -1.056440000

6        4.628303000     -0.871621000     -0.647981000

1        4.452637000     -0.028853000     -1.306896000

6       -3.495608000     -1.859176000      0.612975000

1       -3.323602000     -2.824210000      1.080364000

6        3.845114000     -2.558015000      0.874868000

1        3.047144000     -3.046983000      1.421721000

6       -1.074942000     -1.498336000      0.578718000

1       -0.963810000     -2.425013000      1.142035000

6        5.910989000     -1.389807000     -0.467621000

1        6.756152000     -0.946336000     -0.991273000

6        5.164436000     -2.990608000      0.981289000

1        5.411477000     -3.834112000      1.623626000

6       -7.129120000     -2.034979000      0.408785000

1       -7.294291000     -1.898003000     -0.668238000

1       -7.724017000     -2.880172000      0.759187000

1       -7.443373000     -1.126979000      0.940969000

1        1.086908000      3.092968000     -1.663392000

8        0.596799000      1.983677000      0.432459000

6        0.667506000      2.571289000      1.718172000

6        1.787028000      1.868304000      2.504726000

1        1.571753000      0.799117000      2.601772000

1        2.745561000      1.980206000      1.987003000

1        1.883789000      2.295529000      3.509582000

1        1.946977000      4.185338000      1.009410000

6        0.991801000      4.064075000      1.533006000

6       -0.688612000      2.397955000      2.422652000

1       -0.924096000      1.336073000      2.547631000

1       -0.670123000      2.865762000      3.413921000

1       -1.487549000      2.858870000      1.833593000

1        1.066166000      4.572131000      2.501239000

1        0.206776000      4.555736000      0.947478000

B2 - With Ligand L2

MoO2L2(MeOH)

42       0.227751000     -1.433078000     -0.567858000

8        2.073895000     -0.662662000     -0.318689000

8       -1.591271000     -1.405056000      0.157720000

8       -0.053075000     -1.132358000     -2.212166000

8        0.479929000     -1.466194000      1.918391000

1       -0.406082000     -1.789601000      2.152923000

8        0.652908000     -3.076516000     -0.403993000

7        1.256893000      1.450529000      0.143995000

6        3.633354000      1.127048000     -0.056774000

6       -3.904607000     -0.957226000      0.030592000

1       -4.072336000     -2.028624000     -0.010928000

6       -3.446520000      1.783795000      0.159802000

1       -3.282333000      2.856316000      0.206703000

7        0.061775000      0.774329000      0.043272000

6       -2.586729000     -0.496055000      0.091742000

8       -5.736849000      2.262990000      0.103728000

6       -2.350167000      0.903958000      0.147546000

7        5.990865000      0.642239000     -0.272890000

6       -1.020859000      1.466334000      0.210944000

1       -0.915152000      2.536532000      0.394778000

6        6.241812000      1.934165000     -0.028667000

1        7.291627000      2.223447000     -0.023684000

6        5.245937000      2.886457000      0.209673000

1        5.511010000      3.922010000      0.400397000

6        2.246717000      0.628314000     -0.080816000

6       -7.086816000      1.835467000      0.018133000

1       -7.367120000      1.205717000      0.873289000

1       -7.278390000      1.285959000     -0.913172000

1       -7.689505000      2.745236000      0.029487000

6       -4.981085000     -0.071689000      0.028955000

1       -5.987930000     -0.470045000     -0.021797000

6        4.710765000      0.256689000     -0.285892000

1        4.520160000     -0.793499000     -0.489643000

6        1.473600000     -2.315568000      2.519210000

1        1.366720000     -3.349131000      2.176459000

1        1.405553000     -2.259946000      3.611151000

1        2.440001000     -1.929082000      2.195018000

6        3.918334000      2.477206000      0.195791000

1        3.104358000      3.171576000      0.374173000

6       -4.756598000      1.312954000      0.095484000

MoO2L2

42      -0.305616000     -1.655195000      0.089458000

8       -2.133738000     -0.859062000     -0.155329000

8        1.538174000     -1.453051000     -0.483503000

8       -0.227376000     -1.979417000      1.752115000

8       -0.676160000     -3.069255000     -0.772685000

7       -1.341901000      1.297720000     -0.068623000

6       -3.724191000      0.924208000     -0.057964000

6        3.851473000     -1.013441000     -0.328394000

1        4.035379000     -2.071179000     -0.484508000

6        3.351444000      1.706642000      0.042341000

1        3.169617000      2.767562000      0.185720000

7       -0.146186000      0.608238000     -0.069657000

6        2.526950000     -0.567145000     -0.286183000

8        5.634626000      2.200171000      0.156283000

6        2.270458000      0.815100000     -0.092879000

7       -6.076144000      0.376414000     -0.081431000

6        0.933175000      1.337902000     -0.063715000

1        0.795226000      2.418855000     -0.028494000

6       -6.343911000      1.686308000     -0.016287000

1       -7.398449000      1.957115000     -0.001236000

6       -5.359803000      2.678904000      0.031781000

1       -5.639077000      3.726756000      0.084864000

6       -2.332564000      0.448533000     -0.085966000

6        6.993452000      1.789627000      0.125278000

1        7.255608000      1.333213000     -0.838392000

1        7.221019000      1.083937000      0.935075000

1        7.581709000      2.698050000      0.264430000

6        4.910395000     -0.121346000     -0.181109000

1        5.924301000     -0.502963000     -0.216961000

6       -4.790651000      0.011790000     -0.101728000

1       -4.586378000     -1.053995000     -0.155763000

6       -4.025681000      2.292670000      0.011234000

1       -3.220960000      3.019277000      0.047036000

6        4.666669000      1.251891000      0.005908000

MoO2L2(TBHP)

42      -0.207381000      0.305002000      1.593394000

8       -2.029337000     -0.212509000      0.958198000

8        1.602777000      0.700210000      1.027465000

8        0.034918000     -0.764556000      2.881248000

8       -0.678043000      1.831871000      2.215004000

7       -1.199943000     -1.588418000     -0.688520000

6       -3.583455000     -1.470806000     -0.348822000

6        3.930465000      0.364367000      0.813717000

1        4.084343000      1.207090000      1.479551000

6        3.506568000     -1.780738000     -0.916094000

1        3.355239000     -2.616987000     -1.592096000

7       -0.017278000     -1.091607000     -0.184282000

6        2.619719000     -0.017555000      0.515979000

8        5.803536000     -2.123932000     -1.195610000

6        2.400995000     -1.112560000     -0.359885000

7       -5.944158000     -1.186887000      0.073384000

6        1.075873000     -1.540323000     -0.726814000

1        0.967556000     -2.292620000     -1.508457000

6       -6.185415000     -2.102752000     -0.872531000

1       -7.233640000     -2.333498000     -1.056220000

6       -5.182695000     -2.747665000     -1.603483000

1       -5.440884000     -3.482511000     -2.359927000

6       -2.202681000     -1.085229000     -0.020866000

6        7.150613000     -1.778415000     -0.910465000

1        7.382077000     -0.754661000     -1.233276000

1        7.375953000     -1.881081000      0.159247000

1        7.764332000     -2.481107000     -1.476387000

6        5.016182000     -0.315706000      0.265696000

1        6.018827000      0.006524000      0.522063000

6       -4.667062000     -0.882296000      0.322876000

1       -4.483604000     -0.133531000      1.088220000

6       -3.857368000     -2.427682000     -1.337293000

1       -3.038713000     -2.897051000     -1.872283000

6        4.810278000     -1.398255000     -0.607301000

1       -1.617373000      2.780067000      0.910837000

8       -1.971204000      2.857565000     -0.003794000

8       -0.974284000      2.060823000     -0.705976000

1        1.267035000      3.430102000     -0.072621000

6        0.590490000      3.948486000     -0.760293000

6       -0.212437000      2.940081000     -1.587776000

6       -1.173718000      3.632125000     -2.560144000

1       -0.611880000      4.247751000     -3.271753000

1       -1.749042000      2.888644000     -3.121919000

1       -1.873162000      4.274495000     -2.020569000

1       -0.080002000      4.586697000     -0.178401000

1        1.188414000      4.590620000     -1.416831000

6        0.705243000      1.964849000     -2.331320000

1        1.399836000      1.474333000     -1.643979000

1        0.116094000      1.199319000     -2.846858000

1        1.291761000      2.510394000     -3.078340000

TS

42       0.455243000      1.040208000      1.400969000

8       -1.285749000      0.222523000      0.770933000

8        2.273682000      1.560220000      0.965164000

8        0.836832000     -0.096869000      2.595945000

8       -0.251758000      2.383278000      2.237539000

7       -0.208514000     -1.111874000     -0.779002000

6       -2.600691000     -1.244880000     -0.573792000

6        4.620400000      1.334207000      1.029025000

1        4.656510000      2.242889000      1.621025000

6        4.499715000     -0.978340000     -0.513086000

1        4.468105000     -1.880701000     -1.116572000

7        0.889521000     -0.478335000     -0.241342000

6        3.369246000      0.850832000      0.635444000

8        6.829324000     -1.210725000     -0.513405000

6        3.304927000     -0.333465000     -0.149383000

7       -4.996727000     -1.268115000     -0.252037000

6        2.057212000     -0.893304000     -0.618819000

1        2.094021000     -1.723620000     -1.325288000

6       -5.082094000     -2.184727000     -1.224175000

1       -6.084801000     -2.537519000     -1.460761000

6       -3.975575000     -2.684820000     -1.917049000

1       -4.106886000     -3.430193000     -2.695693000

6       -1.292008000     -0.689453000     -0.180584000

6        8.115637000     -0.755513000     -0.126469000

1        8.326552000      0.246692000     -0.523391000

1        8.228630000     -0.742084000      0.965897000

1        8.825111000     -1.467198000     -0.552330000

6        5.795215000      0.674873000      0.671440000

1        6.744911000      1.080107000      1.001416000

6       -3.777510000     -0.816524000      0.058972000

1       -3.719268000     -0.077031000      0.852792000

6       -2.712653000     -2.207896000     -1.587048000

1       -1.819162000     -2.559380000     -2.091624000

6        5.741237000     -0.492604000     -0.106598000

1       -1.059157000      3.238518000      1.049310000

8       -1.500845000      3.463120000      0.182786000

8       -0.109048000      2.375078000     -0.508849000

1        1.983992000      4.054471000     -0.267693000

6        1.212185000      4.367214000     -0.978344000

6        0.489906000      3.138534000     -1.554453000

6       -0.599630000      3.557840000     -2.558074000

1       -0.154633000      4.067803000     -3.420726000

1       -1.139822000      2.675362000     -2.917339000

1       -1.317389000      4.235429000     -2.089006000

1        0.499425000      5.011083000     -0.453766000

1        1.687949000      4.954899000     -1.772811000

6        1.494093000      2.220864000     -2.283006000

1        2.316544000      1.929908000     -1.627324000

1        0.992457000      1.318941000     -2.647170000

1        1.917168000      2.752313000     -3.143841000

1       -2.338151000      4.997000000      2.242214000

6       -2.758431000      4.882457000      1.248085000

1       -2.765853000      5.753422000      0.602559000

6       -3.211295000      3.658517000      0.801309000

1       -3.320625000      2.822402000      1.484479000

1       -3.747702000      3.574369000     -0.137212000

MoO(OR)(OH)L2

42       0.189384000      0.895975000     -1.132356000

8        2.015564000      0.073076000     -0.900397000

8       -1.656332000      1.093366000     -0.572913000

8       -0.254067000     -0.107160000     -2.430513000

8        0.739619000      2.353103000     -2.226504000

7        1.200615000     -1.538885000      0.526472000

6        3.561081000     -1.477920000      0.048753000

6       -3.969491000      0.613059000     -0.591192000

1       -4.143494000      1.579159000     -1.053415000

6       -3.499114000     -1.851397000      0.618695000

1       -3.330424000     -2.816592000      1.087018000

7        0.014942000     -0.918042000      0.194639000

6       -2.652514000      0.231181000     -0.321576000

8       -5.784311000     -2.353588000      0.694622000

6       -2.409052000     -1.027421000      0.289364000

7        5.901083000     -1.277039000     -0.517697000

6       -1.076988000     -1.497021000      0.588522000

1       -0.969718000     -2.421304000      1.156542000

6        6.145024000     -2.329757000      0.272339000

1        7.185415000     -2.643963000      0.340543000

6        5.153355000     -3.012686000      0.983246000

1        5.412202000     -3.862184000      1.608025000

6        2.188601000     -0.964950000     -0.109110000

6       -7.132591000     -2.018564000      0.408888000

1       -7.445781000     -1.109491000      0.939960000

1       -7.295406000     -1.881456000     -0.668518000

1       -7.730513000     -2.862056000      0.758384000

6       -5.038626000     -0.222548000     -0.271517000

1       -6.045752000      0.105109000     -0.502545000

6        4.632814000     -0.867546000     -0.621316000

1        4.447106000     -0.013888000     -1.267525000

6        3.837656000     -2.580601000      0.869959000

1        3.027433000     -3.072467000      1.397429000

6       -4.809003000     -1.465661000      0.340127000

1        1.107484000      3.070913000     -1.680544000

8        0.608652000      1.979179000      0.425075000

1        0.214119000      4.553207000      0.927413000

6        0.997892000      4.064905000      1.517393000

6        0.674250000      2.572629000      1.708042000

6        1.792222000      1.874179000      2.501030000

1        1.885723000      2.305801000      3.504376000

1        1.577320000      0.805222000      2.601702000

1        2.752054000      1.984738000      1.985425000

1        1.954350000      4.184616000      0.995845000

1        1.069067000      4.577310000      2.483613000

6       -0.683429000      2.401414000      2.410132000

1       -1.481343000      2.858985000      1.817186000

1       -0.918487000      1.339921000      2.539137000

1       -0.667497000      2.873652000      3.399391000

B3 - With Ligand L3

[MoO2L3]2

42       2.205517000     -2.731399000     -0.540364000

8        2.817790000     -3.208164000      1.240762000

8        1.156231000     -1.419242000     -1.671221000

7        2.323864000     -0.650453000      0.398865000

8        5.935074000     -0.881489000      5.174129000

8        3.679566000     -2.658741000     -1.378363000

7        1.724036000      0.359021000     -0.324667000

8        1.381050000     -4.144093000     -1.029451000

7        0.106432000      2.601149000     -0.827563000

1        0.234161000      3.609205000     -0.785899000

1        0.774089000      2.132123000     -0.212227000

6        1.173735000     -0.126540000     -1.411972000

6        0.584587000      0.770357000     -2.425859000

6       -0.341046000      2.409655000     -4.504859000

1       -0.691497000      3.057478000     -5.303652000

6       -0.284970000      2.899073000     -3.204145000

1       -0.611132000      3.912185000     -2.986899000

6        3.686716000     -1.217590000      2.319712000

6        0.495384000      0.287792000     -3.744946000

1        0.812337000     -0.731127000     -3.937586000

6        0.041150000      1.093682000     -4.781065000

1       -0.006610000      0.704774000     -5.793482000

6        2.976767000     -0.298689000      1.463105000

1        3.007126000      0.763725000      1.708114000

6        0.165815000      2.095705000     -2.146880000

6        4.476593000     -0.686004000      3.353840000

1        4.540907000      0.389271000      3.491671000

6        3.608303000     -2.626665000      2.160525000

6        5.124375000     -2.903983000      4.041795000

1        5.674605000     -3.573882000      4.692670000

6        4.335393000     -3.446086000      3.028332000

1        4.267621000     -4.521276000      2.897915000

6        5.198071000     -1.512258000      4.213312000

6        6.695832000     -1.677969000      6.067838000

1        7.446683000     -2.278097000      5.536575000

1        6.055672000     -2.344212000      6.661894000

1        7.201864000     -0.977887000      6.734852000

42      -2.205517000      2.731399000      0.540364000

8       -2.817790000      3.208164000     -1.240762000

8       -1.156231000      1.419242000      1.671221000

7       -2.323864000      0.650453000     -0.398865000

8       -5.935074000      0.881489000     -5.174129000

8       -3.679566000      2.658741000      1.378363000

7       -1.724036000     -0.359021000      0.324667000

8       -1.381050000      4.144093000      1.029451000

7       -0.106432000     -2.601149000      0.827563000

1       -0.234161000     -3.609205000      0.785899000

1       -0.774089000     -2.132123000      0.212227000

6       -1.173735000      0.126540000      1.411972000

6       -0.584587000     -0.770357000      2.425859000

6        0.341046000     -2.409655000      4.504859000

1        0.691497000     -3.057478000      5.303652000

6        0.284970000     -2.899073000      3.204145000

1        0.611132000     -3.912185000      2.986899000

6       -3.686716000      1.217590000     -2.319712000

6       -0.495384000     -0.287792000      3.744946000

1       -0.812337000      0.731127000      3.937586000

6       -0.041150000     -1.093682000      4.781065000

1        0.006610000     -0.704774000      5.793482000

6       -2.976767000      0.298689000     -1.463105000

1       -3.007126000     -0.763725000     -1.708114000

6       -0.165815000     -2.095705000      2.146880000

6       -4.476593000      0.686004000     -3.353840000

1       -4.540907000     -0.389271000     -3.491671000

6       -3.608303000      2.626665000     -2.160525000

6       -5.124375000      2.903983000     -4.041795000

1       -5.674605000      3.573882000     -4.692670000

6       -4.335393000      3.446086000     -3.028332000

1       -4.267621000      4.521276000     -2.897915000

6       -5.198071000      1.512258000     -4.213312000

6       -6.695832000      1.677969000     -6.067838000

1       -7.446683000      2.278097000     -5.536575000

1       -6.055672000      2.344212000     -6.661894000

1       -7.201864000      0.977887000     -6.734852000

MoO2L3(MeOH)

42       0.057873000     -1.618291000     -0.533534000

8        1.887717000     -0.844000000     -0.283766000

8       -1.771613000     -1.573380000      0.173124000

8        0.474209000     -3.259324000     -0.319938000

8        0.274583000     -1.592025000      1.960913000

1       -0.605100000     -1.936810000      2.188434000

7        2.940980000      3.240904000      0.489648000

8       -6.058498000      1.911472000     -0.004680000

7        1.078609000      1.275537000      0.111170000

7       -0.113800000      0.601375000      0.015236000

8       -0.213333000     -1.363912000     -2.188027000

6       -2.763951000     -0.666608000      0.082409000

6        2.089380000      0.453996000     -0.083638000

6       -3.632093000      1.618192000      0.075813000

1       -3.430059000      2.683603000      0.089460000

6        3.851219000      2.273659000      0.157449000

6       -2.530516000      0.728978000      0.094061000

6       -4.934570000      1.137343000      0.026807000

6        4.488477000     -0.032013000     -0.362460000

1        4.182820000     -1.055857000     -0.545085000

6        3.478238000      0.915011000     -0.084988000

6        5.223156000      2.608811000      0.087157000

1        5.512338000      3.641509000      0.269130000

6       -1.202807000      1.292319000      0.151289000

1       -1.104341000      2.368268000      0.305812000

6       -4.087039000     -1.136723000      0.037188000

1       -4.250437000     -2.209509000      0.029248000

6       -5.153353000     -0.253835000      0.007316000

1       -6.176411000     -0.614645000     -0.030483000

6        5.826418000      0.318519000     -0.419149000

1        6.581476000     -0.429270000     -0.639740000

6        1.282964000     -2.401941000      2.589797000

1        2.242359000     -1.993541000      2.271726000

1        1.209490000     -3.444088000      2.264205000

1        1.198636000     -2.329815000      3.679767000

6       -5.898842000      3.320075000     -0.001237000

1       -5.332759000      3.663679000     -0.877623000

1       -5.395775000      3.667113000      0.911656000

1       -6.906794000      3.737028000     -0.037173000

6        6.187110000      1.656013000     -0.194384000

1        7.231642000      1.954016000     -0.239503000

1        3.225160000      4.205496000      0.404762000

1        1.959310000      3.014916000      0.369868000

MoO2L3

42      -0.115035000     -1.827918000      0.101699000

8       -1.924330000     -1.035092000     -0.176508000

8        1.732765000     -1.639083000     -0.475948000

8       -0.474294000     -3.267582000     -0.724204000

7       -3.024632000      3.108147000     -0.118635000

8        5.983885000      1.830543000      0.093248000

7       -1.141638000      1.116841000     -0.106359000

7        0.051364000      0.430582000     -0.091233000

8       -0.034828000     -2.109597000      1.772886000

6        2.721176000     -0.752928000     -0.293456000

6       -2.152179000      0.273987000     -0.117867000

6        3.560837000      1.525930000      0.010016000

1        3.345394000      2.580547000      0.141312000

6       -3.930535000      2.085294000     -0.052271000

6        2.471771000      0.627106000     -0.114800000

6        4.866946000      1.058291000     -0.026502000

6       -4.548005000     -0.285765000     -0.073117000

1       -4.231906000     -1.322078000     -0.105237000

6       -3.544556000      0.709090000     -0.087153000

6       -5.310547000      2.385952000      0.016512000

1       -5.611047000      3.430884000      0.044714000

6        1.136976000      1.153027000     -0.094416000

1        1.007326000      2.235763000     -0.076716000

6        4.049429000     -1.210591000     -0.336811000

1        4.225316000     -2.271208000     -0.481801000

6        5.101268000     -0.322354000     -0.202023000

1        6.129842000     -0.667923000     -0.231410000

6       -5.892502000      0.033934000     -0.012373000

1       -6.643357000     -0.749435000      0.000068000

6        5.814837000      3.227283000      0.274319000

1        5.261409000      3.449209000      1.196715000

1        5.294396000      3.683687000     -0.578500000

1        6.820509000      3.644284000      0.347907000

6       -6.267248000      1.386153000      0.036160000

1       -7.318432000      1.658202000      0.088267000

1       -3.332017000      4.033960000      0.138895000

1       -2.043242000      2.877714000     -0.015095000

MoO2L3(TBHP)

42      -0.074846000     -0.702266000     -1.570721000

8       -1.882163000     -0.127859000     -0.990991000

8        1.748064000     -0.979024000     -0.963726000

8       -0.512181000     -2.316630000     -1.952027000

7       -2.926458000      3.125829000      1.597143000

8        6.071045000      2.091713000      0.570473000

7       -1.071105000      1.522250000      0.377586000

7        0.112146000      0.969213000     -0.049351000

8        0.144258000      0.163385000     -3.008253000

6        2.756950000     -0.170713000     -0.597444000

6       -2.091233000      0.903294000     -0.179404000

6        3.642306000      1.830575000      0.492840000

1        3.448798000      2.762635000      1.012108000

6       -3.842622000      2.401966000      0.884804000

6        2.534882000      1.051321000      0.077360000

6        4.939793000      1.412545000      0.227061000

6       -4.491025000      0.566624000     -0.603375000

1       -4.189729000     -0.270798000     -1.221818000

6       -3.475681000      1.300050000      0.050707000

6       -5.215333000      2.722946000      0.994918000

1       -5.500903000      3.561860000      1.625532000

6        1.209332000      1.515062000      0.389269000

1        1.104983000      2.388317000      1.034229000

6        4.074608000     -0.586704000     -0.849929000

1        4.228543000     -1.530049000     -1.363231000

6        5.146196000      0.192363000     -0.448932000

1        6.166973000     -0.120165000     -0.645098000

6       -5.828346000      0.895012000     -0.472888000

1       -6.588789000      0.315719000     -0.986468000

6        5.928264000      3.333612000      1.240823000

1        5.373182000      4.058535000      0.630390000

1        5.422885000      3.213438000      2.208643000

1        6.941493000      3.702986000      1.407181000

6       -6.183611000      1.988677000      0.332707000

1       -7.228857000      2.265793000      0.444359000

1       -3.211507000      4.016815000      1.974859000

1       -1.944830000      2.974872000      1.395431000

8       -1.710506000     -3.103577000      0.409472000

8       -0.767673000     -2.153097000      0.983964000

6        0.021329000     -2.836333000      2.001866000

6       -0.919078000     -3.400408000      3.072716000

1       -1.579953000     -4.157622000      2.645136000

1       -1.536606000     -2.601364000      3.496283000

1       -0.338797000     -3.858490000      3.881826000

1        0.244954000     -4.694255000      0.901321000

6        0.879205000     -3.930441000      1.359401000

1        1.529559000     -3.505137000      0.587810000

1        1.507863000     -4.415528000      2.114839000

1        1.565397000     -1.307822000      1.819564000

6        0.884819000     -1.708347000      2.575973000

1        0.254893000     -0.895155000      2.951456000

1        1.485402000     -2.092323000      3.407523000

1       -1.364792000     -3.124047000     -0.511376000

TS

42      -0.064539000     -0.909551000     -1.057168000

8       -1.786167000     -0.047263000     -0.482234000

8        1.765330000     -1.380003000     -0.595267000

8       -0.775696000     -2.334582000     -1.742235000

7       -2.301748000      3.058415000      2.422216000

8        6.441924000      1.390878000      0.393360000

7       -0.708127000      1.427772000      0.917347000

7        0.384495000      0.758957000      0.422788000

8        0.304965000      0.097467000     -2.367427000

6        2.858727000     -0.634686000     -0.360998000

6       -1.815201000      0.956918000      0.378323000

6        4.003849000      1.314575000      0.568968000

1        3.937426000      2.270964000      1.076039000

6       -3.322245000      2.565926000      1.653245000

6        2.801707000      0.618796000      0.295695000

6        5.232649000      0.791428000      0.186085000

6       -4.245457000      1.039437000     -0.019853000

1       -4.071696000      0.257671000     -0.750363000

6       -3.127967000      1.529188000      0.688967000

6       -4.632802000      3.063187000      1.840181000

1       -4.785996000      3.851905000      2.573474000

6        1.559439000      1.211305000      0.733538000

1        1.607569000      2.105971000      1.356505000

6        4.110395000     -1.155635000     -0.730158000

1        4.138460000     -2.120803000     -1.225151000

6        5.275600000     -0.455469000     -0.467333000

1        6.243236000     -0.852904000     -0.757139000

6       -5.521094000      1.539045000      0.181700000

1       -6.361292000      1.148184000     -0.383674000

6        6.458548000      2.651913000      1.040352000

1        5.900898000      3.406045000      0.468478000

1        6.043502000      2.590313000      2.055702000

1        7.507848000      2.946699000      1.097922000

6       -5.706042000      2.563450000      1.122524000

1       -6.698050000      2.973735000      1.294475000

1       -2.450744000      3.936954000      2.896008000

1       -1.356473000      2.814929000      2.144869000

6       -3.272168000     -4.728872000     -0.482664000

1       -2.897637000     -4.914670000     -1.484262000

1       -3.255344000     -5.553407000      0.221081000

1       -4.182767000     -3.317287000      0.854677000

6       -3.684728000     -3.468944000     -0.096599000

1       -3.825681000     -2.681665000     -0.830207000

1       -1.551394000     -3.080944000     -0.463688000

8       -1.968932000     -3.231614000      0.430852000

8       -0.578863000     -2.073653000      0.992120000

6        0.048624000     -2.732264000      2.089728000

1        1.538087000     -3.734574000      0.865448000

6        1.048789000     -1.736761000      2.714461000

1        1.858940000     -1.500122000      2.022558000

1        0.537925000     -0.810869000      2.996742000

1        1.489858000     -2.178136000      3.616268000

1        1.278605000     -4.504939000      2.448099000

6        0.782082000     -3.996208000      1.612697000

6       -1.016724000     -3.076411000      3.146969000

1       -0.547511000     -3.491284000      4.047058000

1       -1.725434000     -3.811505000      2.757256000

1       -1.571622000     -2.174953000      3.428227000

1        0.072131000     -4.693853000      1.157639000

MoO(OR)(OH)L3

42      -0.047265000     -1.174109000     -1.064491000

8       -1.862657000     -0.353604000     -0.904957000

8        1.816962000     -1.278276000     -0.517754000

8       -0.590834000     -2.768514000     -1.956790000

7       -2.928795000      3.161288000      1.297101000

8        6.060316000      2.170850000      0.215643000

7       -1.063339000      1.422292000      0.303003000

7        0.125176000      0.789302000      0.019838000

8        0.380079000     -0.354842000     -2.491177000

6        2.801139000     -0.383392000     -0.378890000

6       -2.071128000      0.769332000     -0.238512000

6        3.640740000      1.817161000      0.275739000

1        3.426729000      2.825498000      0.612812000

6       -3.825430000      2.424006000      0.569129000

6        2.551796000      0.938195000      0.059560000

6        4.945598000      1.399891000      0.047695000

6       -4.448614000      0.510123000     -0.824129000

1       -4.140775000     -0.378956000     -1.362691000

6       -3.451481000      1.246436000     -0.148449000

6       -5.186067000      2.807298000      0.552551000

1       -5.477113000      3.703020000      1.096732000

6        1.218828000      1.424462000      0.314480000

1        1.110888000      2.411894000      0.764500000

6        4.127168000     -0.794587000     -0.596812000

1        4.304367000     -1.812710000     -0.927249000

6        5.179087000      0.081887000     -0.392296000

1        6.204599000     -0.228516000     -0.566465000

6       -5.776254000      0.902271000     -0.821969000

1       -6.522107000      0.320233000     -1.353822000

6        5.886159000      3.508338000      0.651090000

1        5.287749000      4.090471000     -0.062913000

1        5.409771000      3.552243000      1.640160000

1        6.887897000      3.936866000      0.714935000

6       -6.138180000      2.065902000     -0.126244000

1       -7.174465000      2.394323000     -0.115150000

1       -3.197628000      4.097226000      1.562653000

1       -1.943897000      2.972257000      1.145067000

8       -0.410656000     -2.069968000      0.622999000

6       -0.417755000     -2.520957000      1.963703000

6       -1.547030000     -1.785354000      2.705908000

1       -2.511797000     -1.987308000      2.228795000

1       -1.375832000     -0.704058000      2.686125000

1       -1.601573000     -2.109927000      3.751689000

1       -1.642611000     -4.254023000      1.471924000

6       -0.679538000     -4.037373000      1.948346000

1        0.110112000     -4.555804000      1.392908000

1       -0.704830000     -4.441899000      2.966763000

1        1.750025000     -2.709857000      2.049578000

6        0.946510000     -2.217006000      2.605375000

1        1.139561000     -1.139344000      2.602593000

1        0.971041000     -2.569489000      3.643304000

1       -0.935244000     -3.414682000     -1.314608000

B4- With Ligand L4

[MoO2L4]2

42       4.358866000      1.901492000     -0.482770000

7        4.292467000     -0.364827000     -0.818005000

7        3.091036000     -0.868481000     -1.261172000

8        2.521766000      1.359634000     -1.077971000

8        5.909285000      1.345180000      0.562423000

8        3.919565000      3.348911000      0.311757000

6       -1.921053000     -0.746599000     -1.962248000

6        2.217408000      0.102380000     -1.365389000

6       -0.983270000     -1.792889000     -1.947433000

1       -1.328798000     -2.822531000     -1.977980000

6        0.369228000     -1.513015000     -1.824629000

1        1.090645000     -2.320604000     -1.768779000

6        0.819906000     -0.185123000     -1.711709000

6       -0.115198000      0.857217000     -1.799706000

1        0.225965000      1.883588000     -1.726083000

6       -1.471074000      0.580545000     -1.933294000

1       -2.189397000      1.395864000     -1.965153000

6        5.279485000     -1.201790000     -0.715312000

1        5.100184000     -2.231057000     -1.029121000

6        6.590261000     -0.848276000     -0.221679000

6        6.863269000      0.411141000      0.375963000

6        8.153406000      0.672410000      0.844811000

1        8.348665000      1.637016000      1.302076000

6        9.167766000     -0.277995000      0.735557000

1       10.156090000     -0.035386000      1.108796000

6        8.904725000     -1.527986000      0.152796000

6        7.619443000     -1.801369000     -0.312454000

1        7.425534000     -2.770339000     -0.763046000

8        5.075791000      2.303196000     -1.965765000

7       -3.304197000     -1.037685000     -1.901274000

1       -3.553640000     -1.916572000     -2.347717000

1       -3.897427000     -0.290677000     -2.251134000

42      -4.358741000     -1.901470000      0.482429000

7       -4.292479000      0.364796000      0.818080000

7       -3.091015000      0.868518000      1.261083000

8       -2.521620000     -1.359532000      1.077635000

8       -5.909266000     -1.345059000     -0.562512000

8       -3.919350000     -3.348589000     -0.312606000

6        1.921165000      0.746971000      1.961629000

6       -2.217303000     -0.102306000      1.365093000

6        0.983295000      1.793178000      1.947004000

1        1.328724000      2.822850000      1.977679000

6       -0.369194000      1.513202000      1.824277000

1       -1.090686000      2.320736000      1.768605000

6       -0.819765000      0.185287000      1.711237000

6        0.115440000     -0.856981000      1.798993000

1       -0.225640000     -1.883374000      1.725272000

6        1.471305000     -0.580210000      1.932509000

1        2.189703000     -1.395468000      1.964212000

6       -5.279617000      1.201644000      0.715702000

1       -5.100391000      2.230900000      1.029598000

6       -6.590493000      0.848055000      0.222345000

6       -6.863457000     -0.411279000     -0.375549000

6       -8.153631000     -0.672673000     -0.844079000

1       -8.348920000     -1.637188000     -1.301520000

6       -9.168171000      0.277540000     -0.734291000

1      -10.156569000      0.034757000     -1.107197000

6       -8.905180000      1.527430000     -0.151365000

6       -7.619777000      1.800941000      0.313584000

1       -7.425959000      2.769858000      0.764328000

8       -5.075406000     -2.303720000      1.965402000

7        3.304301000      1.038193000      1.900692000

1        3.553600000      1.917076000      2.347229000

1        3.897570000      0.291233000      2.250603000

8        9.823054000     -2.526805000      0.000142000

6       11.152559000     -2.287938000      0.433550000

1       11.606105000     -1.442640000     -0.101035000

1       11.198513000     -2.098155000      1.514441000

1       11.709207000     -3.198463000      0.205152000

8       -9.823623000      2.526045000      0.002095000

6      -11.152657000      2.288277000     -0.433486000

1      -11.607847000      1.443447000      0.100405000

1      -11.708869000      3.199305000     -0.206047000

1      -11.196921000      2.098476000     -1.514436000

MoO2L4(MeOH)

42       0.151482000     -1.516816000     -0.565604000

7        0.171958000      0.696921000      0.037475000

7       -1.061613000      1.291230000      0.140148000

7       -7.471105000      1.923329000     -0.055122000

1       -7.709414000      2.774401000      0.436562000

1       -8.151396000      1.186994000      0.078711000

8       -1.731427000     -0.873545000     -0.318065000

8        1.966377000     -1.371265000      0.160274000

8       -0.161952000     -3.185182000     -0.380942000

8        0.415247000     -1.215402000     -2.213443000

8       -0.085578000     -1.549077000      1.932953000

1        0.820459000     -1.826148000      2.149620000

6       -2.002095000      0.406525000     -0.082826000

6       -3.413079000      0.797674000     -0.063342000

6       -4.421697000     -0.150626000     -0.305366000

1       -4.141855000     -1.178181000     -0.511205000

6       -5.760249000      0.213156000     -0.285872000

1       -6.527976000     -0.531911000     -0.481452000

6       -6.137550000      1.544387000     -0.023302000

6       -5.125396000      2.496563000      0.219087000

1       -5.400526000      3.529815000      0.418206000

6       -3.790563000      2.128338000      0.197198000

1       -3.017169000      2.865306000      0.384363000

6        1.209720000      1.456933000      0.199313000

1        1.035521000      2.518838000      0.378294000

6        2.573527000      0.981596000      0.137669000

6        2.901409000     -0.399944000      0.092841000

6        4.246352000     -0.775606000      0.039456000

1        4.482375000     -1.834452000      0.006431000

6        5.264407000      0.176944000      0.034417000

1        6.294986000     -0.156285000     -0.009987000

6        4.949602000      1.543750000      0.088776000

6        3.611424000      1.929449000      0.145226000

1        3.378321000      2.989506000      0.183708000

6       -1.022105000     -2.455665000      2.537730000

1       -2.012066000     -2.120033000      2.227783000

1       -0.945233000     -2.406034000      3.629757000

1       -0.863270000     -3.479389000      2.185081000

8        5.867167000      2.556523000      0.092487000

6        7.240830000      2.215339000      0.012326000

1        7.559579000      1.610764000      0.872409000

1        7.469783000      1.671952000     -0.914343000

1        7.785066000      3.161495000      0.017799000

MoO2L4

42      -0.102549000      1.737629000      0.090447000

7       -0.132709000     -0.530555000     -0.086424000

7        1.097127000     -1.147936000     -0.093519000

8        1.757703000      1.052806000     -0.163722000

8       -1.937840000      1.438669000     -0.469903000

8        0.176725000      3.174772000     -0.771526000

6        6.183099000     -1.345752000     -0.009227000

6        2.044540000     -0.244046000     -0.101989000

6        5.175009000     -2.332460000      0.034816000

1        5.456486000     -3.381417000      0.090837000

6        3.837911000     -1.975766000      0.004359000

1        3.068611000     -2.739499000      0.042042000

6        3.454539000     -0.623121000     -0.072080000

6        4.458758000      0.359964000     -0.117428000

1        4.173243000      1.404675000     -0.175305000

6        5.799159000      0.007798000     -0.085937000

1        6.563983000      0.779746000     -0.124523000

6       -1.171043000     -1.318176000     -0.083676000

1       -0.972862000     -2.389878000     -0.058208000

6       -2.537223000     -0.871232000     -0.101908000

6       -2.873804000      0.495458000     -0.277641000

6       -4.221440000      0.866696000     -0.305899000

1       -4.465082000      1.914310000     -0.448373000

6       -5.228610000     -0.084733000     -0.162722000

1       -6.262526000      0.239932000     -0.187823000

6       -4.905179000     -1.442814000      0.006458000

6       -3.565724000     -1.822591000      0.029688000

1       -3.323653000     -2.873109000      0.160288000

8       -0.191859000      2.052362000      1.755838000

7        7.520224000     -1.704464000     -0.027781000

1        7.749928000     -2.620368000      0.334055000

1        8.184778000     -0.991816000      0.242703000

8       -5.817391000     -2.447752000      0.152667000

6       -7.196047000     -2.113265000      0.135193000

1       -7.457124000     -1.429545000      0.953921000

1       -7.490812000     -1.661259000     -0.821343000

1       -7.732792000     -3.054148000      0.268155000

MoO2L4(TBHP)

42      -0.127246000      0.619230000     -1.599940000

8        1.718261000      0.149769000     -1.035604000

8       -1.947710000      0.845367000     -0.966322000

8        0.236839000      2.238804000     -2.036556000

8       -6.106995000     -2.337777000      0.779057000

7        0.997096000     -1.475498000      0.423286000

7       -0.213664000     -0.991259000     -0.009036000

8       -0.332261000     -0.302785000     -3.004690000

6       -2.914996000      0.011057000     -0.547435000

6        1.968469000     -0.836342000     -0.179976000

6       -3.693268000     -1.979087000      0.639074000

1       -3.449908000     -2.880159000      1.190951000

6        3.712043000     -2.243987000      0.915660000

6       -2.628004000     -1.172151000      0.170422000

6       -5.012260000     -1.626319000      0.384127000

6        4.397969000     -0.429119000     -0.530569000

1        4.141318000      0.400450000     -1.180082000

6        3.366838000     -1.172526000      0.070153000

6        5.038555000     -2.561934000      1.151067000

1        5.290643000     -3.390387000      1.808998000

6       -1.277857000     -1.565750000      0.473839000

1       -1.117657000     -2.405105000      1.151063000

6       -4.253390000      0.361192000     -0.789417000

1       -4.456845000      1.275685000     -1.336663000

6       -5.283542000     -0.444736000     -0.335585000

1       -6.320210000     -0.183053000     -0.522671000

6        5.727839000     -0.744108000     -0.298416000

1        6.514160000     -0.156276000     -0.765882000

6       -5.897461000     -3.541331000      1.499683000

1       -5.325505000     -4.269625000      0.909136000

1       -5.376611000     -3.357432000      2.449104000

1       -6.890394000     -3.944426000      1.705864000

6        6.073613000     -1.816929000      0.546887000

8        1.446404000      3.170876000      0.264605000

8        0.571045000      2.197585000      0.904386000

6       -0.229987000      2.881297000      1.911351000

6        0.702785000      3.538262000      2.934991000

1        1.312965000      4.309518000      2.459527000

1        1.371014000      2.791081000      3.376086000

1        0.117834000      4.000105000      3.738589000

1       -0.578024000      4.673611000      0.736348000

6       -1.159636000      3.901271000      1.246749000

1       -1.808727000      3.408986000      0.514937000

1       -1.791166000      4.388471000      1.998483000

1       -1.698712000      1.272380000      1.828270000

6       -1.019941000      1.734463000      2.550589000

1       -0.339799000      0.968065000      2.936712000

1       -1.617331000      2.119112000      3.384240000

1        1.079212000      3.128774000     -0.647427000

1        2.921281000     -2.822358000      1.381112000

7        7.400709000     -2.103185000      0.821099000

1        7.603136000     -3.034524000      1.159093000

1        8.083408000     -1.764991000      0.156091000

TS

42      -0.071661000     -0.941016000     -1.085163000

8       -1.812020000     -0.100033000     -0.530456000

8        1.757641000     -1.386883000     -0.601503000

8       -0.760086000     -2.386935000     -1.753133000

8        6.398054000      1.428687000      0.432087000

7       -0.755601000      1.412718000      0.859080000

7        0.345464000      0.743778000      0.383067000

8        0.289713000      0.053127000     -2.407224000

6        2.842389000     -0.631039000     -0.357570000

6       -1.841736000      0.917958000      0.315771000

6        3.958297000      1.332559000      0.575595000

1        3.876728000      2.291054000      1.076397000

6       -3.277618000      2.554786000      1.544645000

6        2.765745000      0.625495000      0.290736000

6        5.196430000      0.817447000      0.211772000

6       -4.316248000      0.997691000      0.017919000

1       -4.229644000      0.184950000     -0.694964000

6       -3.153152000      1.492675000      0.630318000

6       -4.517479000      3.099034000      1.837519000

1       -4.596833000      3.916390000      2.550764000

6        1.512122000      1.209897000      0.706850000

1        1.537544000      2.109824000      1.322959000

6        4.102567000     -1.143392000     -0.708493000

1        4.145044000     -2.110989000     -1.197761000

6        5.258716000     -0.432109000     -0.434412000

1        6.233338000     -0.822958000     -0.709434000

6       -5.560465000      1.541266000      0.304144000

1       -6.450704000      1.146211000     -0.180103000

6        6.394462000      2.692553000      1.073417000

1        5.837840000      3.439217000      0.490808000

1        5.965999000      2.631964000      2.083257000

1        7.440218000      2.997191000      1.144012000

6       -5.684306000      2.602410000      1.221080000

6       -3.180146000     -4.849219000     -0.529628000

1       -2.787120000     -5.018345000     -1.527010000

1       -3.147940000     -5.676301000      0.170547000

1       -4.145150000     -3.470120000      0.803406000

6       -3.627120000     -3.600958000     -0.140411000

1       -3.784866000     -2.816301000     -0.873608000

1       -1.512209000     -3.144510000     -0.482468000

8       -1.937658000     -3.312213000      0.406383000

8       -0.596767000     -2.101261000      0.981625000

6        0.028877000     -2.728520000      2.097138000

1        1.562404000     -3.711049000      0.911825000

6        0.994354000     -1.699607000      2.722588000

1        1.810277000     -1.454763000      2.040365000

1        0.457422000     -0.781440000      2.980358000

1        1.430278000     -2.116129000      3.638678000

1        1.297507000     -4.463778000      2.502079000

6        0.801488000     -3.980688000      1.651214000

6       -1.043973000     -3.084427000      3.143120000

1       -0.579375000     -3.477113000      4.055553000

1       -1.729595000     -3.840629000      2.752112000

1       -1.623814000     -2.192638000      3.404341000

1        0.116706000     -4.702805000      1.195738000

1       -2.383740000      2.944995000      2.018905000

7       -6.932345000      3.114321000      1.551376000

1       -6.940789000      4.049766000      1.936724000

1       -7.666351000      2.968942000      0.870401000

MoO(OR)(OH)L4

42      -0.151828000      1.107799000     -1.094943000

8        1.709969000      0.404144000     -0.897008000

8       -2.019895000      1.133112000     -0.546413000

8        0.327224000      2.682017000     -2.062338000

8       -6.062222000     -2.515150000      0.344586000

7        1.004547000     -1.365417000      0.391095000

7       -0.214155000     -0.808381000      0.079782000

8       -0.540806000      0.211106000     -2.485179000

6       -2.952323000      0.190376000     -0.369963000

6        1.963635000     -0.679411000     -0.180290000

6       -3.666897000     -2.019996000      0.389763000

1       -3.396505000     -2.996686000      0.775918000

6        3.712711000     -2.234034000      0.692457000

6       -2.629160000     -1.091912000      0.132361000

6       -4.992663000     -1.689912000      0.139549000

6        4.384610000     -0.354142000     -0.671304000

1        4.124055000      0.524589000     -1.251412000

6        3.362283000     -1.091676000     -0.050659000

6        5.036238000     -2.623915000      0.812348000

1        5.291982000     -3.506759000      1.393838000

6       -1.271062000     -1.488087000      0.410142000

1       -1.102289000     -2.442823000      0.908738000

6       -4.298526000      0.513196000     -0.611067000

1       -4.532432000      1.502109000     -0.991345000

6       -5.299744000     -0.411263000     -0.365549000

1       -6.340575000     -0.169247000     -0.556627000

6        5.711582000     -0.741852000     -0.556458000

1        6.491102000     -0.159376000     -1.042007000

6       -5.812052000     -3.816188000      0.847208000

1       -5.178335000     -4.398181000      0.164174000

1       -5.337095000     -3.782317000      1.837394000

1       -6.787373000     -4.298744000      0.932453000

6        6.062432000     -1.884508000      0.188119000

8        0.146009000      2.114544000      0.544294000

6        0.083347000      2.651450000      1.850710000

6        1.233248000      2.037437000      2.668232000

1        2.197321000      2.268811000      2.203040000

1        1.128037000      0.948482000      2.713245000

1        1.237936000      2.430039000      3.692003000

1        1.214014000      4.423059000      1.276951000

6        0.252058000      4.177328000      1.741528000

1       -0.550530000      4.607136000      1.131576000

1        0.221013000      4.648872000      2.730620000

1       -2.093578000      2.711167000      1.874375000

6       -1.277075000      2.304548000      2.478605000

1       -1.405024000      1.219021000      2.539664000

1       -1.350765000      2.718635000      3.491246000

1        0.639593000      3.368805000     -1.446705000

1        2.927977000     -2.810184000      1.170637000

7        7.392133000     -2.246749000      0.348465000

1        7.565724000     -3.211876000      0.596832000

1        8.036778000     -1.901085000     -0.3503070