## Slide 1
Fig. 1
https://www.bepanthen.co.uk/en/understanding-your-skin/your-skins-structure/
https://www.bepanthen.co.uk/en/understanding-your-skin/your-skins-structure/
Notes: Skin cream effects the skins surface! The stratum corneum! Not collagen/elastin fibers
 The biological effects of the cosmeceutical effects of skin cream on collagen fibers is not part of this work
 Cosmeceuticals: pharmaceuticals and cosmetics – not well developed; A LOT of missing scientific information…

## Slide 2
Table 1 Existing testing Methods
[11, 14-17]

## Slide 3
Fig. 2 Existing testing Methods
a) Cutometer
b) piezoelectric sensors
c) Durometers
Skin indenter
corneometers
b
a
c
d: skin corneometer
a and b: skin indenters
Basic principle of
skin indenters
Notes: Cutometer - elasticity
piezoelectric sensors – mechanical properties
Durometers - hardness
Corneometers – water content
No surface properties – friction (adhesion), roughness/smoothness
There’s also Atomic Force Microscopy AFM – not practical, more nano scale, samples are so small
https://www.courage-khazaka.de/index.php/en/products/scientific/134-skin-glossymeter

## Slide 4: Fig. 3 Draping of a fabric and paper
a) A fabric wrinkles
b) A paper sheet can only bend

## Slide 5: Table 2 Different testing methods and challenges
 | Existing methods | PhabrOmeter
Issues Subjective and random bias Complex deformation Connecting to sense Skin properties Elasticity Surface friction Moisture content | X Y X Y X Y | Y Y Y Y Y X
X: unable to dealt with.
Y: able to dealt with.

## Slide 6
a
b
c
Fig. 4 A Vitro-skin sample tested on PhabrOmeter

## Slide 7
a
d
c
Fig. 5 Vitro-skin sample and hydration treatment
b

## Slide 8
Product Name | Manufacturer | Unit Price /fl.oz | Notes
Badger Aloe Vera Gel Unscented | Badger | $1.25 * | 
Luminesce Daily Moisturizing Complex | Jeunesse Global | $47.00 * | 
Bio-Performance Advanced Super Restoring Cream | Shiseido Company | $50.80 * | 
Table 3a The specs of the creams used
* The prices are all from Amazon.

## Slide 9
Tested Curve Properties ( within group CV values%, 3 repeat each) |  |  | 
Name | Peak | Slope | Area
Original | 3.12 | 3.37 | 1.97
Aloe vera | 2.05 | 4.45 | 2.51
Luminesce | 3.18 | 2.88 | 3.52
Shiseido | 0.75 | 0.8 | 1.7
Table 3b The repeatability of the tests
All the data are in relative terms for now.

## Slide 10
Chart: 
S
P
A
Fig. 6a Analysis of a single extraction curve
Time t (s)
Load (kg)

## Slide 11
Chart: 
Fig. 6b the repeatability of the tests
Time t (s)

## Slide 12
Chart: 
Fig. 6c Sensitivity test by PhabrOmeter
Time t (s)

## Slide 13
Chart: 
Fig. 7a The effect of cream Aloe vera
Time t (s)

## Slide 14
Chart: 
Fig. 7b The effect of cream Luminesce
Time t (s)

## Slide 15
Chart: 
Fig. 7c The effect of cream Shiseido
Time t (s)

## Slide 16
Chart: 
| Original | Aloe vera | Luminesce | Shiseido
RHV | 0 | 2.87 | 4.97 | 7.77
Fig. 8 Overall comparison
(a)
(b)
Chart: 
| Luminesce | Aloe vera | Shiseido | Original
Resilience Score | 6.37 | 7.12 | 7.23 | 8.3

## Slide 17
Chart: 
| Shiseido | Luminesce | Aloe vera | Original
Softness Score | 63.86 | 58.55 | 53.46 | 50.08
Chart: 
| Aloe vera | Luminesce | Original | Shiseido
Smoothness Score | 83.3 | 80.87 | 78.27 | 77.08
Fig. 8 Overall comparison
(c)
(d)