Supporting Information.

| Elements | Nude | APTES | APTES+GA | APTES+GA+PSGL-1 |
| --- | --- | --- | --- | --- |
| O1s | 74.52% | 68.05% | 51.17% | 29.08% |
| C1s | 24.42% | 28.78% | 45.8% | 60.85% |
| N1s | 1.06% | 3.17% | 3.13% | 10.06% |

Table S1. Element contents on the modified surface

Figure S1. Electrical characteristics of the poly-Si NWFET

ID−VG curve of the poly-Si NWFET device, the drain current (ID) and gate leakage (IG) were showed

respectively.

Figure S2. Eight consecutive measurements of ID-VG of the device

Eight consecutive measurements of the ID-VG curve are shown. Each of the ID-VG curves is close, indicating the stability of the device.

Figure S3. Electrical responses of the functionalized pSNWFET to PSGL-1 sulfation

(A)(B)(C) ID–VG curve obtained from the synthesized sulfated PSGL-1 peptide and interaction with anti-sulfotyrosine, and anti-GST antibodies as the controls. (D)(E)(F) ID–VG curve obtained through PSGL-1 sulfation and interaction with anti-sulfotyrosine, and anti-GST antibodies as the controls. (G)(H)(I) ID–VG curve obtained from non-sulfated PSGL-1 following coupled enzyme treatment without the critical enzyme TPST and the interaction with anti-sulfotyrosine, and anti-GST antibodies as the controls.

Figure S4. Real-time response of the pSNWFET following different surface modifications

(A) Response of the pSNWFET with an unmodified surface to anti-GST and anti-sulfotyrosine antibodies. (B) Response of the pSNWFET with a non-sulfated PSGL-1 peptide-modified surface to anti-GST and anti-sulfotyrosine antibodies. (C) Response of the pSNWFET with native PSGL-1 peptide-modified surface following PTS catalyzed by PST–TPST coupled enzyme system to anti-GST and anti-sulfotyrosine antibodies. The conductance was measured at fixed gate voltage. G0 was the conductance obtained from the anti-GST treatment as the baseline, and the changes in the conductance (G/G0 = Ganti-sulfotyrosine/Ganti-GST) were calculated.

Figure S5. pH profile of the PSGL-1 modified surface

The real-time conductance response of the PSGL-1 modified NWFET device in 2 different pH buffers.