Table S1: 3D-printed scaffolds for periodontal tissue engineering

|  | Authors | 3D printing technology | Printed material(s), bioactive factor(s) and / or cells used |  | Scaffold geometry |  | Mesh thickness | Porosity |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MONOPHAS I C | Kim [123] | Extrusion | PCL (80%) + HA (20%) with SDF1 and BMP-7 (100 ng/mL each) |  | Shape of tooth (rat mandibular central incisor and human mandibular first molar) |  | 200 μm | 200 µm diameter interconnecting channels |
|  | Mangano [124] | Extrusion | 30% HA, 60% β-TCP, 10% α-TCP |  | Blocks with a volume of about 0.14 cm³ |  | 300 ± 30 μm | 370 ± 25 μm Open interconnecting microporosity with pores sizes of about 1 μm Total porosity : 60% |
|  | Baba [125, 126] | Melt spinning | 75/25 PLGA+BMMSCs+PRP |  | 1.5 diameter |  | - | - |
|  | Carrel [127] | Extrusion | α-TCP + HA (calcium-to-phosphate ratio : 1.43) |  | Hemispheric blocks |  | 400 µm | 250 µm Total porosity: 50-65% Macroporosity: 40-50% |
|  | Cho [128] | Extrusion | PCL scaffolds with microspheres of 75/25 PLGA with BMP-2, BMP-7 + CTGF |  | Rectangular scaffolds (5×3×0.5mm3) |  | 200 μm | 500 μm transverse pores |
|  | Puppi [129] | Extrusion (wet spinning) | PCL fiber construct and a chitosan/poly(𝜸-glutamic acid) polyelectrolyte complex hydrogel |  | Rectangular scaffold: 10 × 10 mm, 50 layers |  | 200–300 μm | 200-1800 μm |
| BIPHASIC | Park [130] | 3D wax printing system | Bone compartment : 25% PCL with recombinantadenovirus-encodingmurine BMP-7 |  | Rectangular scaffolds: 1.75 x 5.0 x 4.0 mm |  | - | Windows dimensions: 0.75 x 0.50 x 0.05 mm3 |
|  |  |  | PDL compartment: 25% PGA |  | Rectangular scaffolds: 1.5 x 5.0 x 4.0 mm |  | Diameter: 0.8 mm Height: 0.3 mm | - |
|  | Park [131] | 3D wax printing system | Bone compartment: PCL + BMP-7 |  | 3 x 2 x 2 mm |  | - | 0.60 x 0.50 mm2 window pores to contact residual bone tissue |
|  |  |  | PDL compartment: PCL+PDL cells |  | 3 cylindrical-shaped PDL fiber-guiding architectures per layer 0.225 mm diameter, 0.250 mm ligament interface |  | - | 0.175 mm thick interconnective space between PDL and bone regions |
|  | Vaquette [79, 132] Dan [133] Mathew [134] | Electrospinning | Calcium phosphate coated melt electrospun polycaprolactone (CaP-PCL) scaffold |  | Small pieces (approximately 3 mm x 1.5 mm x 0.5 mm in size) |  | 500 µm | over 150 µm diameter interconnecting pores |
|  |  |  | PCL membrane (associated) (can be loaded with azithromycin) |  | Small pieces (approximately 8 mm x 5 mm x 0.3 mm in size) |  | 300-400 µm with 3 μm diameter fibers | 5-10 μm |
|  | Vaquette [84] | Extrusion (FDM) | Bone compartment: PCL + b-tricalcium Phosphate (β-TCP, 20% wt.) |  | 100 x 100 x 2 mm3 sectioned into 5 x 5 x 2 mm3 |  | - | interconnectivity, 70% porosity |
|  |  | Electrospinning | PDL compartment: PCL |  | cell membrane: 7 x 9 x 0.4 mm3 |  | - | - |
|  | Costa [85] | FDM | Bone compartment: PCL + β-TCP (20% wt.) |  | 100 x 100 x 2 mm3 sectioned into 5 x 5 x 2 mm3 |  | - | interconnectivity, 70% porosity |
|  |  | Electrospinning | PDL compartment: PCL |  | Circular membranes with 8 mm diameter |  | Fiber diameter: 10–15 µm | Interconnected pore Pore size: 100-400 µm |
| TR I PHAS I C | Lee [135] | Extrusion (layer-by-layer deposition) | PCL/HA scaffolds and poly(lactic-co-glycolic acid) microspheres encapsulating factors | Bone compartment: +BMP2 | 5 x 5x 3mm3 | 2.25mm (width) | - | 300-mm microchannels |
|  |  |  |  | PDL compartment: + CTGF |  | 0.5mm (width) | - | 600-mm transverse microchannels |
|  |  |  |  | Cementum/dentin interface: +amelogenin |  | 2.25mm (width) | - | 100-mm transverse microchannels |
| CUSTOM | Rasperini [136] | SLS | PCL and 4% HA |  | Customized scaffold: patient’s defect |  | Mean strut length: 600 μm for support of extensions in the PDL region | Channel width for PDGF delivery was ≈500 μm |
| OR IENTE | Jiang [137] | Electrospinning | Biodegradable poly PCE copolymer electrospun nanofibrous mats into porous CHI |  | 30 layers of nanofibers embedded within the porous CHI, with thickness ≈ 4 mm |  | Diameter (nm): - Random fibers: 574.3±218.2 - Aligned fibers: 616.1±213.1 nm | 103.38 ± 49.54 µm between layers |
|  | Kim [138] | Electrospinning | PCL/gelatin (Gel) nanofiber with periodontal ligament cells |  | 30 mm x 4 mm x 200 μm |  | - | - |
|  | Pilipchuk [139] | SLS | Bone compartment: PCL and 4% HA |  | Idem [130]: 5.1 x 4.1 x 3.2 mm |  | ≈ 0.7 x 0.7 mm | 0.7 x 0.7 mm |
|  |  | Molding | Periodontal ligament: PCL |  | Idem [130]: 3.6 x 2.8 x 0.4 mm |  | 400 x 250 µm, with/ without grooves | 400 µm wide pores |

BMMSCs: mesenchymal cells derived from bone marrow, BMP: Bone morphogenetic protein, CHI: chitosan, CTGF: Connective tissue growth factor, FDM: Fused Deposition Modeling, HA: hydroxyapatite, SLS: selective laser sintering, PCE: poly (e-caprolactone)-poly(ethylene glycol), PCL: polycaprolactone, PDGF: Platelet-derived growth factor, PDL: periodontal ligament, PGA: Polyglycolic acid, PLGA: poly-L-lactic acid, PRP: Platelet Rich Plasma, SDF: Stromal-derived factor, SLS: Selective Laser Sintering, TCP: tricalcium phosphate