Calcium-based biochar loading Paenibacillus mucilaginosus an eco-friendly strategy to enhance soil nutrients and plant biomass with biochar-based fertilizers

Supplementary tables:

Table S1. Soil physical and chemical properties.

Table S2. BCEKH physical and chemical properties.

Table S3. Coefficients of determination (R2) and rate constants (b) for the kinetic model of phosphorus release from biochar in soil.

Table S4. Coefficients of determination (R2) and rate constants (b) for kinetic models of potassium release from biochar in soil.

Table S5. Coefficient of determination (R2) and rate constant (b) for a kinetic model of potassium release from biochar in soil.

Table S1

Soil physical and chemical properties.

| Property | pH | EC (ms·cm-1) | Total Calcium (mg·kg-1) | Active Phosphorus (mg·kg-1) | Active Potassium (mg·kg-1) | Organic matter (%) | Moisture content (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Value | 8.51 | 1.151 | 1800 | 44.57 | 225.41 | 17.79 | 13.15 |

Table S2

BCEKH physical and chemical properties.

| Property | pH | EC (ds·m-1) | Total Calcium (g·kg-1) | Total Phosphorus (g·kg-1) | Total Potassium (g·kg-1) | Surface Area (m2·g-1) | Pore Volume (cm3·g-1) | Pore Size (nm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Value | 7.79 | 8.07 | 126.10 | 188.93 | 159.88 | 73.92 | 0.06 | 5.48 |

Table S3

Coefficient of determination (R2) and slope (K) for a kinetic model of phosphorus release from experimental groups

| P soil | The zero order (linear) |  | pseudo-first order |  | pseudo-second order |  | Elovich |  | parabolic diffusion model |  | power function |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 |
| CS | 0.992 | 0.020 | 0.907 | 0.055 | 0.920 | 0.036 | 0.935 | 2.674 | 0.992 | 0.040 | 0.978 | 0.140 |
| T | 0.996 | 1.959 | 0.998 | -0.008 | 0.995 | 0.000 | 0.995 | 0.000 | 0.996 | 3.918 | 0.998 | 1.433 |
| J | 0.998 | 0.171 | 0.956 | 0.037 | 0.960 | 0.028 | 0.964 | 0.204 | 0.998 | 0.343 | 0.986 | 0.759 |
| 10TJ | 0.994 | 2.290 | 0.997 | -0.009 | 0.993 | 0.000 | 0.993 | 0.000 | 0.994 | 4.580 | 0.997 | 1.545 |
| 20TJ | 0.997 | 2.148 | 0.998 | -0.004 | 0.997 | 0.000 | 0.997 | 0.000 | 0.997 | 4.295 | 0.997 | 1.900 |
| 30TJ | 0.998 | 2.499 | 0.998 | -0.002 | 0.997 | 0.000 | 0.998 | 0.000 | 0.998 | 4.998 | 0.998 | 2.275 |

Table S4

Coefficient of determination (R2) and slope (K) for a kinetic model of potassium release from experimental groups

| K soil | The zero order (linear) |  | pseudo-first order |  | pseudo-second order |  | Elovich |  | parabolic diffusion model |  | power function |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 |
| CS | 0.998 | 0.024 | 0.844 | 0.065 | 0.865 | 0.063 | 0.896 | 2.799 | 0.998 | 0.047 | 0.963 | 0.216 |
| T | 0.998 | 2.327 | 0.971 | 0.000 | 0.980 | 0.008 | 0.981 | 0.006 | 0.998 | 4.655 | 0.987 | 4.894 |
| J | 1.000 | 0.195 | 0.956 | 0.030 | 0.959 | 0.020 | 0.961 | 0.146 | 1.000 | 0.391 | 0.981 | 0.731 |
| 10TJ | 0.996 | 2.826 | 0.972 | 0.000 | 0.977 | 0.005 | 0.977 | 0.003 | 0.996 | 5.651 | 0.983 | 5.321 |
| 20TJ | 0.995 | 2.983 | 0.975 | 0.000 | 0.976 | 0.003 | 0.976 | 0.002 | 0.994 | 5.966 | 0.981 | 5.000 |
| 30TJ | 0.989 | 3.104 | 0.969 | -0.001 | 0.962 | 0.001 | 0.969 | 0.001 | 0.989 | 6.207 | 0.972 | 4.700 |

Table S5

Coefficient of determination (R2) and slope (K) for a kinetic model of calcium release from experimental groups

| Ca soil | The zero order (linear) |  | pseudo-first order |  | pseudo-second order |  | Elovich |  | parabolic diffusion model |  | power function |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 | R2 | K1 |
| CS | 0.989 | 0.027 | 0.975 | 0.000 | 0.975 | 0.001 | 0.975 | 0.031 | 0.989 | 0.055 | 0.978 | 0.041 |
| T | 0.992 | 1.112 | 0.998 | -0.012 | 0.991 | 0.000 | 0.991 | 1.093 | 0.991 | 2.223 | 0.996 | 0.717 |
| J | 0.998 | 0.024 | 0.984 | 0.025 | 0.985 | 0.016 | 0.985 | 0.043 | 0.998 | 0.049 | 0.993 | 0.068 |
| 10TJ | 0.985 | 1.113 | 0.997 | -0.017 | 0.984 | 0.000 | 0.984 | 1.085 | 0.985 | 2.226 | 0.994 | 0.578 |
| 20TJ | 0.992 | 1.215 | 0.998 | -0.013 | 0.991 | 0.000 | 0.991 | 1.189 | 0.992 | 2.430 | 0.997 | 0.754 |
| 30TJ | 0.991 | 1.203 | 0.997 | -0.012 | 0.991 | 0.000 | 0.991 | 0.001 | 0.991 | 2.406 | 0.996 | 0.782 |