Supplementary Material

Cellulose-based waste in a close loop: adsorbent for dyes removal from textile industry wastewater

Marija Vukčević1,*, Marina Maletić2, Biljana Pejić1, Ana Kalijadis3, Mirjana Kostić1, Katarina Trivunac1, Aleksandra Perić Grujić1

1University of Belgrade, Faculty of Technology and Metallurgy, Karnegijeva 4, 11000 Belgrade, Serbia

2Innovation Center of Faculty of Technology and Metallurgy, Karnegijeva 4, 11000 Belgrade, Serbia

3Department of Materials „VINČA” Institute of Nuclear Sciences - National Institute of thе Republic of Serbia, University of Belgrade, Mike Petrovica Alasa 12-14, 11000 Belgrade, Serbia

Table S1. Pseudo-first and pseudo-second order adsorption rate constants, calculated using appropriate model, and experimental qe values for adsorption of selected dyes on cotton-based adsorbents

| Dye | Sample | Cott | Cottc | Cottac | Cott/PES | Cott/PESc | Cott/PESac |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MO | qe,exp, mg g-1 | 0.25 | 0.33 | 99.75 | 0.31 | 0.50 | 37.78 |
| MB |  | 10.78 | 2.85 | 99.33 | 6.30 | 1.62 | 79.37 |
| Pseudo-first order model |  |  |  |  |  |  |  |
| MO | qe,cal, mg g-1 | 0.23 | 0.28 | 96.30 | 0.28 | 0.40 | 33.51 |
| MB |  | 10.31 | 2.59 | 99.91 | 5.82 | 1.40 | 72.29 |
| MO | k1, min-1 | 0.0343 | 0.0798 | 0.2979 | 0.0481 | 0.0877 | 0.1593 |
| MB |  | 0.1095 | 0.1977 | 0.3928 | 0.1172 | 0.1807 | 0.0421 |
| MO | R2 | 0.96328 | 0.80869 | 0.67796 | 0.91629 | 0.59018 | 0.34174 |
| MB |  | 0.83565 | 0.67271 | 0.98308 | 0.54210 | 0.62056 | 0.79825 |
| Pseudo-second order model |  |  |  |  |  |  |  |
| MO | qe,cal, mg g-1 | 0.28 | 0.32 | 100.39 | 0.33 | 0.45 | 36.26 |
| MB |  | 11.12 | 2.76 | 101.71 | 6.28 | 1.51 | 82.50 |
| MO | k2, g mg-1min-1 | 0.1304 | 0.3177 | 0.0065 | 0.1646 | 0.2411 | 0.0067 |
| MB |  | 0.0151 | 0.1215 | 0.0137 | 0.0292 | 0.1902 | 0.0006 |
| MO | R2 | 0.98134 | 0.92104 | 0.97229 | 0.93567 | 0.78692 | 0.71694 |
| MB |  | 0.95622 | 0.91631 | 0.68521 | 0.80863 | 0.78059 | 0.89764 |

Table S2. Kinetic parameters for MO and MB adsorption on cotton-based adsorbents obtained by Elovich and intraparticle diffusion model

| Material | Dye | Cott | Cottc | Cottac | Cott/PES | Cott/PESc | Cott/PESac |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Elovich model |  |  |  |  |  |  |  |
| R2 | MO | 0.99026 | 0.96500 | 0.87480 | 0.93400 | 0.92319 | 0.94111 |
|  | MB | 0.93148 | 0.97093 | 0.24819 | 0.93096 | 0.84670 | 0.95216 |
| α, mg/g min | MO | 0.022 | 0.100 | 1.081x106 | 0.036 | 0.180 | 131.3 |
|  | MB | 14.63 | 55.21 | 1.32x1016 | 10.34 | 11.17 | 12.56 |
| β, g/mg | MO | 16.7 | 18.3 | 0.17 | 14.3 | 13.2 | 0.23 |
|  | MB | 0.66 | 3.66 | 0.41 | 1.19 | 5.98 | 0.07 |
| RE | MO | 0.240 | 0.164 | 0.060 | 0.228 | 0.152 | 0.117 |
|  | MB | 0.142 | 0.096 | 0.025 | 0.133 | 0.103 | 0.193 |
| Intra-particle diffusion |  |  |  |  |  |  |  |
| kid,1, mg/g min1/2 | MO | 0.051 | 0.017 | 5.29 | 0.087 | 0.024 | 1.64 |
|  | MB | 1.10 | 0.082 | 14.9 | 0.420 | 0.052 | 4.88 |
| C1, mg/g | MO | 0.84 | 0.11 | 67.76 | 0.002 | 0.16 | 19.71 |
|  | MB | 3.21 | 1.84 | 52.25 | 2.61 | 0.93 | 17.06 |
| kid,2, mg/g min1/2 | MO | 0.022 |  | 0.51 | 0.022 |  | 0.18 |
|  | MB | 0.490 |  | 0.009 | 0.070 |  |  |
| C2, mg/g | MO | 0.024 |  | 93.55 | 0.079 |  | 35.36 |
|  | MB | 6.59 |  | 99.66 | 5.38 |  |  |
| kid,3, mg/g min1/2 | MO | 0.010 |  |  | 0.010 |  |  |
|  | MB | 0.063 |  |  |  |  |  |
| C3, mg/g | MO | 0.12 |  |  | 0.17 |  |  |
|  | MB | 9.93 |  |  |  |  |  |