Supporting informations

Effect of Chitin Nanocrystal Deacetylation on a Nature-Mimicking Interface in Carbon Fiber Composites

A. M. Abdel-Mohsena, R. M. Abdel-Rahmana, L. Kalinab, V. Vishakhac, L. Kaprálkováa, P. Němečeka, J. Jančářb,c, I. Kelnara*

a Institute of Macromolecular Chemistry, Czech Academy of Sciences, Heyrovského nám. 2, Praha 162 00, Czech Republic

b Faculty of Chemistry, Materials Research Center, Brno University of Technology, Purkyňova 464/118, Brno 612 00, Czech Republic

c CEITEC-Central European Institute of Technology, Brno University of Technology, Purkyňova 656/123, Brno 612 00, Czech Republic

*Corresponding author: email: kelnar@imc.cas.cz

Fig. S1. Rheological characterization of water suspensions  (5mg/ml) of single components and adducts

Fig. S2. Effects of voltage and DDA percentages on OCF coating efficiency Conditions: 10 min; 5 mg; pH 3.5, rt.

Fig. S3. Effect of concetration of GO/ChNCs30 adduct suspension on OCF coating structure Conditions: 10 min, 5 V, DDA 30 %, pH 3.5, different concentration of GO-g-ChNCs (0.01 to 15 mg/ml)., rt.