Supporting Information for

Super long green persistent luminescence from X-ray excited β-NaYF4: Tb3+

Yue Hu,1 Yanmin Yang1,*, Xiaoxiao Li,1 Xin Wang,1 Yunqian Li,1 Tianyi Li,1 Hongwu Zhang2,*

1 College of Physics Science and Technology, Hebei University, Midwest universities comprehensive strength promotion project, Hebei Key Lab of Optic-electronic Information and Materials, Baoding, 071002, China.

2 Institute of Urban Environment, Chinese Academy of Sciences, Xiamen 361021, China.

Email address for all co-authors:

17631645514@163.com (Yue Hu)

mihuyym@163.com (Yanmin Yang)

leexiaoxiaoxiaolxx@163.com (Xiaoxiao Li)

1043846176@qq.com (Xin Wang)

349345164@qq.com (Yunqian Li)

1759493876@qq.com (Tianyi Li)

hwzhang@iue.ac.cn (Hongwu Zhang).

Supplementary Figure 1. Schematic energy level diagram of β-NaYF4: Tb3+ phosphors. Some low-energy 4f8 levels, some high-energy levels, valence band (VB) and conduction band (CB) in the simulated position are shown.

Supplementary Figure 2. The excitation-afterglow process of the sample at different times (1 min, 5 min, 10 min, 15 min, 20 min and 25 min, respectively) of X-ray irradiation, from which can be seen 10-15 min irradiation was the most suitable for X-ray induced long persistence luminescence of β-NaYF4: Tb3+.

Supplementary Figure 3. X-ray excited luminescence (red) and afterglow (blue) spectra of β-NaYF4: Tb3+ phosphor powder. The absorption spectrum of g-C3N4 is displayed in black. The spectra are normalized in comparison.

Supplementary Figure 4. Schematic diagram of photodynamic therapy (PDT) for in vivo stent infection.

Supplementary Figure 5. Experiment procedure of bacterial inactivation by X-PDT. a, Setup schematic. b, setup photograph.

Supplementary Figure 6. Reciprocal of the persistent luminescence intensity (I-1) at 543 nm as a function of time (t). The sample was irradiated by X-ray for 10 min. A linear relationship can be seen clearly from 10800 to 38000 s, which indicates a tunneling mechanism of the process.

Supplementary Figure 7. Afterglow intensity from β-NaYF4: Tb3+ phosphor monitored at 543 nm as a function of time made at -196℃. The top inset shows the same data plotted as I-10 versus t, which more confirmed the tunneling process. The sample was irradiated by X-ray for 10 min.

Supplementary Figure 8. Emission spectra of β-NaYF4: xTb3+ (x=1, 3, 5, 10, 15 and 20 mol%) excited by X-ray. The upper inset shows that the emission intensity of the samples ( monitored at 543 nm) increases with the increase of Tb3+ doping concentration initially and then decreases. The most intense emission is obtained with a Tb3+ concentration of 10 mol%.