Electronic Supplementary Information for:

A luminescent MOF based on pyrimidine-4,6-dicarboxylate ligand and lead(II) with unprecedented topology

Laura Razquin-Bobillo †, 1 Oier Pajuelo-Corral †, 1 Andoni Zabala-Lekuona, 1 Iñigo Vitorica-Yrezabal, 3 Jose Angel García, 2 Jose M. Moreno, 3 Antonio Rodríguez-Diéguez 3 and Javier Cepeda 1,*

1	Departamento de Química Aplicada, Facultad de Química, Universidad del País Vasco/Euskal Herriko Unibertsitatea (UPV/EHU), 20018, Donostia, Spain.

2	Departamento de Física, Facultad de Ciencia y Tecnología, Universidad del País Vasco/Euskal Herriko Unibertsitatea (UPV/EHU), 48940, Leioa, Spain.

3	Departamento de Química Inorgánica, Facultad de Ciencias, Universidad de Granada, 18071, Granada, Spain.

† These authors contributed equally to this work.

Contents:

S1.	Structural details.

S2.	Continuous Shape Measurements (CShMs).

S3.	Powder X-ray Diffraction Analysis.

S4.	FT-IR spectroscopy.

S5.	Photoluminescence measurements and calculations.

S1. Additional structural details.

Figure S Packing of compound 1 along the c axis viewing direction.

Figure S Packing of compound 1 along the a axis viewing direction.

S2. Continuous Shape Measurements (CShMs).

Table S1. Continuous Shape Measurements for the coordination environments for compound 1. The lowest SHAPE values are shown in bold blue, indicating best fits.

Codes:

HP-7            	1 D7h   Heptagon

HPY-7		2 C6v   Hexagonal pyramid

PBPY-7	3 D5h   Pentagonal bipyramid

COC-7		4 C3v   Capped octahedron

CTPR-7	5 C2v   Capped trigonal prism

JPBPY-7	6 D5h   Johnson pentagonal bipyramid J13

JETPY-7	7 C3v   Johnson elongated triangular pyramid J7

| Structure [ML7] | HP-7 | HPY-7 | PBPY-7 | COC-7 | CTPR-7 | JPBPY-7 | JETPY-7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pb1 | 32.503 | 19.509 | 5.861 | 2.872 | 2.159 | 9.258 | 20.855 |

Codes:

OP-8		1 D8h   Octagon

HPY-8		2 C7v   Heptagonal pyramid

HBPY-8	3 D6h   Hexagonal bipyramid

CU-8		4 Oh    Cube

SAPR-8	5 D4d   Square antiprism

TDD-8		6 D2d   Triangular dodecahedron

JGBF-8		7 D2d   Johnson gyrobifastigium J26

JETBPY-8        8 D3h   Johnson elongated triangular bipyramid J14

JBTPR-8	9 C2v	Biaugmented trigonal prism J50

BTPR-8	10 C2v   Biaugmented trigonal prism

JSD-8		11 D2d	Snub diphenoid J84

TT-8		12 Td	Triakis tetrahedron

ETBPY-8	13 D3h	Elongated trigonal bipyramid

| Structure [ML8] | OP-8 | HPY-8 | HBPY-8 | CU-8 | SAPR-8 | TDD-8 | JGBF-8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pb2 | 27.041 | 24.070 | 16.303 | 10.258 | 1.768 | 3.401 | 13.684 |

| Structure [ML8] | JETBPY-8 | JBTPR-8 | BTPR-8 | JSD-8 | TT-8 | ETBPY-8 |
| --- | --- | --- | --- | --- | --- | --- |
| Pb2 | 24.012 | 3.876 | 3.624 | 5.445 | 10.587 | 19.375 |

Codes:

DP-12		1 D12h	Dodecagon

HPY-12	2 C11v	Hendecagonal pyramid

DBPY-12	3 D10h	Decagonal bipyramid

HPR-12	4 D6h	Hexagonal prism

HAPR-12	5 D6d	Hexagonal antiprism

TT-12		6 Td	Truncated tetrahedron

COC-12	7 Oh	Cuboctahedron

ACOC-12	8 D3h	Anticuboctahedron J27

IC-12		9 Ih	Icosahedron

JSC-12		10 C4v 	Johnson square cupola J4

JEPBPY-12	11 D6h	Johnson elongated pentagonal bipyramid J16

JBAPPR-12	12 C2v	Biaugmented pentagonal prism J53

JSPMC-12	13 Cs	Sphenomegacorona J88

| Structure [ML12] | DP-12 | HPY-12 | DBPY-12 | HPR-12 | HAPR-12 | TT-12 | COC-12 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Pb3 | 31.836 | 28.687 | 19.525 | 10.661 | 17.152 | 11.788 | 1.830 |

| Structure [ML12] | ACOC-12 | IC-12 | JSC-12 | JEPBPY-12 | JBAPPR-12 | JSPMC-12 |
| --- | --- | --- | --- | --- | --- | --- |
| Pb3 | 7.325 | 5.604 | 20.646 | 11.573 | 12.422 | 19.913 |

S3. Powder X-ray Diffraction Analysis.

Figure S	Pattern-matching analysis of polycrystalline sample of compound 1.

S4. FT-IR spectroscopy.

Infrared spectroscopy was used as an initial characterization technique to check the presence of pmdc in compound 1 (Figure S4). Table S2 shows the wavenumbers of the most relevant bands, together with their relative intensities and the proposed assignation in each case for the compound 1.

The spectrum of compound 1 shows a broad and intense band in frequency region of 3550-3100 cm-1, assigned to the characteristic peaks of OH vibration of free water molecules and to the C-H vibration of the pyrimidinic ring of the pmdc ligand. The intense vibrations around 1650 cm-1 and 1360 cm-1 correspond to the asymmetric and symmetric stretching vibrations of the carboxylate groups. At 1385 cm-1 appears the strong vibration of the nitrate anion, while in the 1300-1000 cm-1 region several medium- and weak-intensity peaks appear that can be attributed to the distortions originated in the aromatic ring of pmdc ligand. The vibration bands of the M-O and M-N bonds are observed below 550 cm-1.

Table S2. Main IR absorption bands (cm–1) for the compound 1.a

| Asig.b | Compound 1 |
| --- | --- |
| ν (O–H) | 3470m, 3170m |
| ν (C–H) | 3075m |
| νas(O–C–O) + ν (C=C + C=N) | 1635s, 1600s, 1585sh, 1535s |
| ν (Car–C) | 1460w |
| νs (O–C–O) | 1360s, 1305w |
| ν (NO3) | 1385s |
| δip(C–H) | 1285m, 1185m, 1095w, 1040w, 1015m |
| δop(C–H) | 940w |
| δring | 835m |
| δip(O–C–O) | 810m |
| δop(O–C–O) | 730s, 715ss |
| τring | 695m, 670m, 560w |
| ν (M–O + M–N) | 505w, 485w, 445w, 415w |

a vs: very strong, s: strong, m: medium, w: weak, sh: shoulder. b ν: stretching, δ: bending, ip: inside plane, op: out of plane, s: symmetric, as: antisymmetric.

Figure S	Comparison of the FTIR spectra of compound 1 and the free H2pmdc ligand.

S5. Photoluminescence measurements and calculations.

Figure S	Excitation (λem = 435 nm) and emission (λex = 335 nm) spectra of H2pmdc ligand recorded at room temperature.

The emission lifetimes were estimated by measuring the decay curves for both maxima. The signal for the first maximum was so weak and the lifetime quite short so it was estimated by deconvolution. On the contrary, the lifetime of the maximum at 550 nm was estimated by tail fitting procedure and gave two components of 5.71(59) µs with a weight of 40% and a second component of 116.4(34) µs with a weight of 60%.

Figure S	Decay curves of the emission of compound 1 at room temperature for the main emission maxima.

Figure S	Monomeric model taking from the X-ray coordinates used for the calculations of the PL properties of compound 1.

Table S3. Calculated main excitation and emission energies (nm), singlet electronic transitions and associated oscillator strengths of model of compound 1 in gas phase.

| Exc. state | Calcd. λ (nm) | Significant contributions | Osc. strength (a.u.) |
| --- | --- | --- | --- |
| Excitation energies |  |  |  |
| 7 | 395 | HOMO – 5 → LUMO (99%) | 0.1421 |
| 10 | 335 | HOMO – 7 → LUMO (99%) | 0.0356 |

Figure S	Emission spectrum of compound 1 collected at 15 K under monochromatic laser light (λex = 325 nm).

Figure S	Comparison of the low temperature excitation spectra collected over the two maxima observed in the emission of compound 1.

The emission lifetimes for the low temperature decay curves were estimated with the same fitting procedure explained for RT measurements by measuring the decay curves for both maxima. The signal for the first maximum was so weak and the lifetime quite short so it was estimated by deconvolution. On the contrary, the lifetime of the maximum at 550 nm was estimated by tail fitting procedure and gave two components of 5.71(59) µs with a weight of 40% and a second component of 116.4(34) µs with a weight of 60%.

Figure S	Decay curves of the emission of compound 1 at low temperature for the main emission maxima.

Figure S	TRES recorded at 15 K for compound 1 showing a selection of spectra.

S6. Diffuse reflectance.

Figure S	Diffuse reflectance spectrum acquired on polycrystalline sample of compound 1.