# Supplementary Materials

Single crystal structure analysis of two novel iron(II) coordination polymers with bridging 1,3,5-tris(1H-1,2,4-triazol-1-yl)methyl)benzene

Aysenur Limon 1, Dustin N. Jordan 1, Till Strothmann 1, Laure P. Cuignet 1,2, Yann Garcia 2, and Christoph Janiak *,1

1 Institut für Anorganische Chemie und Strukturchemie, Heinrich-Heine-Universität, Universitätsstraße 1, 40225 Düsseldorf, Germany

2 Institute of Condensed Matter and Nanosciences, Molecular Chemistry, Materials and Catalysis (IMCN/MOST), Université Catholique de Louvain, 1348 Louvain-la-Neuve, Belgium

Emails: aysenur.limon@uni-duesseldorf.de, dustin.jordan@uni-duesseldorf.de, till.strothmann@uni-duesseldorf.de, laure.cuignet@sciensano.be, yann.garcia@uclouvain.be, janiak@uni-duesseldorf.de

Content

S1	Used chemicals

S2	Ligand analyses

S3	Infrared spectra of 1-3

S4	Thermogravimetric analyses of 1-3

S5	Crystal images of 1-3

S6	Crystal data of 1-3

S7	Distortion of the Fe coordination polyhedra of 1-3

S8	Powder X-ray diffraction patterns of 1-3

S9	References

S1	Used chemicals

Table S1. Overview of used chemicals.

| Chemical | Supplier | Purity |
| --- | --- | --- |
| 1,2,4-Triazole | BLDpharm | 97% |
| 1,3,5-Tris(bromomethyl)benzene | BLDpharm | 99.44% |
| Acetonitrile | Riedel-de Haën | 99.9% |
| Ascorbic acid | Roth | 99% |
| Chloroform | Fisher | 99.8% |
| DSMO-d6 | Sigma-Aldrich | 99.9% |
| Ethanol | Chemsolute | 99.9% |
| Fe(BF4)2·6H2O | Merck | 97% |
| Fe(ClO4)2·xH2O | Sigma-Aldrich | 98% |
| KOH | Merck | p.a. |
| MgSO4 | Fisher Chemical | 99% |
| (NH4)2Fe(SO4)2·6H2O | Fluka | 99% |
| NH4SCN | Riedel-de Haën | 99% |

S2	Ligand analyses

To eliminate the water signals in the spectrum, the sample was dried at 60 °C in vacuo before the analyses.

Figure S1. 1H-NMR spectrum (300 MHz, DMSO-d6) of ttmb. The water peak of the used DMSO-d6 is still visible since it is difficult to avoid the content of water in the solvent.

Figure S2. 13C{1H}-NMR spectrum (75 MHz, DMSO-d6) of ttmb.

Figure S3. IR spectrum of ttmb (ATR).

Figure S4. TGA of ttmb (heating rate 5 K min–1).

S3	Infrared spectra of 1-3

Figure S5. IR spectrum of 1 (ATR).

Figure S6. IR spectrum of 2 (ATR).

Figure S7. IR spectrum of 3 (ATR).

S4	Thermogravimetric analyses of 1-3

Figure S8. TGA of 1 (heating rate 5 K min–1). Caution! If 1 is dried at 60 °C in vacuo before the TGA, an explosion is visible at 200 °C.

Figure S9. TGA of 2 (heating rate 5 K min–1).

Figure S10. TGA of 3 (heating rate 5 K min–1).

S5	Crystal images of 1-3

Figure S11. Crystal image of 1.

Figure S12. Crystal image of 2.

Figure S13. Crystal image of 3.

S6	Crystal data of 1-3

Table S2. Crystal data for compounds 1-3.

| Compound | 1 | 2 | 3 |
| --- | --- | --- | --- |
| CCDC no. | 2297073 | 2297074 | 2297075 |
| Empirical formula | C30H34FeN18O2·2(ClO4)·4(H2O) | C30H34FeN18O2·2(BF4)·4(H2O) | C32H30FeN20S2 |
| Mr [g/mol] | 1005.56 | 980.28 | 814.73 |
| Temperature [K] | 294 | 273 | 298 |
| Crystal system | Monoclinic | Monoclinic | Triclinic |
| Space group | P21/n | P21/n | P1 |
| a [Å] | 8.9918(1) | 8.9379(8) | 8.5918(4) |
| b [Å] | 18.0165(2) | 17.9291(16) | 9.4947(3) |
| c [Å] | 13.4614(2) | 13.4514(13) | 11.7005(3) |
| α [°] | 90 | 90 | 80.490(2) |
| β [°] | 91.565(1) | 91.562(4) | 85.194(3) |
| γ [°] | 90 | 90 | 89.497(3) |
| Volume [Å3] | 2179.94(5) | 2154.8 | 938.05 |
| Z | 2 | 2 | 1 |
| ρcalc [g/cm3] | 1.532 | 1.511 | 1.442 |
| μ [mm–1] | 4.64 | 0.45 | 4.72 |
| F(000) | 1040 | 1008 | 420 |
| Crystal size [mm3] | 0.37 × 0.19 × 0.08 | 0.5 × 0.2 × 0.2 | 0.13 × 0.07 × 0.06 |
| Wavelength [Å] | 1.54184 | 0.71073 | 1.54184 |
| No. of unique reflections | 3890 | 4915 | 3321 |
| No. of total reflections | 16794 | 15411 | 10116 |
| Rint | 0.040 | 0.024 | 0.039 |
| R[F2 > 2s(F2)] | 0.045 | 0.044 | 0.038 |
| wR(F2) | 0.127 | 0.138 | 0.104 |

Table S3. Selected bond lengths and bond angles for 1-3.

| Compound 1 |  |  |  |
| --- | --- | --- | --- |
| Bond lengths [Å] |  |  |  |
| Fe1—O1 | 2.0745(19) | Fe1—N1i | 2.2014(19) |
| Fe1—O1i | 2.0746(19) | Fe1—N7ii | 2.227(2) |
| Fe1—N1 | 2.2014(19) | Fe1—N7iii | 2.227(2) |
| Bond angles [°] |  |  |  |
| O1—Fe1—O1i | 180.00(4) | O1—Fe1—N7ii | 91.48(8) |
| O1i—Fe1—N1 | 93.54(8) | N1—Fe1—N1i | 180.0 |
| O1i—Fe1—N1i | 86.46(8) | N1i—Fe1—N7ii | 93.34(7) |
| O1—Fe1—N1 | 86.46(8) | N1—Fe1—N7ii | 86.66(7) |
| O1—Fe1—N1i | 93.54(8) | N1i—Fe1—N7iii | 86.66(7) |
| O1i—Fe1—N7ii | 88.52(8) | N1—Fe1—N7iii | 93.34(7) |
| O1i—Fe1—N7iii | 91.48(8) | N7ii—Fe1—N7iii | 180.00(11) |
| O1—Fe1—N7iii | 88.52(8) |  |  |
| Symmetry transformations: i = -x+1, -y+1, -z; ii = -x+1, -y+1, -z+1; iii = x, y, z-1; iv = x, y, z+1. (v) -x+2, -y+1, -z+1; vi = x-1/2, -y+3/2, z-1/2; vii = -x+3/2, y-1/2, -z+3/2; viii = x+1, y, z+1. |  |  |  |

| Compound 2 |  |  |  |
| --- | --- | --- | --- |
| Bond lengths [Å] |  |  |  |
| Fe1—O1i | 2.0781(14) | Fe1—N1 | 2.1940(15) |
| Fe1—O1 | 2.0781(14) | Fe1—N9ii | 2.2179(16) |
| Fe1—N1i | 2.1940(15) | Fe1—N9iii | 2.2179(16) |
| Bond angles [°] |  |  |  |
| O1i—Fe1—O1 | 180.0 | O1i—Fe1—N9ii | 91.60(7) |
| O1—Fe1—N1 | 93.72(6) | N1—Fe1—N1i | 180.00(8) |
| O1—Fe1—N1i | 86.28(6) | N1i—Fe1—N9ii | 93.50(6) |
| O1i—Fe1—N1 | 86.28(6) | N1—Fe1—N9ii | 86.50(6) |
| O1i—Fe1—N1i | 93.72(6) | N1—Fe1—N9iii | 93.50(6) |
| O1—Fe1—N9ii | 88.40(6) | N1i—Fe1—N9iii | 86.50(6) |
| O1—Fe1—N9iii | 91.60(7) | N9ii—Fe1—N9iii | 180.0 |
| O1i—Fe1—N9iii | 88.40(6) |  |  |
| Symmetry transformations: i = −x+2, −y+1, −z+2; ii = −x+2, −y+1, −z+1; iii = x, y, z+1; iv = x, y, z−1; v = −x+1, −y+1, −z+1; vi = −x+3/2, y+1/2, −z+3/2. |  |  |  |

| Compound 3 |  |  |  |
| --- | --- | --- | --- |
| Bond lengths [Å] |  |  |  |
| Fe1—N1i | 2.1813(17) | Fe1—N7iii | 2.2150(17) |
| Fe1—N1 | 2.1813(17) | Fe1—N10 | 2.143(2) |
| Fe1—N7ii | 2.2150(17) | Fe1—N10i | 2.143(2) |
| Bond angles [°] |  |  |  |
| N1i—Fe1—N1 | 180.0 | N10i—Fe1—N1i | 90.09(7) |
| N1—Fe1—N7ii | 95.59(6) | N10—Fe1—N1 | 90.09(7) |
| N1i—Fe1—N7iii | 95.59(6) | N10—Fe1—N7ii | 89.32(7) |
| N1—Fe1—N7iii | 84.41(6) | N10i—Fe1—N7iii | 89.32(7) |
| N1i—Fe1—N7ii | 84.41(6) | N10i—Fe1—N7ii | 90.68(7) |
| N7ii—Fe1—N7iii | 180.00(9) | N10—Fe1—N7iii | 90.68(7) |
| N10—Fe1—N1i | 89.91(7) | N10—Fe1—N10i | 180.0 |
| N10i—Fe1—N1 | 89.91 (7) |  |  |
| Symmetry transformations: i = -x+1, -y+2, -z; ii = x, y+1, z-1; iii = -x+1, -y+1, -z+1; iv = x, y-1, z+1; v = -x, -y+1, -z+1; vi = x, y-1, z. |  |  |  |

Table S4. Hydrogen-bond geometry for 1-3.

| Compound 1 |  |  |  |  |
| --- | --- | --- | --- | --- |
| D—H···A | D—H [Å] | H···A [Å] | D···A [Å] | D—H···A [°] |
| C1—H1···N8v | 0.93 | 2.50 | 3.346 (3) | 151 |
| C2—H2···O6vi | 0.93 | 2.44 | 3.264 (4) | 148 |
| C10—H10A···N2ii | 0.97 | 2.65 | 3.572 (4) | 158 |
| C12—H12···O6vii | 0.87 (4) | 2.51 (4) | 3.279 (5) | 148 (4) |
| C13—H13A···O2viii | 0.97 | 2.59 | 3.436 (4) | 145 |
| C15—H15···O7 | 0.93 | 2.54 | 3.386 (5) | 152 |
| O2—H2A···N5 | 1.03 | 2.31 | 2.904 | 115 |
| O3—H3C···N2 | 0.96 | 2.17 | 3.020 | 148 |
| O1—H1A···O2 | 0.74 | 1.90 | 2.643 | 176 |
| O2—H2A···O7 | 1.03 | 2.50 | 3.435 | 151 |
| O2—H2B···O3 | 0.91 | 1.87 | 2.745 | 160 |
| O3—H3D···O4 | 1.04 | 2.57 | 3.050 | 108 |
| O3—H3D···O5 | 1.04 | 2.48 | 3.424 | 152 |
| Symmetry transformations: ii = -x+1, -y+1, -z+1; v = -x+2, -y+1, -z+1; vi = x-1/2, -y+3/2, z-1/2; vii = -x+3/2, y-1/2, -z+3/2; viii = x+1, y, z+1. |  |  |  |  |

| Compound 2 |  |  |  |  |
| --- | --- | --- | --- | --- |
| D—H···A | D—H [Å] | H···A [Å] | D···A [Å] | D—H···A [°] |
| C1—H1···F4Bi | 0.93 | 2.50 | 3.218(7) | 134 |
| C1—H1···F4Ai | 0.93 | 2.47 | 3.308(8) | 151 |
| C2—H2···N8v | 0.93 | 2.49 | 3.329(3) | 151 |
| C10—H10A···N3ii | 0.97 | 2.61 | 3.537(3) | 161 |
| C12—H12···F4Biv | 0.93 | 2.45 | 3.362(9) | 167 |
| C12—H12···F2Aiv | 0.93 | 2.55 | 3.290(9) | 136 |
| C12—H12···F4Aiv | 0.93 | 2.40 | 3.196(6) | 144 |
| C13—H13A···O2v | 0.97 | 2.58 | 3.419(3) | 145 |
| C14—H14···F2Bvi | 0.93 | 2.46 | 3.243(8) | 142 |
| C14—H14···F2Avi | 0.93 | 2.51 | 3.357(10) | 152 |
| O2—H2A···N5 | 0.85 | 2.32 | 2.895(27) | 125 |
| O3—H3C···N3 | 0.85 | 2.36 | 3.025(34) | 136 |
| O1—H1A···O2 | 0.85 | 1.78 | 2.626(27) | 177 |
| O2—H2B···O3 | 0.85 | 1.88 | 2.723(40) | 170 |
| Symmetry transformations: i = −x+2, −y+1, −z+2; ii = −x+2, −y+1, −z+1; iv = x, y, z−1; v = −x+1, −y+1, −z+1; vi = −x+3/2, y+1/2, −z+3/2. |  |  |  |  |

| Compound 3 |  |  |  |  |
| --- | --- | --- | --- | --- |
| D—H···A | D—H [Å] | H···A [Å] | D···A [Å] | D—H···A [°] |
| C2—H2···N8v | 0.93 | 2.45 | 3.256 (3) | 146 |
| C12—H12···N2iii | 0.93 | 2.64 | 3.484 (4) | 152 |
| C13—H13B···S1vi | 0.97 | 2.75 | 3.668 (2) | 157 |
| C15—H15···S1iii | 0.93 | 2.98 | 3.877 (2) | 163 |
| Symmetry transformations: iii = -x+1, -y+1, -z+1; v = -x, -y+1, -z+1; vi = x, y-1, z. |  |  |  |  |

S7	Distortion of the Fe coordination polyhedra of 1-3

The indices for distortion were calculated using OctaDist software [1]. The distortion parameters were calculated as follows:

ζ parameter [2]: ζ= i=16di-dmean

di: individual M–L bond distance

dmean: mean metal-ligand bond distance

Σ parameter [3]: Σ= i=11290-ϕi

ϕ: individual cis angle

θ parameter [4]: θ= i=12460-θi

θi: individual angle between two vectors of two twisting face

These parameters are zero for a perfect octahedron.

The values Σ and θ are derived by summation over the absolute values of all 12 differences 90 – ϕi and 24 differences 60 – i, respectively, in the octahedron. The angles ϕi and i are 90° and 60°, respectively, giving the parameters Σ and θ as zero for a perfect octahedron [1]. However, a very small deviation in ϕi and i by only 1° will already result in Σ = 12° and θ = 24°.

The Fe(II) atoms in compound 1-3 are in a somewhat distorted coordination environment [5] (Table S5).

Table S5. Mean M–L distance and values for distortion indices of the metal atom coordination environment in compounds 1-3.

| Compound | M | Mean distance <D> [Å] | Distance distortion ζ [Å] | Angle distortion Σ [°] | Torsional distortion θ [°] |
| --- | --- | --- | --- | --- | --- |
| 1 | Fe1 | 2.17 | 0.37 | 33.47 | 89.64 |
| 2 | Fe1 | 2.16 | 0.34 | 35.27 | 93.84 |
| 3 | Fe1 | 2.18 | 0.15 | 25.52 | 103.91 |

S8	Powder X-ray diffraction patterns of 1-3

Figure S14. Powder X-ray diffraction pattern of 1 compared to the simulation with preferred orientation (h = -7, k = 0, l = -6, March-Dollase = 10).

Figure S15. Powder X-ray diffraction pattern of 2 compared to the simulation with preferred orientation (h = -6, k = 0, l = -3, March-Dollase =5).

Figure S16. Powder X-ray diffraction pattern of 3 compared to the simulation with preferred orientation (h = -2, k = 8, l = -16, March-Dollase = 3).

S9	References

Ketkaew, R.; Tantirungrotechai, Y.; Harding, P.; Chastanet, G.; Guionneau, P.; Marchivie, M.; Harding, D.J. OctaDist: a tool for calculating distortion parameters in spin crossover and coordination complexes. Dalton Trans. 2021, 50, 1086–1096. https://doi.org/10.1039/d0dt03988h

Buron-Le Cointe, M.; Hébert, J.; Baldé, C.; Moisan, N.; Toupet, L.; Guionneau, P.; Létard, J.F.; Freysz, E.; Cailleau, H.; Collet, E. Intermolecular control of thermoswitching and photoswitching phenomena in two spin-crossover polymorphs. Phys. Rev. B 2012, 85, 064114. https://doi.org/10.1103/PhysRevB.85.064114

McCusker, J.K.; Rheingold, A.L.; Hendrickson, D.N. Variable-Temperature Studies of Laser-Initiated 5 T 2 → 1 A 1 Intersystem Crossing in Spin-Crossover Complexes: Empirical Correlations between Activation Parameters and Ligand Structure in a Series of Polypyridyl Ferrous Complexes. Inorg. Chem. 1996, 35, 2100–2112. https://doi.org/10.1021/ic9507880

Marchivie, M.; Guionneau, P.; Létard, J.F.; Chasseau, D. Photo-induced spin-transition: the role of the iron(II) environment distortion. Acta Crystallogr. B 2005, 61, 25–28. https://doi.org/10.1107/S0108768104029751

Avila, Y.; Pérez, O.; Sánchez, L.; Vázquez, M.C.; Mojica, R.; González, M.; Ávila, M.; Rodríguez-Hernández, J.; Reguera, E. Spin crossover in Hofmann-like coordination polymers. Effect of the axial ligand substituent and its position. New J. Chem. 2023, 47, 10781–10795. https://doi.org/10.1039/D3NJ01498C