Supplementary Materials

Optical Evaluation of Dansyl Derivatives and Their Implementation in ‎Low-Cost and Flexible Dye-Doped PMMA Platforms for Efficient ‎Detection of Hazardous Chemical Vapours

Gonçalo Pedro 1, Frederico Duarte 1, Georgi M. Dobrikov *2, Atanas Kurutos 2,3, Hugo M. Santos 1,4, Jose Luis Capelo-Martinez 1,4, Elisabete Oliveira *1,4, and Carlos Lodeiro *1,4

1	BIOSCOPE Research Group, LAQV-REQUIMTE, Chemistry Department, NOVA School of Science and ‎Technology, FCT NOVA, Universidade NOVA de Lisboa, 2829-516 Caparica, Portugal‎

2	Institute of Organic Chemistry with Centre of Phytochemistry, Bulgarian Academy of Sciences,‎ Acad. G. Bonchev str., bl. 9, 1113 Sofia, Bulgaria

3	University of Chemical Technology and Metallurgy, 8 St. Kliment Ohridski blvd, 1756 Sofia, Bulgaria

4	ROTEOMASS Scientific Society, BIOSCOPE Research Group, Departamental Building, Ground floor Caparica ‎Campus, 2829-516 Caparica, Portugal. ‎

*	Correspondence: Georgi.Dobrikov@orgchm.bas.bg (GD); ej.oliveira@fct.unl.pt (EO) and cle@fct.unl.pt (CL)‎

Figure S1. 1H NMR spectrum of L1.

Figure S1. 1H NMR spectrum of L1 (details).

Figure S1. 1H NMR spectrum of L1 (details).

Figure S1. 1H NMR spectrum of L1 (details).

Figure S1. 1H NMR spectrum of L1 (details).

Figure S1. 1H NMR spectrum of L1 (details).

Figure S1. 1H NMR spectrum of L1 (details).

Figure S1. 13C NMR spectrum of L1.

Figure S1. COSY-NMR spectrum of L1.

Figure S1. COSY-NMR spectrum of L1 (details).

Figure S1. COSY-NMR spectrum of L1 (details).

Figure S1. COSY-NMR spectrum of L1 (details).

Figure S1. COSY-NMR spectrum of L1 (details).

Figure S1. HSQC-NMR spectrum of compound L1.

Figure S1-14. HSQC-NMR spectrum of compound L1.

Figure S1. HSQC-NMR spectrum of compound L1 (details).

Figure S1. HSQC-NMR spectrum of compound L1 (details).

Figure S1. HSQC-NMR spectrum of compound L1 (details).

Figure S1. HSQC-NMR spectrum of compound L1 (details).

Figure S2. 1H-NMR spectrum of compound 2.

Figure S2. 1H-NMR spectrum of compound 2 (details).

Figure S2. 1H-NMR spectrum of compound 2 (details).

Figure S2. 13C-NMR spectrum of compound 2.

Figure S2. 13C-NMR spectrum of compound 2 (details).

Figure S2. 13C-NMR spectrum of compound 2 (details).

Figure S2. COSY-NMR spectrum of L2.

Figure S2. COSY-NMR spectrum of L2.

Figure S2. COSY-NMR spectrum of L2.

Figure S2. COSY-NMR spectrum of L2.

Figure S2. HSQC-NMR spectrum of L2.

Figure S2. HSQC-NMR spectrum of L2.

Figure S2. HSQC-NMR spectrum of L2.

Figure S3. 1H NMR spectrum of L3.

Figure S3. 1H NMR spectrum of L3 (details).

Figure S3. 1H NMR spectrum of L3 (details).

Figure S3. 1H NMR spectrum of L3 (details).

Figure S3. 13C NMR spectrum of L3.

Figure S3. 13C NMR spectrum of L3 (details).

Figure S3. 13C NMR spectrum of L3 (details).

Figure S3. COSY NMR spectrum of L3.

Figure S3. COSY NMR spectrum of L3.

Figure S3. COSY NMR spectrum of L3.

Figure S3. HSQC NMR spectrum of L3.

Figure S3. HSQC NMR spectrum of L3.Figure S3-12. HSQC NMR spectrum of L3.	.

Figure S4. 1H NMR spectrum of L4.

Figure S4. 1H NMR spectrum of L4.

Figure S4. 1H NMR spectrum of L4.

Figure S4. 1H NMR spectrum of L4.

Figure S4. 13C NMR spectrum of L4.

Figure S4. 13C NMR spectrum of L4.

Figure S4. 13C NMR spectrum of L4.

Figure S4. COSY NMR spectrum of L4.

Figure S4. COSY NMR spectrum of L4.

Figure S4. COSY NMR spectrum of L4.

Figure S4. HSQC NMR spectrum of L4.

Figure S4. COSY NMR spectrum of L4.

Figure S4. COSY NMR spectrum of L4.

Figure S5. 1H NMR spectrum of L5.

Figure S5. 1H NMR spectrum of L5.

Figure S5. 1H NMR spectrum of L5.

Figure S5-4. 1H NMR spectrum of L5.

Figure S5. 13C NMR spectrum of L5.

Figure S5. 13C NMR spectrum of L5.

Figure S5. COSY NMR spectrum of L5.

Figure S5. COSY NMR spectrum of L5.

Figure S5. COSY NMR spectrum of L5.

Figure S5. HSQC NMR spectrum of L5.

Figure S5. HSQC NMR spectrum of L5.

Figure S5. HSQC NMR spectrum of L5.

Figure S5. HSQC NMR spectrum of L5.

Figure S6. 1H NMR spectrum of L6.

Figure S6. 1H NMR spectrum of L6.

Figure S6. 1H NMR spectrum of L6.

Figure S6. 1H NMR spectrum of L6.

Figure S6. 13C NMR spectrum of L6.

Figure S6. 13C NMR spectrum of L6.

Figure S6. 13C NMR spectrum of L6.

Figure S6. COSY NMR spectrum of L6.

Figure S6. COSY NMR spectrum of L6.

Figure S6. COSY NMR spectrum of L6.

Figure S6. HSQC NMR spectrum of L6.

Figure S6-12. HSQC NMR spectrum of L6.

Figure S6-13. HSQC NMR spectrum of L6.

Figure S6-14. HSQC NMR spectrum of L6.

Figure S6-15. HSQC NMR spectrum of L6.

Figure S6-16. HSQC NMR spectrum of L6.

.

Figure S7-1. ESI-HRMS spectrum of compound L1.

Figure S7-2. ESI-HRMS spectrum of compound L2.

Figure S7-3. ESI-HRMS spectrum of compound L3.

Figure S7-4. ESI-HRMS spectrum of compound L4.

Figure S7-5. ESI-HRMS spectrum of compound L5.

Figure S7-6. ESI-HRMS spectrum of compound L6.

Figure S8. Photophysical characterization of compound L1 in A) CH3CN B) EtOH, C) DMSO, D) THF ([L] = 10 mM) and E) CHCl3 ([L] = 3 mM) excL1= 341 nm, T = 298 K.

Figure S9. Photophysical characterization of compound L2 in a) CH3CN b) CHCl3, c) DMSO, d) EtOH, e) THF ([L] = 10 mM). excL2= 350 nm, T = 298 K.

Figure S10. Photophysical characterization of compound L3 in a) CH3CN b) CHCl3, c) DMSO, d) EtOH, e) THF ([L] = 10 mM). excL3= 351 nm, T = 298 K.

Figure S11. Photophysical characterization of compound L4 in a) CH3CN b) CHCl3, c) DMSO, d) EtOH, e) THF ([L] = 10 mM). excL4= 350 nm, T = 298 K.

Figure S12. Photophysical characterization of compound L5 in a) CH3CN b) CHCl3, c) DMSO, d) EtOH, e) THF ([L] = 10 mM). excL5= 342 nm, T = 298 K.

Figure S13. Photophysical characterization of compound L6 in a) CH3CN b) CHCl3, c) DMSO, d) EtOH, e) THF ([L] = 10 mM). excL6= 350 nm, T = 298 K.

Figure S14. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L2 with increased additions of Cu2+ (A, B), and Hg2+ (C, D) in CH3CN. The inset represents the absorption (A, C) and emission (B-D) as a function of [Cu2+]/[L2] and [Hg2+]/[L2], respectively. [L2] = 20 µM, excL2= 350 nm, T = 298 K).

Figure S15. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L3 with increased additions of Cu2+ (A, B), and Hg2+ (C, D) in CH3CN. The inset represents the absorption (A, C) and emission (B-D) as a function of [Cu2+]/[L3] and [Hg2+]/[L3], respectively. [L3] = 20 µM, excL3= 352 nm, T = 298 K).

Figure S16. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L4 with increased additions of Cu2+ (A, B), and Hg2+ (C, D) in CH3CN. The inset represents the absorption (A, C) and emission (B-D) as a function of [Cu2+]/[L4] and [Hg2+]/[L4], respectively. [L4] = 20 µM, excL4= 348nm, T = 298 K).

Figure S17. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L6 with increased additions of Cu2+ (A, B), and Hg2+ (C, D) in CH3CN. The inset represents the absorption (A, C) and emission (B-D) as a function of [Cu2+]/[L6] and [Hg2+]/[L6], respectively. [L6] = 20 µM, excL6= 350 nm, T = 298 K).

Figure S18. Maximum emission intensities of L2 A), L3 (B), L4 (C), L6 (D) upon the addition of 1, 2 and 10 equivalents of Ag+, Cd2+, Cu2+,Hg2+, Zn2+metal ions. ([L] = 20 μM, λemL2= 527 nm, λemL3 = 521 nm , λemL4 = 530 nm, λemL6 = 532 nm T = 298 K). excL2= 350 nm, excL3= 352 nm, excL4= 348nm, excL6= 350 nm.

Figure S19. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L2 with increased additions of HCl (A, B), and ammonia (C, D) in CH3CN. [L2] = 20 µM, excL2=350 nm, T = 298 K).

Figure S20. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L4 with increased additions of HCl (A, B), and ammonia (C, D) in CH3CN. [L4] = 20 µM, excL4=348 nm, T = 298 K).

Figure S21. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L5 with increased additions of HCl (A, B), and ammonia (C, D) in CH3CN. [L5] = 20 µM, excL5=340 nm, T = 298 K).

Figure S22. Spectrophotometric and spectrofluorometric titrations of dansyl derivative L6 with increased additions of HCl (A, B), and ammonia (C, D) in CH3CN. [L6] = 20 µM, excL6=350 nm, T = 298 K).

Figure S23. (A, C, E, G) Emission spectra of successive immersion of L2, L4, L5, L6 doped PMMA polymer film in a conc. HCl solution (5m in 5min) (B, D, F, H) Emission spectra of exposure to HCl vapors (20m in 20m) of L2, L4, L5 and L6 doped PMMA polymers. excL2= 350 nm, excL4= 348 nm, excL5= 342nm, excL6= 350 nm. T=298K.

Figure S24. Emission spectra of L2 (A), L4 (B), L5 (C) and L6 (D) immersion in the HCl concentrations from 0 to 12 M. excL2= 350 nm, excL4= 348 nm, excL5= 342nm, excL6= 350 nm. T=298K.

Figure S25. Emission intensity of L1@PMMA (A), L2@PMMA (B), L4@PMMA (C), L5@PMMA (D) and L6@PMMA after successive cycles of HCl/NH3 immersion.  excL1= 341 nm, excL2= 350 nm, excL4= 348 nm, excL5= 342nm, excL6= 350 nm. T=298K.