Supporting Information

Enhancing the storage performance and thermal stability of Ni-rich layered cathodes by introducing Li2MnO3

Jun Yang,*a Pingping Yang,a Hongyu Wang b

a School of Materials Science & Engineering, Shaanxi Key Laboratory of Green Preparation and Functionalization for Inorganic Materials, Shaanxi University of Science & Technology, Xi'an, Shaanxi, 710021, People's Republic of China. E-mail: yangjuncl@sust.edu.cn.

b Qinghai Provincial Key Laboratory of New Light Alloys, Qinghai University, Xining, Qinghai, 810016, People's Republic of China.

Table S1 Fitting values of the electrochemical impedance (EIS) curves of the cathodes charged to 4.3 V before and after storage obtained from equivalent circuit in the inset of Figure 5.

| Samples |  |  |  | Rf (Ω) | Rct (Ω) | Total (Rf +Rct) |
| --- | --- | --- | --- | --- | --- | --- |
| NCM-811 |  | Before storage | 59 |  | 62 | 121 |
|  |  | After storage | 98 |  | 163 | 261 |
| LNCMO-1090 |  | Before storage | 64 |  | 77 | 141 |
|  |  | After storage | 90 |  | 147 | 237 |

Table S2 The first discharge capacity and 50th discharge capacity before and after storage and the capacity retention after 50 cycles at 0.1 C of the cathode materials of NCM-811 and LNCMO-1090.

| Samples |  |  | First discharge capacity (mAh g-1) | 50th discharge capacity (mAh g-1) | Capacity retention (%) |
| --- | --- | --- | --- | --- | --- |
| NCM-811 |  | Before storage | 224 | 184 | 82.2 |
|  |  | After storage | 219 | 117 | 53.4 |
| LNCMO-1090 |  | Before storage | 207 | 175 | 84.6 |
|  | After storage |  | 201 | 126 | 62.9 |

Figure S1 The charge/discharge profiles at different cycles of (a, b) the NCM-811 and (c, d) LNCMO-1090 cathodes before and after storage at a rate of 0.1 C between 2.0 and 4.5 V vs Li/Li+: (a, c) before storage, (b, d) after storage.

Figure S2 The charge/discharge profiles at different rates of (a, b) the NCM-811 and (c, d) LNCMO-1090 cathodes before and after storage between 2.0 and 4.5 V vs Li/Li+: (a, c) before storage, (b, d) after storage.

Figure S3 The capacity retention at different rates of (a, b) the NCM-811 and (c, d) LNCMO-1090 cathodes before and after storage between 2.0 and 4.5 V vs Li/Li+.