Efficient photocatalytic core/shell of titanate nanowire/rGO

Xiaofang Ye,1,‡ Yang Tian,2,‡ Mengyao Gao,1,‡ Fangjun Cheng,1 Jinshen Lan,1 Han Chen,1 Mark Lanoue,3 Shengli Huang,1,2,4* Z. Ryan Tian2,3,4*

1 Engineering Research Center of Micro-nano Optoelectronic Materials and Devices, Ministry of Education, Fujian Key Laboratory of Semiconductor Materials and Applications, CI Center for OSED, Department of Physics, Xiamen University, Xiamen 361005, China

2 Material Science and Engineering, University of Arkansas, Fayetteville, AR 72701, USA

3 Environmental Dynamics, University of Arkansas, Fayetteville, AR 72701, USA

4 Chemistry and Biochemistry, University of Arkansas, Fayetteville, AR 72701, USA

Contents

- Image of Photocatalytic workstation

- SEM images and EDS spectra of the specimens

- SAED pattern of the specimens

- FTIR spectra of the NWs

- Raman spectra of the specimens

- XPS of the specimens

- UV-Vis spectra of the NWs

- Hyperspectroscopy of the specimens

- Nitrogen adsorption–desorption isotherm of the specimens

- Adsorption spectra of the degraded MB solution under visible and UV light irradiation

- Photocatalytic mechanism

- Image of photocatalytic study setup.

Figure S1. Photocatalytic workstation.

- SEM images and EDS spectra of the specimens

Figure S2. SEM images and EDS spectra of (a1,a2) TiO2 NWs, (b1,b2) TiO2/GO NWs, and (c1,c2) TiO2/rGO NWs.

- SAED pattern of the specimens

Figure S3. Structural and elemental characterization of the specimens SAED pattern.

- FTIR spectra of the specimens

Figure S4. FT-IR spectra of the specimens.

- Raman spectra of the specimens

Figure S5. Raman spectra of the specimens.

- XPS of the specimens

Figure S6. (a) XPS survey spectra; XPS spectra of (b) O 1s, and (c) Ti 2p.

- UV-Vis spectra of the NWs

Figure S7. UV-Vis absorption spectra for GO-Titanate NFs, rGO-Titanate NFs, and Titanate NFs.

- Hyperspectroscopy of the specimens

Figure S8. Hyperspectroscopy for rGO flakes, rGO-Titanate NFs, and Titanate NFs.

- Nitrogen adsorption–desorption isotherm of the specimens

Figure S9. Nitrogen adsorption–desorption isotherm of the specimens

- Adsorption spectra of the degraded MB solution under visible and UV light irradiation

Figure S10. Absorption spectra of degraded MB aqueous solutions as catalyzed by the specimens under visible (a-c) and UV (d-f) light irradiation in different periods: (a)(c) TiO2 NWs, (b)(d) TiO2/GO NWs, and (c)(f) TiO2/rGO NWs.

- Photocatalytic mechanism

Figure S11. Photocatalytic mechanism.

References

- D. Ma, X. Li, Y. Guo, Y. Zeng, Acta Photonica Sinica 2017, 46, 1216002.

- E. Kusiak-Nejman, A. W. Morawski, Applied Catalysis B: Environmental 2019, 253, 179.

- H. Ding, S. Zhang, J. Chen, X. Hu, Z. Du, Y. Qiu, D. Zhao, Thin Solid Films 2015, 584, 29.

- A. Shaikh, S. P. Mishra, P. Mohapatra, S. Parida, Journal of Nanoparticle Research 2017, 19, 206.

- T.-F. Yeh, J.-M. Syu, C. Cheng, T.-H. Chang, H. Teng, Advanced Functional Materials 2010, 20, 2255.