Supplementary Information

Anion and Cation Dynamics in Mixed-Anion Hydroborate Na3(BH4)(B12H12): 1H, 11B, and 23Na NMR Studies

Olga A. Babanova,1 Yolanda Sadikin,2 Roman V. Skoryunov,1 Alexei V. Soloninin,1 and Alexander V. Skripov,1,*

1 Institute of Metal Physics, Ural Division of the Russian Academy of Sciences, S. Kovalevskoi 18, Ekaterinburg 620108, Russia

2 Laboratory of Crystallography, Department of Quantum Matter Physics, University of Geneva, Quai Ernest-Ansermet 24, 1211 Geneva, Switzerland

* Corresponding author. E-mail: skripov@imp.uran.ru

Expressions used for analysis of the proton spin-lattice relaxation rates (two-peak model)

The observed proton spin-lattice relaxation rate is expressed as the sum of contributions resulting from two independent reorientational processes with the H jump rates τi−1:

R1H=iR1iH ,   i = 1, 2 									(S1)

According to our estimates based on the structure of Na3(BH4)(B12H12) [S1], the “rigid-lattice” second moment of the 1H NMR line in this compound is dominated by the dipole-dipole 1H – 1H and 1H – 11B interactions, while contributions due to interactions of 1H nuclei with other nuclei can be neglected. Therefore, only the contributions of the 1H – 1H and 1H – 11B interactions will be considered for the proton spin-lattice relaxation rates.

Since both reorientational processes show distinct signs of a jump rate distribution, we have used the model [S2, S3] based on a Gaussian distribution of the activation energies. For this model, the corresponding contribution to the relaxation rate is expressed as

R1iH=R1iH(Eai)G(Eai,Eai,ΔEai)dEai ,							(S2)

where G(Eai,Eai,ΔEai) is the Gaussian distribution centered on Eai with the dispersion ΔEai, and R1iH(Eai) is given by the standard expressions [S4]

R1iH(Eai)=2ΔMHHiτi311+ωH2τi2+41+4ωH2τi2+ΔMHBiτi211+(ωH−ωB)2τi2+31+ωH2τi2+61+(ωH+ωB)2τi2				(S3)

coupled with the Arrhenius law,

τi=τi0exp(EaikBT) .									(S4)

Here ωH and ωB are the resonance frequencies of 1H and 11B, respectively, and ΔMHHi and ΔMHBi are the parts of the dipolar second moments due to 1H – 1H and 1H – 11B interactions that are caused to fluctuate by the ith reorientational process. Since each of the H – H and H – B terms in Equation (S3) exhibits nearly the same temperature and frequency dependence, it is practically impossible to distinguish the amplitude factors ΔMHHi and ΔMHBi from the fits to the experimental spin-lattice relaxation rate data. Therefore, for the fits we have assumed that ΔMHHi=ΔMHBi=ΔMi.

Fig. S1. Representative shapes of the 23Na NMR spectra at 8 K, 198 K, and 552 K.

References

[S1]	Sadikin, Y.; Brighi, M.; Schouwink, P.; Ĉerný, R. Superionic Conduction of Sodium and Lithium in Anion-Mixed Hydroborates Na3BH4B12H12 and (Li0.7Na0.3)3BH4B12H12. Adv. Energy Mater. 2015, 1501016.

[S2]	Markert, J.T.; Cotts, E.J.; Cotts, R.M. Hydrogen Diffusion in the Metallic Glass a-Zr3RhH3.5. Phys. Rev. B 1988, 37, 6446-6452.

[S3]	Skripov, A.V., Soloninin, A.V.; Babanova O.A.; Hagemann, H.; Filinchuk, Y. Nuclear Magnetic Resonance Study of Reorientational Motion in α-Mg(BH4)2. J. Phys. Chem. C 2010, 114, 12370-12374.

[S4]	Abragam, A. The Principles of Nuclear Magnetism. Clarendon Press: Oxford, 1961.