Supplementary Material

## A Novel Modeling Optimization Approach for a Seven-channel Titania Ceramic Membrane in an Oily Wastewater Filtration System Based on Experimentation, Full Factorial Design, and Machine Learning

Mohamed Echakouri,1 Amr Henni, 1, * Amgad Salama1

1	Process Systems Engineering, Produced Water Treatment Laboratory, Faculty of Engineering and Applied Science, University of Regina; echakoum@uregina.ca

2	Process Systems Engineering, Produced Water Treatment Laboratory, Faculty of Engineering and Applied

Science, University of Regina; amr.henni@uregina.ca

3	Process Systems Engineering, Produced Water Treatment Laboratory, Faculty of Engineering and Applied

Science, University of Regina; amgad.salama@uregina.ca

*	Correspondence: amr.henni@uregina.ca; Tel.: (1 306 585 4960)

Figure S1. Ceramic membrane dimensions: (a) the complete illustration, (b) cross-sectional area, (c) ceramic membrane internal channels and walls.

Figure S2. Contact angles of a Bakken oil droplet at the ceramic membrane surface.

Figure S3. Contact angles of a water droplet at the ceramic membrane surface.

Figure S4. LabBrain crossflow ceramic membrane filtration unit.

Figure S5. LabBrain P&I control loop schematic diagram unit.

Figure S6. Multiple linear regression models

Figure S7. Machine learning flux regression models analysis

All runs for MLR analysis

Table S1. Algorithms models and their training functions fitted for the experimental run 1

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 28.429 | 0.67 | 808.2 | 22.747 | 6.907 |
| 2 | Linear regression | Interactions linear | 28.501 | 0.67 | 812.32 | 22.788 | 26.614 |
| 3 | Linear regression | Robust Linear | 35.131 | 0.49 | 1234.2 | 20.255 | 24.223 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 28.515 | 0.67 | 813.12 | 22.783 | 23.455 |
| 5 | Tree | Fine Tree | 0.69536 | 0.99 | 0.48352 | 0.40585 | 22.87 |
| 6 | Tree | Medium Tree | 1.4311 | 0.99 | 2.0479 | 0.73886 | 21.765 |
| 7 | Tree | Coarse Tree | 3.9243 | 0.99 | 15.4 | 1.9125 | 21.301 |
| 8 | SVM | Linear SVM | 33.464 | 0.54 | 1119.9 | 20.08 | 20.574 |
| 9 | SVM | Quadratic SVM | 14.445 | 0.91 | 208.66 | 9.1763 | 17.922 |
| 10 | SVM | Cubic SVM | 4.484 | 0.99 | 20.106 | 3.3184 | 17.086 |
| 11 | SVM | Fine Gaussian SVM | 11.473 | 0.95 | 131.63 | 5.4515 | 16.651 |
| 12 | SVM | Medium Gaussian SVM | 5.9821 | 0.99 | 35.785 | 3.2133 | 16.014 |
| 13 | SVM | Coarse Gaussian SVM | 20.482 | 0.83 | 419.51 | 10.48 | 15.245 |
| 14 | Ensemble | Boosted Trees | 13.048 | 0.93 | 170.25 | 12.85 | 14.343 |
| 15 | Ensemble | Bagged Trees | 8.3093 | 0.97 | 69.045 | 4.7875 | 13.822 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.11847 | 0.99 | 0.014036 | 0.078545 | 177.84 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.22 | 0.99 | 0.039999 | 0.078125 | 344.26 |
| 18 | Gaussian Process Regression | Exponential GPR | 2.0966 | 0.99 | 4.3958 | 0.66784 | 172.35 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.11581 | 0.99 | 0.013412 | 0.076448 | 632.7 |

Table S2. Algorithms models and their training functions fitted for the experimental run 2

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 43.758 | 0.69 | 1914.8 | 35.093 | 1.2577 |
| 2 | Linear regression | Interactions linear | 43.833 | 0.69 | 1921.3 | 35.102 | 3.5282 |
| 3 | Linear regression | Robust Linear | 52.554 | 0.55 | 2761.9 | 32.171 | 3.3376 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 43.396 | 0.69 | 1930.4 | 35.174 | 3.6711 |
| 5 | Tree | Fine Tree | 1.64412 | 0.99 | 2.6936 | 0.90334 | 3.04441 |
| 6 | Tree | Medium Tree | 3.4007 | 0.99 | 11.565 | 1.727 | 2.7862 |
| 7 | Tree | Coarse Tree | 8.2559 | 0.99 | 68.161 | 4.2186 | 2.5456 |
| 8 | SVM | Linear SVM | 51.327 | 0.57 | 2634.5 | 31.43 | 3.295 |
| 9 | SVM | Quadratic SVM | 21.204 | 0.93 | 449.62 | 13.653 | 4.7413 |
| 10 | SVM | Cubic SVM | 0.244 | 0.99 | 38.988 | 4.8416 | 3.8689 |
| 11 | SVM | Fine Gaussian SVM | 22.668 | 0.92 | 513.83 | 10.961 | 1.7156 |
| 12 | SVM | Medium Gaussian SVM | 10.514 | 0.98 | 110.54 | 5.3972 | 1.0433 |
| 13 | SVM | Coarse Gaussian SVM | 33.249 | 0.82 | 1105.5 | 17.154 | 2.2603 |
| 14 | Ensemble | Boosted Trees | 9.5902 | 0.99 | 91.972 | 8.8499 | 8.3556 |
| 15 | Ensemble | Bagged Trees | 15.807 | 0.96 | 249.87 | 9.2271 | 10.743 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.22253 | 0.99 | 0.04952 | 0.16429 | 117.31 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.3335 | 0.99 | 0.11122 | 0.14526 | 188.22 |
| 18 | Gaussian Process Regression | Exponential GPR | 3.7225 | 0.99 | 13.857 | 1.3026 | 111.69 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.20797 | 0.99 | 0.043251 | 0.14847 | 284.6 |

Table S3. Algorithms models and their training functions fitted for the experimental run 3

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 29.504 | 0.80 | 870.47 | 24.387 | 5.8006 |
| 2 | Linear regression | Interactions linear | 29.561 | 0.79 | 873.84 | 24.379 | 5.5124 |
| 3 | Linear regression | Robust Linear | 30.104 | 0.79 | 906.24 | 23.305 | 4.8347 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 29.579 | 0.79 | 874.94 | 24.416 | 8.074 |
| 5 | Tree | Fine Tree | 1.0089 | 0.99 | 1.0179 | 0.66786 | 7.8541 |
| 6 | Tree | Medium Tree | 2.2571 | 0.99 | 5.0945 | 1.2932 | 7.5005 |
| 7 | Tree | Coarse Tree | 5.8136 | 0.99 | 33.798 | 3.4576 | 7.2166 |
| 8 | SVM | Linear SVM | 33.02 | 0.74 | 1090.3 | 22.623 | 6.8945 |
| 9 | SVM | Quadratic SVM | 10.047 | 0.98 | 100.95 | 7.5186 | 9.1211 |
| 10 | SVM | Cubic SVM | 4.1641 | 0.99 | 17.34 | 3.7413 | 8.8379 |
| 11 | SVM | Fine Gaussian SVM | 14.83 | 0.95 | 219.92 | 8.7513 | 8.5498 |
| 12 | SVM | Medium Gaussian SVM | 5.6381 | 0.99 | 31.788 | 3.6645 | 8.3157 |
| 13 | SVM | Coarse Gaussian SVM | 16.427 | 0.94 | 269.83 | 9.6486 | 8.0373 |
| 14 | Ensemble | Boosted Trees | 12.389 | 0.96 | 153.49 | 12.018 | 9.6828 |
| 15 | Ensemble | Bagged Trees | 12.113 | 0.97 | 146.73 | 7.2512 | 10.084 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.14564 | 0.99 | 0.02121 | 0.098603 | 61.78 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.22425 | 0.99 | 0.050287 | 0.092411 | 90.139 |
| 18 | Gaussian Process Regression | Exponential GPR | 2.3813 | 0.99 | 5.6708 | 0.78877 | 62.477 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.14351 | 0.99 | 0.020595 | 0.097105 | 123.38 |

Table S4. Algorithms models and their training functions fitted for the experimental run 4

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 27.781 | 0.67 | 771.8 | 22.21 | 4.8178 |
| 2 | Linear regression | Interactions linear | 27.878 | 0.67 | 777.18 | 22.261 | 7.4377 |
| 3 | Linear regression | Robust Linear | 34.061 | 0.50 | 1160.1 | 19.672 | 7.1827 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 27.814 | 0.67 | 773.64 | 22.226 | 8.0331 |
| 5 | Tree | Fine Tree | 0.66027 | 0.99 | 0.43595 | 0..39209 | 6.9139 |
| 6 | Tree | Medium Tree | 1.2826 | 0.99 | 1.645 | 0.67065 | 6.6744 |
| 7 | Tree | Coarse Tree | 3.9155 | 0.99 | 15.331 | 1.9036 | 7.7719 |
| 8 | SVM | Linear SVM | 32.766 | 0.54 | 1073.6 | 19.633 | 8.3373 |
| 9 | SVM | Quadratic SVM | 14.079 | 0.91 | 198.21 | 8.9187 | 8.8662 |
| 10 | SVM | Cubic SVM | 4.3986 | 0.99 | 19.348 | 3.2432 | 10.936 |
| 11 | SVM | Fine Gaussian SVM | 11.359 | 0.94 | 129.02 | 5.3948 | 9.8362 |
| 12 | SVM | Medium Gaussian SVM | 5.9736 | 0.98 | 35.684 | 3.1058 | 8.6073 |
| 13 | SVM | Coarse Gaussian SVM | 19.986 | 0.83 | 399.45 | 10.193 | 9.2706 |
| 14 | Ensemble | Boosted Trees | 13.23 | 0.92 | 175.03 | 13.037 | 12.266 |
| 15 | Ensemble | Bagged Trees | 8.3314 | 0.97 | 69.412 | 4.7482 | 13.767 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.11418 | 0.99 | 0.013038 | 0.07809 | 209.58 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.19434 | 0.99 | 0.037768 | 0.075552 | 349.54 |
| 18 | Gaussian Process Regression | Exponential GPR | 2.013 | 0.99 | 4.052 | 0.63274 | 203.29 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.11066 | 0.99 | 0.12246 | 0.075797 | 507.21 |

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 25.713 | 0.59 | 661.15 | 19.97 | 6.0469 |
| 2 | Linear regression | Interactions linear | 25.753 | 0.59 | 663.21 | 19.963 | 5.3005 |
| 3 | Linear regression | Robust Linear | 36.029 | 0.19 | 1298.1 | 177.644 | 9.6615 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 25.819 | 0.59 | 666.61 | 20.016 | 9.325 |
| 5 | Tree | Fine Tree | 0.53494 | 0.99 | 0.28616 | 0.29344 | 9.0115 |
| 6 | Tree | Medium Tree | 1.0473 | 0.99 | 1.0969 | 0.49271 | 8.72998 |
| 7 | Tree | Coarse Tree | 2.9843 | 0.99 | 8.9062 | 1.2966 | 8.494 |
| 8 | SVM | Linear SVM | 31.131 | 0.40 | 969.11 | 16.998 | 8.0144 |
| 9 | SVM | Quadratic SVM | 15.707 | 0.85 | 246.72 | 9.1192 | 7.406 |
| 10 | SVM | Cubic SVM | 6.2853 | 0.98 | 39.504 | 3.8657 | 10.884 |
| 11 | SVM | Fine Gaussian SVM | 10.149 | 0.94 | 103.01 | 3.9022 | 10.735 |
| 12 | SVM | Medium Gaussian SVM | 6.9883 | 0.97 | 48.836 | 3.113 | 10.565 |
| 13 | SVM | Coarse Gaussian SVM | 21.11 | 0.72 | 445.64 | 10.09 | 10.39 |
| 14 | Ensemble | Boosted Trees | 13.739 | 0.88 | 188.76 | 13.613 | 11.418 |
| 15 | Ensemble | Bagged Trees | 6.4706 | 0.97 | 41.868 | 3.2969 | 11.815 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.1406 | 0.99 | 0.019768 | 0.11035 | 545.17 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 00.17149 | 0.99 | 0.029408 | 0.067625 | 615.09 |
| 18 | Gaussian Process Regression | Exponential GPR | 1.9171 | 0.99 | 3.67511 | 0.54674 | 313.72 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.10319 | 0.99 | 0.010647 | 0.070112 | 113.44 |

Table S5. Algorithms models and their training functions fitted for the experimental run 5

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 15.266 | 0.81 | 233.06 | 12.688 | 1.1876 |
| 2 | Linear regression | Interactions linear | 15.277 | 0.81 | 233.4 | 12.654 | 0.95009 |
| 3 | Linear regression | Robust Linear | 15.53 | 0.81 | 241.19 | 12.219 | 0.82172 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 15.278 | 0.81 | 233.43 | 12.69 | 2.986 |
| 5 | Tree | Fine Tree | 0.54347 | 0.99 | 0.29536 | 0.36254 | 0..61165 |
| 6 | Tree | Medium Tree | 1.1196 | 0.99 | 1.2535 | 0.66896 | 2.8324 |
| 7 | Tree | Coarse Tree | 3.0142 | 0.99 | 9.0855 | 1.8007 | 2.7174 |
| 8 | SVM | Linear SVM | 16.962 | 00.77 | 287.71 | 11.817 | 2.6191 |
| 9 | SVM | Quadratic SVM | 4.8753 | 0.98 | 23.769 | 3.7454 | 2.5074 |
| 10 | SVM | Cubic SVM | 2.2937 | 0.99 | 5.2611 | 2.0552 | 2.3825 |
| 11 | SVM | Fine Gaussian SVM | 8.5056 | 0.94 | 72.346 | 5.0542 | 2.2667 |
| 12 | SVM | Medium Gaussian SVM | 2.7675 | 0.99 | 7.6591 | 1.9751 | 2.1536 |
| 13 | SVM | Coarse Gaussian SVM | 8.0278 | 0.95 | 64.445 | 4.8415 | 2.0439 |
| 14 | Ensemble | Boosted Trees | 15.969 | 0.79 | 25 | 155.886 | 4.0774 |
| 15 | Ensemble | Bagged Trees | 6.6427 | 0.96 | 44.125 | 4.292 | 3.8628 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.062457 | 0.99 | 0.0039009 | 0.04504 | 52.072 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.099443 | 0.99 | 0.0098889 | 0.044781 | 69.53 |
| 18 | Gaussian Process Regression | Exponential GPR | 1.0945 | 0.99 | 1.1979 | 0.39418 | 48.874 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.062188 | 0.99 | 0.0038674 | 0.044647 | 97.315 |

Table S6. Algorithms models and their training functions ions fitted for the experimental run 6

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 36.739 | 0.65 | 1349.8 | 29.128 | 1.8351 |
| 2 | Linear regression | Interactions linear | 36.633 | 0.65 | 1342 | 28.995 | 1.5596 |
| 3 | Linear regression | Robust Linear | 47.295 | 0.42 | 2236.8 | 25.862 | 1.3992 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 36.732 | 0.65 | 1349.2 | 299.132 | 3.0758 |
| 5 | Tree | Fine Tree | 0.94998 | 0.99 | 0.90245 | 0.52139 | 1.0653 |
| 6 | Tree | Medium Tree | 1.9171 | 0.99 | 3.6753 | 0.91812 | 0.89322 |
| 7 | Tree | Coarse Tree | 5.0678 | 0.99 | 25.683 | 2.4312 | 2..897 |
| 8 | SVM | Linear SVM | 43.596 | 0.50 | 1900.6 | 25.573 | 2.7984 |
| 9 | SVM | Quadratic SVM | 19.843 | 0.90 | 393.73 | 12.194 | 2.7012 |
| 10 | SVM | Cubic SVM | 6.6846 | 0.99 | 44.684 | 4.6318 | 3.3783 |
| 11 | SVM | Fine Gaussian SVM | 15.979 | 0.93 | 255.33 | 7.1442 | 2.5064 |
| 12 | SVM | Medium Gaussian SVM | 8.6115 | 0.98 | 74.158 | 4.3876 | 2.36 |
| 13 | SVM | Coarse Gaussian SVM | 27.982 | 0.880 | 783.01 | 13.956 | 2.8723 |
| 14 | Ensemble | Boosted Trees | 11.121 | 0.97 | 123.67 | 10.745 | 3.0947 |
| 15 | Ensemble | Bagged Trees | 10.075 | 0.97 | 101.51 | 5.663 | 3.0853 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.15389 | 0.99 | 0.023682 | 0.11191 | 159.26 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.2544 | 0.99 | 0.064719 | 0.10792 | 266.67 |
| 18 | Gaussian Process Regression | Exponential GPR | 2.749 | 0.99 | 7.5571 | 0.90354 | 145.66 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.14963 | 0.99 | 0.02239 | 0.10718 | 400.54 |

Table S7. Algorithms models and their training functions fitted for the experimental run 7

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 27.758 | 0.67 | 770.49 | 22.207 | 4.3776 |
| 2 | Linear regression | Interactions linear | 27.768 | 0.67 | 771.08 | 22.206 | 8.6775 |
| 3 | Linear regression | Robust Linear | 33.922 | 0.51 | 1150.7 | 19.656 | 8.3485 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 27.814 | 0.67 | 773.6 | 22.226 | 8.0916 |
| 5 | Tree | Fine Tree | 0.65681 | 0.99 | 0.4314 | 0.39461 | 7.8005 |
| 6 | Tree | Medium Tree | 1.2283 | 0.99 | 1.5088 | 0.65118 | 7.3483 |
| 7 | Tree | Coarse Tree | 3.9777 | 0.99 | 15.822 | 1.9508 | 6.8737 |
| 8 | SVM | Linear SVM | 32.941 | 0.53 | 1085.1 | 19.615 | 11.456 |
| 9 | SVM | Quadratic SVM | 14.158 | 0.91 | 200.44 | 8.9564 | 11.137 |
| 10 | SVM | Cubic SVM | 4.3763 | 0.99 | 19.152 | 3.2418 | 10.799 |
| 11 | SVM | Fine Gaussian SVM | 11.314 | 0.95 | 128 | 5.3063 | 10.478 |
| 12 | SVM | Medium Gaussian SVM | 6.1635 | 0..98 | 37.988 | 3.1359 | 9.8724 |
| 13 | SVM | Coarse Gaussian SVM | 20.03 | 0.83 | 401.18 | 10.223 | 9.4104 |
| 14 | Ensemble | Boosted Trees | 13.207 | 0.93 | 174.43 | 13.019 | 12.467 |
| 15 | Ensemble | Bagged Trees | 8.2759 | 0.97 | 68.491 | 4.6454 | 11.834 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.11037 | 0.99 | 0.012181 | 0.077144 | 168.74 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.18257 | 0.99 | 0.03333 | 0.071992 | 280.2 |
| 18 | Gaussian Process Regression | Exponential GPR | 1.9958 | 0.99 | 3.9832 | 0.65374 | 155.7 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.10843 | 0.99 | 0.011757 | 0.074881 | 399.61 |

Table S8. Algorithms models and their training functions fitted for the experimental run 8

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 32.667 | 0.81 | 1067.1 | 27.128 | 4.7646 |
| 2 | Linear regression | Interactions linear | 32.708 | 0..81 | 1069.88 | 27.13 | 4.5421 |
| 3 | Linear regression | Robust Linear | 33.311 | 0.80 | 1109.7 | 26.143 | 4.3286 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 32.661 | 0.81 | 1066.8 | 27.117 | 6.7763 |
| 5 | Tree | Fine Tree | 1.1321 | 0..99 | 1.2817 | 0.75576 | 6.5779 |
| 6 | Tree | Medium Tree | 2.3012 | 0.99 | 5.2956 | 1.4001 | 6.3933 |
| 7 | Tree | Coarse Tree | 6.7389 | 0.99 | 45.412 | 4.0861 | 6.1694 |
| 8 | SVM | Linear SVM | 36.259 | 0.77 | 1314.7 | 25.292 | 77.8145 |
| 9 | SVM | Quadratic SVM | 10.523 | 0.98 | 110.73 | 8.006 | 7.6279 |
| 10 | SVM | Cubic SVM | 4.7712 | 0.99 | 22.764 | 4.2537 | 7.4558 |
| 11 | SVM | Fine Gaussian SVM | 16.095 | 0.95 | 259.04 | 9.9045 | 8.2249 |
| 12 | SVM | Medium Gaussian SVM | 5.9298 | 0.99 | 35.163 | 4.2364 | 7.1841 |
| 13 | SVM | Coarse Gaussian SVM | 17.177 | 0.95 | 295.05 | 10.399 | 6.9416 |
| 14 | Ensemble | Boosted Trees | 11.495 | 0.98 | 132.13 | 10.952 | 9.7087 |
| 15 | Ensemble | Bagged Trees | 15.197 | 0.96 | 230.95 | 10.06 | 10.186 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.14689 | 0.99 | 0.021576 | 0.10004 | 57.39 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.22347 | 0.99 | 0.0499937 | 0.096519 | 66.298 |
| 18 | Gaussian Process Regression | Exponential GPR | 2.4836 | 0.99 | 6.1681 | 0.85892 | 62.774 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.14578 | 0.99 | 0.021251 | 0.099163 | 132.73 |

Table S9. Algorithms models and their training functions fitted for the experimental run 9

Table S10. Algorithms models and their training functions fitted for the experimental run 10

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 44.796 | 0.48 | 2006.6 | 33.015 | 4.6327 |
| 2 | Linear regression | Interactions linear | 44.908 | 0.48 | 2016.7 | 33.063 | 4.4272 |
| 3 | Linear regression | Robust Linear | 65.591 | 0.11 | 4302.2 | 28.354 | 4.2213 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 44.813 | 0.48 | 2008.2 | 33.026 | 6.5623 |
| 5 | Tree | Fine Tree | 0.91438 | 0.99 | 0.8361 | 0.42329 | 6.3459 |
| 6 | Tree | Medium Tree | 2.1937 | 0.99 | 4.8125 | 0.83907 | 6.1669 |
| 7 | Tree | Coarse Tree | 5.2123 | 0.99 | 27.168 | 2.0812 | 5.9854 |
| 8 | SVM | Linear SVM | 55.789 | 0.20 | 3112.4 | 26.17 | 6.8465 |
| 9 | SVM | Quadratic SVM | 34.474 | 0.69 | 1188.5 | 17.14 | 7.1263 |
| 10 | SVM | Cubic SVM | 18.124 | 0.92 | 328.48 | 9.0185 | 8.0766 |
| 11 | SVM | Fine Gaussian SVM | 25.573 | 0.83 | 654 | 8.0496 | 8.572 |
| 12 | SVM | Medium Gaussian SVM | 21.217 | 0.88 | 450.16 | 7.9039 | 7.88 |
| 13 | SVM | Coarse Gaussian SVM | 44.342 | 0.49 | 1966.2 | 18.84 | 8.3659 |
| 14 | Ensemble | Boosted Trees | 8.9627 | 0.98 | 80.33 | 8.4859 | 10.992 |
| 15 | Ensemble | Bagged Trees | 10.478 | 0.97 | 109.79 | 5.0743 | 10.811 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.26835 | 0.99 | 0.072011 | 0.18279 | 586.1 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.5149 | 0.99 | 0.26512 | 0.18982 | 488.06 |
| 18 | Gaussian Process Regression | Exponential GPR | 4.502 | 0.99 | 20.268 | 1.3263 | 268.85 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.16317 | 0.99 | 0.063572 | 0.27709 | 474.03 |

Table S11. Algorithms models and their training functions fitted for the experimental run 11

|  | Algorithms models | Training Function | RMSE | R2 | MSE | MAE | Training Time, sec |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Linear regression | Linear | 51.235 | 0.44 | 2625 | 36.86 | 3.7994 |
| 2 | Linear regression | Interactions linear | 51.311 | 0.44 | 2632.8 | 36.819 | 3.5066 |
| 3 | Linear regression | Robust Linear | 73.471 | 0.15 | 5398 | 30.335 | 5.5203 |
| 4 | Stepwise Linear Regression | Stepwise Linear | 51.24 | 0.44 | 2625.6 | 36.841 | 5.3291 |
| 5 | Tree | Fine Tree | 1.2376 | 0.99 | 1.5316 | 0.52774 | 5.1203 |
| 6 | Tree | Medium Tree | 2.5712 | 0.99 | 6.6113 | 0.96842 | 4.9658 |
| 7 | Tree | Coarse Tree | 6.0438 | 0.99 | 36.528 | 2.368 | 4.803 |
| 8 | SVM | Linear SVM | 64.328 | 0.12 | 4138.1 | 28.14 | 5.6889 |
| 9 | SVM | Quadratic SVM | 42.652 | 0.61 | 1819.2 | 19.829 | 5.4898 |
| 10 | SVM | Cubic SVM | 24.698 | 0.87 | 610 | 11.473 | 4.0662 |
| 11 | SVM | Fine Gaussian SVM | 35.43 | 0.73 | 1255.3 | 14.495 | 4.915 |
| 12 | SVM | Medium Gaussian SVM | 30.177 | 0.81 | 910.66 | 10.508 | 3.8976 |
| 13 | SVM | Coarse Gaussian SVM | 53.824 | 0.38 | 2897 | 21.698 | 4.6595 |
| 14 | Ensemble | Boosted Trees | 7.2421 | 0.99 | 52.448 | 6.5008 | 7.3543 |
| 15 | Ensemble | Bagged Trees | 12.016 | 0.97 | 144.39 | 5.3114 | 7.6324 |
| 16 | Gaussian Process Regression | Squared Exponential GPR | 0.26505 | 0.99 | 0.070251 | 0.16968 | 697.1 |
| 17 | Gaussian Process Regression | Matern 5/2 GPR | 0.65118 | 0.99 | 0.42404 | 0.28285 | 557.8 |
| 18 | Gaussian Process Regression | Exponential GPR | 5.3675 | 0.99 | 28.81 | 1.6417 | 300.29 |
| 19 | Gaussian Regression Process | Rational Quadratic GPR | 0.23217 | 0.99 | 0.31526 | 1.15277 | 271.19 |