Supplementary Material

Chemically degradable vitrimeric materials based on divanillin imine epoxy monomer and aliphatic diamines. Effect of transamination in the stress relaxation process

Tommaso Telatin 1, Silvia De la Flor 2, Xavier Montané 1,* and Àngels Serra 1,*

1 Departament of Analytical and Organic Chemistry, Universitat Rovira i Virgili, C/ Marcel·lí Domingo 1, 43007 Tarragona, Spain

2 Department of Mechanical Engineering, Universitat Rovira i Virgili, Av. Països Catalans 26, 43007 Tarragona, Spain

* Corresponding authors.

E-mail address: xavier.montane@urv.cat; Tel.: +34-977559768 (X. Montané)

E-mail address: angels.serra@urv.cat; Tel.: +34-977559768 (À. Serra)

Table of Contents:

- Structural characterization of the monomer							S3

- Study of the curing process by 1H NMR spectroscopy						S5

- Thermogravimetric analysis of the prepared materials						S6

- Storage moduli as a function of the angular frequency for the prepared materials		S7

- Stress relaxation profiles and Kohlrausch-Williams-Watts (KKW) model analysis		S8

- Frequency sweeps experiments for DIDE-PPO/MXDA						S9

- Frequency sweeps experiments for DIDE-PPO/IPDA						S10

- Carbon fibers reinforced composites								S11

- Structural characterization of the monomer

Figure S1. 1H NMR spectrum of EVan in CDCl3.

Figure S2. 13C NMR spectrum of EVan in CDCl3.

Figure S3. 1H NMR spectrum of DIDE-PPO in CDCl3.

Figure S4. 13C NMR spectrum of DIDE-PPO in CDCl3.

- Study of the curing process by 1H NMR spectroscopy

Figure S5. 1H NMR spectra in CDCl3 of the curing mixture at 40, 60 and 100 °C collected after 10 minutes of equilibration at each temperature.

Table S1. Integrals of the main peaks of the curing mixture at different temperatures.

| Temperature (°C) | I8.27 ppma | I8.18 ppmb | I4.77 ppmc | I8.18 ppm/I8.27 ppmd |
| --- | --- | --- | --- | --- |
| 40 | 1.00 | 0.82 | 1.95 | 0.82 |
| 60 | 1.00 | 0.86 | 1.95 | 0.86 |
| 100 | 1.00 | 0.89 | 2.10 | 0.89 |

a Normalized integral of the original imine proton signal.

b Normalized integral of the MXDA-derived imine proton signal.

c Normalized integral of the methylene protons signal relative to the reacted MXDA hardener.

d Ratio between the integrals of the two imine signals.

- Thermogravimetric analysis of the prepared materials

Figure S6. a) Thermogravimetric curves in N2 atmosphere and b) their derivatives for the materials prepared.

- Storage Moduli as a function of the angular frequency for the prepared materials

Figure S7. Storage modulus of DIDE-PPO/MXDA and DIDE-PPO/IPDA as a function of angular frequency at different temperatures.

- Stress relaxation profiles and Kohlrausch-Williams-Watts (KKW) model analysis

Figure S8. Tension mode stress relaxation profiles of the prepared materials (colored lines) fit by a stretched exponential decay function (dashed black lines).

Table S2. Fitting parameters for the stretched exponential decay function for the prepared materials.

| Sample | T (°C) | βa | τb (s) | R2 |
| --- | --- | --- | --- | --- |
|  | 130 | 0.46 | 29.64 | 0.976 |
|  | 140 | 0.41 | 17.39 | 0.962 |
| DIDE-PPO/IPDA | 150 | 0.41 | 11.27 | 0.958 |
|  | 160 | 0.46 | 7.36 | 0.976 |
|  | 170 | 0.57 | 5.22 | 0.955 |
|  | 130 | 0.49 | 22.95 | 0.981 |
|  | 140 | 0.68 | 12.49 | 0.991 |
| DIDE-PPO/MXDA | 150 | 0.60 | 9.38 | 0.980 |
|  | 160 | 0.71 | 5.55 | 0.976 |
|  | 170 | 1.00 | 3.42 | 0.983 |

a Stretched exponential parameter.

b Characteristic relaxation time.

- Frequency sweeps experiments for DIDE-PPO/MXDA

Figure S9. Storage and Loss Moduli of DIDE-PPO/MXDA as a function of the angular frequency.

- Frequency sweeps experiments for DIDE-PPO/IPDA

Figure S10. Storage and Loss Moduli of DIDE-PPO/IPDA as a function of the angular frequency.

- Carbon fibers reinforced composites

Figure S11. Evolution of storage modulus and tan δ with temperature for the prepared composite materials.

Table S3. Main thermomechanical properties of the prepared composite materials.

| Sample | E’Glassy a (MPa) | E’Rubberyb (MPa) | Ttan δc |
| --- | --- | --- | --- |
| DIDE-PPO/IPDA-CF | 34422 | 708 | 76 |
| DIDE-PPO/MXDA-CF | 31146 | 2427 | 64 |

Table S4. Creep rate and strain recovery for the prepared carbon fiber reinforced composites.

| Sample | dε/dta | % Residual deformationb |
| --- | --- | --- |
| DIDE-PPO/IPDA | 2.39 x 10-3 | 0.61 |
| DIDE-PPO/MXDA | 2.13 x 10-3 | 0.37 |
| DIDE-PPO/IPDA-CF | 4.24 x 10-4 | 0.13 |
| DIDE-PPO/MXDA-CF | 4.12 x 10-4 | 0.02 |

a Determined from the slope of the steady-state region of the creep curve.

b Determined after 30 min of releasing the stress.