Supplementary Materials

Bimetallic mesoporous MCM-41 nanoparticles with Ta/(Ti, V, Co, Nb) with catalytic and photocatalytic properties

Viorica Parvulescu, Gabriela Petcu, Nicoleta G. Apostol, Irina Atkinson, Simona Petrescu, Adriana Baran, Daniela C. Culita, Ramona Ene, Bogdan Trica and Elena M. Anghel

Figure S1. The high angles XRD diffractograms of TaMe/MCM-41 samples.

| a | b |
| --- | --- |
| c | d |
| e |  |

Figure S2. TEM images of Ta-MCM-41 (a); TaV-MCM-41 (b);

TaTi-MCM-41 (c); TaNb-MCM-41 (d) and TaCo-MCM-41 (e) samples.

Figure S3. Raman spectra of the monometallic (Ta, V, Ti, Nb, Co)-MCM-41 samples

Figure S4. Comparative Raman spectra of monometallic (Ta, V, Ti, Nb, Co)-MCM-41 and bimetallic Ta(V, Ti, Nb, Co) samples

Figure S5. XPS full scan survey spectra for the bimetallic Ta/Me samples.

Figure S6. XPS spectra for Nb3d of the sample TaNb-MCM-41 sample.

Figure S7. XPS spectra for O1s of the bimetallic Ta/Me-MCM-41 samples.

Figure S8. XPS valence band spectra of the bimetallic Ta/Me-MCM-41 samples.

Figure S9. Photodegradation of methyl orange in aqueous solution.

Table S1. Peak position and assignments for the monometallic (Ta/Nb/Ti/Co/V)-MCM41 catalysts.

| Peak position (cm-1) |  |  |  |  | Assignments | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Ta | Nb | Ti | Co | V | <650 cm-1 n-SiO4 rings | 34,35 |
|  |  |  |  | 356 |  (O-V-O) in polymeric VOx | 36, 37 |
| 360 | 368 |  |  |  | 5,6,7-SiO4 rings | 34 |
| 441 | 443 | 440 | 436 |  | 5,6,7-SiO4 rings | 34 |
| 497 | 490 | 495 | 497 | 481 | D1 modes (4- SiO4 rings) | 34 |
|  |  |  |  | 552 | Silicalite framework breathing modes | 36 |
| 608 | 610 | 607 | 608 |  | D2 modes (3- SiO4 rings) | 34 |
| 660 |  |  |  |  | TaO6 | 38 |
|  |  |  | 664 |  | CoO6 in Co3O4 | 39 |
|  | 822 | 800 | 798 | 821 | s (Si-O-Si) and surface polymerized niobia | 34, 38 |
| 828 |  |  | 838 |  | s of the [SiO4] units | 34 |
|  | 935 |  |  |  | surface polymerized niobia species (820-935 cm-1) | 38 |
| 958 |  | 954 |  | 958 | s (Si-O-Si/Ti/V) | 40,41 |
| 980 | 975 |  | 976 |  |  (Si-OH) and TaOx species (965-980 cm-1) | 34,38,42 |
|  |  |  |  | 1028 | Pyramidal structure of (SiO)3V=O when vanadium content is less than 2wt.% (1033-1036 cm-1) | 36 |
| 1050 | 1091 |  | 1052 |  | Antisymmetric stretching  (Si-O) | 34 |
|  |  | 1100 |  |  | as (Si-O-Ti) with Ti4+ | 40 |
| 1185 | 1150 |  |  | 1123 |  |  |
|  |  |  |  |  | >3000 cm-1 | 42 |
|  | 3233 |  |  |  | ν(OH) moodes of H2O involved in a tetrahedral structure | 42 |
| 3600 | 3594 | 3595 | 3623 |  | MeO-H and free H2O | 41,42 |
| 3700 | 3690 |  | 3695 |  | HO-H dangling | 42 |
| 3747 | 3746 | 3743 | 3745 | 3740 | SiO-H and Free SiO-H | 42 |