Supplementary Materials

Contents

1. Spectra of compounds

2. Thermal properties

3. Density Functional Theory (DFT) Calculations

4. Cyclic voltammetry studies

1. Spectra of compounds

Figure S1.  1H NMR spectra of 6-(N,N-diphenylaniline)-2-(4,4,5,5-tetramethyl-1,3,2-dioxaborolanyl)-azulene  4.

1H NMR: δ 8.25 (d, J = 9.40 Hz, 2H), 7.84 (d, J = 8.3 Hz, 4H), 7.62 (s, 2H), 7.29 – 6.94 (m, 12H), 1.40 (s, 12H).

In this spectrum, the proton signals at С-1 and  С-3  (singlet at 7.62 δ) are consistent with the signals of the same protons of the initial molecule 2 [1], which confirms the structure of molecule 4. In the case of substitution of the azulene position 2 with a diphenylaniline group, a significant shift of proton signals during C-1 and C-3 in a strong field would occur by an average of 1.0 δ due to an increase in electron density in the five-membered ring [2].

Figure S2. 13C NMR spectra of  6-(N,N-diphenylaniline)-2-(4,4,5,5-tetramethyl-1,3,2-dioxaborolanyl)-azulene  4.

13C NMR: δ 149.66, 148.13, 147.54, 141.53, 135.77, 135.26, 130.26, 129.44, 129.35, 128.50, 124.88, 124.40, 123.85, 123.43, 123.35, 113.94, 60.20, 29.84.

Figure S3.  1H NMR spectra of  6,6-Bis(N,N-diphenylaniline)- 2,2-(4-(diphenylamino)phenyl)-bis-azulene  6.

1H NMR: δ 8.24 (d, J = 9.4 Hz, 10H), 7.88 (d, J = 12.3 Hz, 4H), 7.62 (s, 4H), 7.47 (t, J = 9.9 Hz, 5H ),7.37 – 7.04 (m, 30H).

Figure S4.   13C NMR spectra of  6,6-Bis(N,N-diphenylaniline)- 2,2-(4-(diphenylamino)phenyl)-bis-azulene  6.

13C NMR: δ 147.84, 147.63, 147.44, 141.64, 135.88, 135.37, 132.44, 129.78, 129.21, 128.41, 125.33, 124.78, 124.47, 124.36, 123.76, 123.72, 123.34, 123.46, 123.22, 122.61, 113.84

Figure S5.  1H NMR spectra of  6,6,6-tris(N,N-diphenylaniline)- 2,2,2-(4-(triphenylamino)-tris-azulene 8.

1H NMR: δ 8.24 (d, J = 9.4 Hz, 12H), 7.88 (d, J = 12.3 Hz, 6H), 7.62 (s, 6H), 7.47 (t, J = 9.9 Hz, 6H ),7.37 – 7.04 (m, 42H).

Figure S6. 13C NMR spectra of  6,6,6-tris(N,N-diphenylaniline)- 2,2,2-(4-(triphenylamino)-tris-azulene 8.

13C NMR: δ 149.57, 148.23, 147.84, 147.43, 147.66, 147.21, 141.44, 135.68, 137.37, 132.14, 130.36, 129.58, 129.55, 129.21, 128.41, 125.75, 125.46, 125.32, 124.77, 124.46, 123.36, 13.52, 123.14, 123.66, 123.13, 122.36, 114.55, 113.25.

2. Thermal properties

Figure S7. Thermogravimetric measurements of   co-oligomers 6 and 8

(a)                                                                                                        (b)

Figure S8. Differential scanning calorimetry measurements of  co-oligomers 6 (a) and 8 (b)

3. Density Functional Theory (DFT) Calculations

To characterize the geometry and orbitals of HOMO-LUMO of co-oligomers 6 and 8, DFT calculations based on the level of B3LYP/6-31G * (d, p) Gaussian 16 were used. The geometry of the molecules was optimized in a singlet state using the keywords Opt and Freq, and the results were recorded in a .chk file to visualize the boundary orbitals.

After the correct completion of the calculations, the .chk file was opened in GaussView 6.0 and the HOMO-LUMO orbitals were visualized from it using the built-in GaussView tool. Then we obtained the energies of the boundary orbitals in Hartree units and recalculated them into eV, multiplying by the recalculation coefficient 27.2114.

Table S1. Atomic coordinates of optimized geometry of 6

---------------------------------------------------------------------

Center     Atomic      Atomic             Coordinates (Angstroms)

Number     Number       Type             X           Y           Z

---------------------------------------------------------------------

1          7           0        0.000016    5.209712   -0.000009

2          6           0        0.000032    6.641096    0.000008

3          6           0       -0.882430    7.353068    0.833264

4          6           0       -0.884358    8.750167    0.824065

5          6           0        0.000046    9.457247    0.000018

6          6           0        0.884443    8.750164   -0.824035

7          6           0        0.882501    7.353067   -0.833245

8          6           0       -1.236834    4.500898   -0.003050

9          6           0       -2.324929    4.956612   -0.772650

10          6           0       -3.534011    4.267328   -0.765797

11          6           0       -3.711757    3.090761   -0.005472

12          6           0       -2.610105    2.643332    0.756374

13          6           0       -1.400737    3.332112    0.765894

14          6           0        1.236836    4.500851    0.003087

15          6           0        2.324975    4.956620    0.772590

16          6           0        3.534029    4.267285    0.765791

17          6           0        3.711710    3.090617    0.005611

18          6           0        2.610005    2.643124   -0.756128

19          6           0        1.400663    3.331943   -0.765694

20          6           0       -9.616429    1.091014   -0.447769

21          6           0       -9.586557   -0.252657   -0.009380

22          6           0       -8.447079   -0.965039    0.429476

23          6           0       -7.118814   -0.553799    0.553948

24          6           0       -6.534148    0.682198    0.265004

25          6           0       -7.223288    1.893795   -0.280723

26          6           0       -8.584204    2.022735   -0.570988

27          6           0       -5.179407    1.022003    0.415473

28          6           0       -4.984971    2.365768   -0.006488

29          6           0       -6.239153    2.885059   -0.429519

30          6           0        8.446998   -0.965231   -0.429291

31          6           0        9.586482   -0.252830    0.009510

32          6           0        9.616369    1.090840    0.447894

33          6           0        8.584149    2.022569    0.571104

34          6           0        7.223229    1.893625    0.280862

35          6           0        6.534065    0.681997   -0.264777

36          6           0        7.118723   -0.554005   -0.553713

37          6           0        6.239108    2.884907    0.429608

38          6           0        4.984906    2.365597    0.006654

39          6           0        5.179323    1.021803   -0.415227

40          7           0      -14.599922   -3.099852   -0.009067

41          6           0      -15.309485   -3.309380    1.216062

42          6           0      -15.896771   -4.557781    1.492447

43          6           0      -16.600060   -4.755825    2.683379

44          6           0      -16.715379   -3.722791    3.621671

45          6           0      -16.125483   -2.481760    3.351606

46          6           0      -15.434747   -2.269421    2.155833

47          6           0      -15.144877   -3.600890   -1.233953

48          6           0      -16.517444   -3.461701   -1.510446

49          6           0      -17.049280   -3.963205   -2.701159

50          6           0      -16.222977   -4.594344   -3.639108

51          6           0      -14.855355   -4.727438   -3.368959

52          6           0      -14.317742   -4.244037   -2.173385

53          6           0      -13.361652   -2.397393   -0.009534

54          6           0      -12.439638   -2.559301    1.042909

55          6           0      -11.230979   -1.866232    1.039872

56          6           0      -10.884119   -0.990540   -0.009754

57          6           0      -11.813796   -0.840234   -1.059493

58          6           0      -13.028250   -1.523086   -1.062336

59          7           0       14.599961   -3.099849    0.008948

60          6           0       15.144902   -3.601030    1.233776

61          6           0       16.517461   -3.461854    1.510324

62          6           0       17.049273   -3.963489    2.700991

63          6           0       16.222958   -4.594749    3.638848

64          6           0       14.855345   -4.727830    3.368647

65          6           0       14.317755   -4.244299    2.173117

66          6           0       13.361644   -2.397454    0.009492

67          6           0       13.028230   -1.523228    1.062354

68          6           0       11.813749   -0.840421    1.059569

69          6           0       10.884063   -0.990705    0.009840

70          6           0       11.230922   -1.866339   -1.039836

71          6           0       12.439612   -2.559359   -1.042933

72          6           0       15.309568   -3.309121   -1.216195

73          6           0       15.897001   -4.557416   -1.492755

74          6           0       16.600325   -4.755208   -2.683707

75          6           0       16.715538   -3.722027   -3.621851

76          6           0       16.125499   -2.481102   -3.351612

77          6           0       15.434725   -2.269015   -2.155815

78          1           0       -1.558877    6.808453    1.482219

79          1           0       -1.570103    9.286373    1.472656

80          1           0        0.000051   10.542240    0.000022

81          1           0        1.570191    9.286369   -1.472623

82          1           0        1.558941    6.808449   -1.482205

83          1           0       -2.212149    5.846561   -1.381175

84          1           0       -4.346430    4.628558   -1.387138

85          1           0       -2.714678    1.760277    1.377551

86          1           0       -0.579043    2.975530    1.376371

87          1           0        2.212252    5.846642    1.381017

88          1           0        4.346472    4.628558    1.387074

89          1           0        2.714513    1.759961   -1.377162

90          1           0        0.578928    2.975296   -1.376078

91          1           0      -10.601521    1.466217   -0.709975

92          1           0       -8.628065   -2.003656    0.691161

93          1           0       -6.432634   -1.314822    0.924418

94          1           0       -8.887486    3.001577   -0.941323

95          1           0       -4.408916    0.347499    0.763367

96          1           0       -6.425284    3.892189   -0.776931

97          1           0        8.627984   -2.003848   -0.690969

98          1           0       10.601466    1.466040    0.710082

99          1           0        8.887439    3.001418    0.941412

100          1           0        6.432530   -1.315043   -0.924128

101          1           0        6.425253    3.892053    0.776963

102          1           0        4.408816    0.347273   -0.763037

103          1           0      -15.798369   -5.363743    0.774066

104          1           0      -17.047611   -5.724448    2.883113

105          1           0      -17.256704   -3.882066    4.548339

106          1           0      -16.214048   -1.670156    4.067059

107          1           0      -14.992295   -1.302619    1.943810

108          1           0      -17.157673   -2.961999   -0.792294

109          1           0      -18.110075   -3.848300   -2.901001

110          1           0      -16.638176   -4.976865   -4.565610

111          1           0      -14.205176   -5.221554   -4.084174

112          1           0      -13.261144   -4.362409   -1.961184

113          1           0      -12.677840   -3.224544    1.864645

114          1           0      -10.551349   -1.993494    1.876054

115          1           0      -11.574988   -0.191425   -1.895739

116          1           0      -13.721661   -1.386854   -1.884016

117          1           0       17.157703   -2.962055    0.792251

118          1           0       18.110062   -3.848591    2.900872

119          1           0       16.638140   -4.977373    4.565314

120          1           0       14.205154   -5.222036    4.083790

121          1           0       13.261165   -4.362667    1.960874

122          1           0       13.721643   -1.387028    1.884036

123          1           0       11.574926   -0.191675    1.895861

124          1           0       10.551267   -1.993603   -1.875996

125          1           0       12.677820   -3.224565   -1.864695

126          1           0       15.798687   -5.363493   -0.774491

127          1           0       17.047988   -5.723753   -2.883573

128          1           0       17.256888   -3.881108   -4.548537

129          1           0       16.213981   -1.669382   -4.066944

130          1           0       14.992166   -1.302291   -1.943659

------------------------------------------------------------------------------

Method: DFT B3LYP 6-31G*

Key word: opt freq

Etotal (RB3LYP)= -3015.311973 Hartree

Table S2. Atomic coordinates of optimized geometry of 8

---------------------------------------------------------------------

Center     Atomic      Atomic             Coordinates (Angstroms)

Number     Number       Type             X           Y           Z

---------------------------------------------------------------------

1          7           0        0.002269    0.000027   -0.001192

2          6           0        0.717952   -1.234013    0.008182

3          6           0        1.877505   -1.387611    0.792488

4          6           0        2.575416   -2.591804    0.793479

5          6           0        2.146002   -3.697250    0.026744

6          6           0        0.978294   -3.529356   -0.749486

7          6           0        0.280115   -2.325456   -0.766622

8          6           0        0.712706    1.237070   -0.010418

9          6           0        1.872075    1.395382   -0.794068

10          6           0        2.564936    2.602485   -0.794881

11          6           0        2.130404    3.706282   -0.028663

12          6           0        0.962928    3.533670    0.746880

13          6           0        0.269826    2.326838    0.763891

14          6           0       -1.424747   -0.003054   -0.001176

15          6           0       -2.142285   -0.917695    0.793381

16          6           0       -3.534202   -0.920821    0.785120

17          6           0       -4.272405   -0.009162   -0.001006

18          6           0       -3.538214    0.905632   -0.787246

19          6           0       -2.146296    0.908474   -0.795684

20          6           0        6.194875    8.427721   -0.528145

21          6           0        5.496742    9.568383   -0.068989

22          6           0        4.162313    9.601228    0.397375

23          6           0        3.224071    8.574989    0.520222

24          6           0        3.342205    7.214319    0.224033

25          6           0        4.547706    6.518290   -0.325874

26          6           0        5.780656    7.099007   -0.635290

27          6           0        2.348755    6.234277    0.385313

28          6           0        2.859990    4.976894   -0.037807

29          6           0        4.201076    5.164684   -0.471043

30          6           0      -10.395986    0.657777   -1.062833

31          6           0      -11.032742   -0.023227   -0.000094

32          6           0      -10.392856   -0.701653    1.062434

33          6           0       -9.034577   -0.870474    1.336768

34          6           0       -7.916357   -0.420349    0.629594

35          6           0       -7.918207    0.386727   -0.630747

36          6           0       -9.038489    0.832184   -1.337604

37          6           0       -6.570409   -0.639433    0.966518

38          6           0       -5.738205   -0.012261   -0.000863

39          6           0       -6.573260    0.611392   -0.968044

40          7           0        8.367151   14.566519   -0.099922

41          6           0        7.709878   15.778139    0.285492

42          6           0        7.904485   16.958322   -0.455421

43          6           0        7.272282   18.143057   -0.069579

44          6           0        6.426976   18.167302    1.046543

45          6           0        6.226626   16.992037    1.781200

46          6           0        6.867735   15.806638    1.412549

47          6           0        9.742939   14.605905   -0.492714

48          6           0       10.668153   15.374639    0.237126

49          6           0       12.008062   15.422113   -0.155998

50          6           0       12.449116   14.694849   -1.268390

51          6           0       11.531079   13.923636   -1.991960

52          6           0       10.186020   13.883395   -1.616062

53          6           0        7.658687   13.332778   -0.092488

54          6           0        6.303465   13.276149   -0.472932

55          6           0        5.611679   12.067327   -0.454586

56          6           0        6.239622   10.861741   -0.077298

57          6           0        7.599388   10.930406    0.292034

58          6           0        8.294870   12.137246    0.295537

59          7           0      -16.798058   -0.034846    0.000930

60          6           0      -17.520768    0.832365    0.880727

61          6           0      -18.645217    0.357541    1.580666

62          6           0      -19.356950    1.209615    2.428922

63          6           0      -18.952121    2.538450    2.605443

64          6           0      -17.829007    3.010921    1.915181

65          6           0      -17.121164    2.170782    1.051909

66          6           0      -15.374493   -0.031967    0.000686

67          6           0      -14.652850    0.126335    1.199927

68          6           0      -13.259626    0.132074    1.193794

69          6           0      -12.525374   -0.026234    0.000177

70          6           0      -13.259413   -0.187487   -1.193173

71          6           0      -14.652650   -0.187356   -1.198812

72          6           0      -17.517504   -0.904998   -0.878653

73          6           0      -18.643933   -0.434697   -1.578456

74          6           0      -19.352403   -1.289662   -2.426538

75          6           0      -18.942326   -2.616896   -2.603001

76          6           0      -17.817255   -3.084855   -1.912854

77          6           0      -17.112630   -2.241837   -1.049755

78          6           0        6.229368   -8.402061    0.529137

79          6           0        5.536730   -9.545299    0.068047

80          6           0        4.203210   -9.583333   -0.400535

81          6           0        3.260882   -8.560933   -0.524078

82          6           0        3.372848   -7.200012   -0.226635

83          6           0        4.574605   -6.499350    0.325552

84          6           0        5.809476   -7.075150    0.636497

85          6           0        2.375555   -6.224015   -0.388703

86          6           0        2.880895   -4.964802    0.036063

87          6           0        4.222119   -5.147305    0.471141

88          7           0        8.427813  -14.531501    0.100932

89          6           0        9.803040  -14.565438    0.496188

90          6           0       10.732765  -15.329790   -0.232517

91          6           0       12.072144  -15.371973    0.163012

92          6           0       12.508140  -14.643698    1.276737

93          6           0       11.585589  -13.876833    1.999186

94          6           0       10.241065  -13.841901    1.620856

95          6           0        7.776281  -15.745651   -0.286323

96          6           0        7.974067  -16.925277    0.454624

97          6           0        7.347502  -18.112433    0.067022

98          6           0        6.504714  -18.139709   -1.050934

99          6           0        6.301186  -16.965016   -1.785635

100          6           0        6.936696  -15.777158   -1.415202

101          6           0        7.714234  -13.300738    0.092925

102          6           0        8.346202  -12.102274   -0.292957

103          6           0        7.645697  -10.898346   -0.289972

104          6           0        6.284933  -10.835581    0.076743

105          6           0        5.661275  -12.044057    0.451898

106          6           0        6.358025  -13.250014    0.470697

107          1           0        2.219633   -0.562090    1.406112

108          1           0        3.451111   -2.689433    1.426051

109          1           0        0.631862   -4.344951   -1.375015

110          1           0       -0.602373   -2.219239   -1.387124

111          1           0        2.218023    0.571183   -1.407327

112          1           0        3.440593    2.703679   -1.426951

113          1           0        0.612713    4.347958    1.372010

114          1           0       -0.612570    2.217049    1.383901

115          1           0       -1.602387   -1.624424    1.413136

116          1           0       -4.059387   -1.646955    1.395969

117          1           0       -4.066592    1.629534   -1.397995

118          1           0       -1.609510    1.617533   -1.415482

119          1           0        7.204527    8.618873   -0.880103

120          1           0        3.820559   10.573109    0.741550

121          1           0        2.257660    8.878677    0.921530

122          1           0        6.527665    6.413347   -1.034146

123          1           0        1.345060    6.425300    0.739950

124          1           0        4.869824    4.390429   -0.821715

125          1           0      -11.067979    1.146668   -1.762356

126          1           0      -11.062617   -1.193311    1.762158

127          1           0       -8.812959   -1.453142    2.230412

128          1           0       -8.819562    1.415716   -2.231347

129          1           0       -6.234193   -1.173286    1.844866

130          1           0       -6.239495    1.146659   -1.846469

131          1           0        8.548193   16.939903   -1.327569

132          1           0        7.431476   19.045823   -0.651016

133          1           0        5.932691   19.087564    1.339661

134          1           0        5.580247   16.999273    2.653306

135          1           0        6.722251   14.902430    1.992764

136          1           0       10.332420   15.928655    1.106431

137          1           0       12.710677   16.019210    0.416894

138          1           0       13.491561   14.729008   -1.567156

139          1           0       11.858502   13.361671   -2.861108

140          1           0        9.475232   13.297426   -2.187756

141          1           0        5.800923   14.180697   -0.795159

142          1           0        4.577414   12.050524   -0.782254

143          1           0        8.107868   10.031686    0.625360

144          1           0        9.331109   12.162034    0.612053

145          1           0      -18.953701   -0.674301    1.456285

146          1           0      -20.222322    0.829198    2.962622

147          1           0      -19.503292    3.195571    3.269909

148          1           0      -17.509179    4.041092    2.037129

149          1           0      -16.261134    2.544561    0.507786

150          1           0      -15.188610    0.251137    2.133689

151          1           0      -12.731727    0.279501    2.130210

152          1           0      -12.731258   -0.332783   -2.129780

153          1           0      -15.188234   -0.314324   -2.132382

154          1           0      -18.956474    0.595929   -1.454121

155          1           0      -20.219350   -0.912731   -2.960154

156          1           0      -19.490983   -3.276258   -3.267330

157          1           0      -17.493368   -4.113762   -2.034749

158          1           0      -16.251055   -2.612152   -0.505708

159          1           0        7.239216   -8.589262    0.882648

160          1           0        3.866067  -10.556357   -0.746022

161          1           0        2.296393   -8.868344   -0.927174

162          1           0        6.552999   -6.386664    1.036994

163          1           0        1.373235   -6.418996   -0.745067

164          1           0        4.887129   -4.370555    0.823395

165          1           0       10.400917  -15.884557   -1.102834

166          1           0       12.778278  -15.965726   -0.409027

167          1           0       13.550171  -14.673743    1.577383

168          1           0       11.909086  -13.314142    2.869334

169          1           0        9.526807  -13.259298    2.191664

170          1           0        8.615797  -16.904527    1.328175

171          1           0        7.509084  -19.014748    0.648499

172          1           0        6.014791  -19.061863   -1.345424

173          1           0        5.656724  -16.974577   -2.659135

174          1           0        6.788801  -14.873337   -1.995414

175          1           0        9.383163  -12.122498   -0.607420

176          1           0        8.151110   -9.997290   -0.621645

177          1           0        4.626321  -12.031804    0.777578

178          1           0        5.858596  -14.156865    0.791282

---------------------------------------------------------------------

Method: DFT B3LYP 6-31G*

Key word: opt freq

Etotal (RB3LYP)= -4148.205875 Hartree

4. Cyclic voltammetry studies

Electrochemical studies were performed in an acetonitrile solution containing tetrabutylammonium hexafluorophosphate (nBu4NPF6) under an argon atmosphere. Ag/AgCl electrode, glassy carbon electrodes and platinum electrodes were used as reference electrodes, working electrodes and counter electrodes, respectively. 5 μl of a 0.8 mg/ml dichloromethane solution of co-oligomer 6 (or 8) was pipetted and dropped onto a glass-carbon electrode which was allowed to evaporate under the pressure of a washing flask at room temperature (the circular opening of the electrode had a diameter of 4 mm).

References

- M. Fujinaga, T. Murafuji, K. Kurotobi, Y. Sugihara, Polyborylation of azulenes. Tetrahedron 2009, Volume 65, 7115–7121.

- T.Tsuchiya, T. Hamano,  M. Inoue, T. Nakamura, A. Wakamiya, Y. Mazaki.  Intense absorption of azulene realized by molecular orbital inversion. Chem. Commun. 2023, Volume 59, 10604–10607.