Supporting information

Enzyme free Impedimetric Sensor for L-Glutamic Acid Using Flower-Like NiO/Carbon Microspheres

Najva Sadri1, Mohammad Mazloum-Ardakani1*, Farzaneh Asadpour2, Yvonne Joseph3, Parvaneh Rahimi3*

1Department of Chemistry, Faculty of Science, Yazd University, Yazd 89195-741, Islamic Republic of Iran; Najva.Sadri.0226@gmail.com; mazloum@yazd.ac.ir

2Department of Chemistry, University of Cincinnati, 312 College Drive 404 Crosley Tower, Cincinnati, Ohio 45221-0172, United States.

3Institute of Nanoscale and Biobased Materials, Faculty of Materials Science and Technology, Technische Universität Bergakademie Freiberg, 09599 Freiberg, Germany.

*Corresponding authors:  E-mail: mazloum@yazd.ac.ir (M. Mazloum-Ardakani), Parvaneh.Rahimi@esm.tu-freiberg.de (P.Rahimi)

Figure S1. CVs of fl-NiO/C/GCE in 5.0 mM [Fe (CN)6]3-/4- in 0.1 M KCl at a scan rate of 20-800 mv/s (A), the plot of I versus υ1/2 (B).

(B)

(A)

Figure S2. Cyclic voltammogram of fl-NiO/C/GCE in 1M NaOH solution at various scan rate 10-100mV/s. (Inset: Plot of I versus υ)

Figure S3. CVs of fl-NiO/C/GCE in 1mM LGA in 1 M NaOH at a scan rate of 10 mV/s (A). Tafel plot E vs log I (B).

(A)

(B)

Laviron’s equation: E = E0′ + [2.303 R T/ (1- α) nα F] log ν + constant where E0′, ν, α, F, T, and R are the formal potential, scan rate (mV/s ); the electron transfer coefficient; Faraday’s constant, the temperature, and the universal gas constant, respectively. nα is the electron number involved in the rate determining step; as the reaction is irreversible, assume that the value of α is 0.5.

Figure S4. The IC/IL vs. t1/2 plot at different concentrations of LGA (250, 500, 700, 1000 μM) (A). The plot of the slope of the (IC/IL vs.t1/2) vs. C1/2 (B).

(A)

(B)

Figure S5. Amprometric response of fl-NiO/C/GCE 600 second before and after injection of 200µL GLA.

Figure S6. CVs of 5 prepared fl-NiO/C/GCE in 1mM LGA in 1 M NaOH at a scan rate of 50 mV/s.

Figure S7. EIS responses of sample (I-III) were recorded at the fl-NiO/C/GCE using standard addition method.