## Slide 1: Figure 1
Chart: TC/RC historical data
Annual benchmark contract | 54.7209 | 54.6143 | 0 | 61.9212 | 61.9212 | 0 | 68.3211 | 68.1611 | 0 | 89.7615 | 89.7084 | 0 | 104.6951 | 104.7485 | 0 | 94.8816 | 94.8816 | 0 | 90.4549 | 90.2949 | 0 | 80.4814 | 80.3748 | 0 | 78.6148 | 78.7214 | 0 | 60.641 | 60.5344
Annual benchmark contract | 57.9855 | 57.9088 | 0 | 63.5844 | 63.5076 | 0 | 85.8274 | 85.8274 | 0 | 78.081 | 77.9274 | 0 | 38.8103 | 38.7336 | 0 | 43.9493 | 43.7957

## Slide 2: Figure 2
Chart: wt.% Cu in concentrate
| 0 | 10 | 15 | 20.198399999999999 | 20.380400000000002 | 20.785299999999999 | 20.9892 | 21.986499999999999 | 22.994599999999998 | 23.997299999999999 | 24.404900000000001 | 24.587 | 24.788 | 24.994599999999998 | 26.008099999999999 | 26.9999 | 27.9999 | 28.994399999999999 | 29.206299999999999 | 29.402000000000001 | 29.613900000000001 | 29.8123 | 29.9998 | 31.0105 | 32.007599999999996 | 33.0184 | 34.015599999999999 | 35.015500000000003 | 36.012599999999999 | 37.0152 | 38.012300000000003 | 39.020299999999999 | 40.017499999999998 | 45 | 50
Copper payable | 80 | 90 | 93.2 | 95.0464 | 95.0972 | 95.1848 | 95.2303 | 95.4528 | 95.6533 | 95.8347 | 95.903 | 95.938 | 95.9669 | 96.0028 | 96.1605 | 96.2989 | 96.4312 | 96.5574 | 96.5793 | 96.6012 | 96.6013 | 96.6022 | 96.6547 | 96.6531 | 96.6532 | 96.7032 | 96.7034 | 96.7516 | 96.7562 | 96.7537 | 96.7547 | 96.7539 | 96.7549 | 97 | 97
Recovery from smelter survey | 97.2 | 98.5 | 98.8 | 98.8
Recovery, this study estimate | 98.5443 | 97.4806
Chart: ppm Au in concentrate
| 0 | 1 | 1.9911099999999999 | 2.9801500000000001 | 3.0024500000000001 | 3.9914900000000002 | 4.9888199999999996 | 4.9927099999999998 | 5.9962600000000004 | 6.9832299999999998 | 6.9933300000000003 | 7.9948100000000002 | 8.9942200000000003 | 9.9874100000000006 | 9.9954499999999999 | 10.999000000000001 | 12.000500000000001 | 12.9999 | 14.0014 | 14.9946 | 20 | 30
Gold payable | 92 | 92 | 92.0005 | 91.9973 | 93.9936 | 93.9923 | 93.9928 | 94.9984 | 95.0008 | 95.0032 | 96.0032 | 96.0056 | 96.0061 | 95.9992 | 96.9992 | 97.0016 | 97.004 | 97.004 | 97.004 | 97.004 | 97.004 | 97.004
Recovery at 21 wt%Cu in conc. | 98 | 98
Recovery at 25 wt%Cu in conc. | 99 | 99
Recovery, this study estimate | 99.1944 | 98.2329

## Slide 3: Figure 3

## Slide 4: Figure 4
Pt wire
Working
thermocouple
Heating elements
Gas outlet
Ar-CO-CO2-SO2 gas flow
Controller
thermocouple
Hot zone
Quenching bucket
Alumina
tube
Removable
cap
Quenching
solution
Steel block
Pt wire
Sample
Ar-CO-CO2-SO2
Ar-CO-CO2-SO2 gas flow

## Slide 5: Figure 5
matte
slag
spinel
60 μm
matte
slag
spinel
olivine
120 μm

## Slide 6: Figure 6
Flash smelting
1300 °C, -30 MW, 85 vol% O2 in blast
Flash converting
1260 °C, -7 MW, 85 vol% O2 in blast
Anode furnace
Oxidation and Reduction
1190 °C , -0.2 MW
Fe/SiO2 = 1.4 (0% solids)
70 wt% Cu in matte
1900 ppm S
20 ppm S, 1490 ppm O
Gas cleaning
-101 MW, 250 °C
Gas cleaning
Slag crushing
and flotation
Concentrate
+ 0.5 t/h H2O
30 t/h SiO2
61 kNm3/h Blast
4 t/h Coal
50 kNm3 Air
4 t/h CaCO3
85.5 t/h Matte
57.4 t/h Blister copper
0.2 t/h Scrap
SiO2
Air, N2
Anode copper
97 kNm3/h Off-gas, 40 vol% SO2
CH4
10.2 t/h Slag conc.
15.2 t/h Converter
slag
0.3 t/h Anode slag
22wt% Cu in slag, Fe/CaO = 3.0
34 t/h Smelter dust
9.2 t/h Converter Dust
0.1 t/h Dust
Cooling
230 t/h dry
57.1 t/h
(56.9 t/h Cu)
17 kNm3/h Blast
0.7 t/h Coal
10 kNm3 Air
26 kNm3/h Off-gas, 49 vol% SO2
158.1 t/h Slag
Gas cleaning
-23 MW, 250 °C
147.9 t/h Discard slag (0.6 wt% Cu)

## Slide 7: Figure 7
Bottom-blown
Refining
1240 °C , 0 MW, 31 vol%O2 in blast
Bottom-blown
Converting furnace
1250 °C , -4 MW, 24 vol%O2 in blast
Bottom-blown
Smelting furnace
1200 °C , -15 MW, 68 vol%O2 in blast
Fe/SiO2 = 1.55 (8% solid spinel)
74 wt% Cu in matte
750 ppm S
20 ppm S, 45 ppm O
Gas cleaning
Slag crushing
and flotation
SiO2
Anode copper
CH4
23wt% Cu in slag, Fe/SiO2 = 1.0
150 t/h dry
Same furnace
12 t/h SiO2
57 kNm3/h Blast
0 t/h Coal
7.3 t/h Slag conc.
8.3 t/h Smelter dust
5.7 t/h Converter
slag
25 kNm3 Air
1.5 t/h SiO2
28 kNm3/h Blast
0.05 t/h Coal
43.5 t/h hot Matte
0.3 t/h Anode slag
0.9 t/h Converter Dust
3 kNm3 Air
0.2 t/h Scrap
31.5 t/h Blister copper
31.4 t/h
(31.1 t/h Cu)
69 kNm3/h Off-gas, 19 vol% SO2
30 kNm3/h Off-gas, 17 vol% SO2
0.1 t/h Dust
Air, N2
107.4 t/h Slag
(including 8.7 t/h spinel)
101.1 t/h Discard slag (0.8 wt% Cu)
Concentrate
+ 13 t/h H2O
Gas cleaning
-80 MW, 250 °C
Gas cleaning
-15 MW, 250 °C

## Slide 8: Figure 8
Chart: P(SO2), atm
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Target | 0.85772 | 0.82993 | 0.82993 | 0.85732 | 0.85732 | 0.83286 | 0.83957 | 0.80927 | 0.82284 | 0.83957 | 0.85772 | 0.999 | 0.999 | 0.83286 | 0.999 | 0.999 | 0.8 | 0.8 | 0.8 | 0.8 | 0.8 | 0.8 | 0.8 | 0.8 | 0.8
Calculated | 0.85707 | 0.82927 | 0.8292 | 0.8567 | 0.85661 | 0.83213 | 0.83888 | 0.8086 | 0.82218 | 0.83878 | 0.85709 | 0.99559 | 0.99638 | 0.83239 | 0.99242 | 0.99505 | 0.79928 | 0.79931 | 0.79879 | 0.79878 | 0.79868 | 0.7985 | 0.79875 | 0.79879 | 0.7988
Chart: Matte grade, wt. % Cu in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Target | 65.6693 | 74.8919 | 75.7631 | 77.5158 | 65.4071 | 59.6717 | 60.5279 | 71.2246 | 64.5054 | 49.5525 | 55.3001 | 60.7674 | 67.5816 | 48.758 | 48.9644 | 57.8259 | 76.6561 | 73.3104 | 77.0583 | 74.412 | 58.0162 | 57.731 | 72.4425 | 70.027 | 55.2964
Calculated | 66.041 | 75.2205 | 76.1304 | 77.9078 | 65.7678 | 59.9865 | 60.8149 | 71.4742 | 64.783 | 49.9132 | 55.6599 | 60.9964 | 67.837 | 49.0142 | 49.287 | 58.369 | 76.9702 | 73.6014 | 77.3236 | 74.7227 | 58.4086 | 58.1478 | 72.7522 | 70.402 | 55.6868
Chart: Temperature, °C
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Target | 1200 | 1200 | 1200 | 1250 | 1250 | 1200 | 1250 | 1250 | 1250 | 1250 | 1200 | 1250 | 1250 | 1200 | 1200 | 1200 | 1270 | 1270 | 1300 | 1300 | 1250 | 1250 | 1250 | 1200 | 1200
Calculated | 1200 | 1200 | 1200 | 1250 | 1250 | 1200 | 1250 | 1250 | 1250 | 1250 | 1200 | 1250 | 1250 | 1200 | 1200 | 1200 | 1270 | 1270 | 1300 | 1300 | 1250 | 1250 | 1250 | 1200 | 1200
Chart: wt% Al2O3 in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 8.75 | 9.21 | 11.58 | 12.9017 | 8.2569 | 0 | 10.9123 | 12.27 | 7.8 | 0 | 9.14 | 0 | 0 | 19.7072 | 19.7065 | 9.3007 | 9.3616 | 12.1717 | 0 | 0
Calculated | 0 | 0 | 0 | 0 | 0 | 7.9347 | 8.5391 | 11.3928 | 12.5065 | 7.5772 | 0 | 10.5782 | 11.5055 | 6.8739 | 0 | 8.2817 | 0 | 0 | 18.9169 | 17.5052 | 9.1736 | 9.7114 | 12.2416 | 0 | 0
Chart: wt% MgO in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 1.3991 | 2.8493 | 3.1233 | 1.96 | 4.14 | 0 | 0 | 0 | 0 | 0 | 1.8784 | 0 | 0 | 0 | 2.1845 | 0 | 5.6863 | 4.6341 | 0.13947 | 0.2133 | 0 | 0 | 0 | 2.93 | 2.04
Calculated | 1.3786 | 2.5935 | 3.2925 | 1.9119 | 4.3455 | 0 | 0 | 0 | 0 | 0 | 1.7232 | 0 | 0 | 0 | 1.9197 | 0 | 5.6694 | 4.7138 | 0.16302 | 0.21363 | 0 | 0 | 0 | 2.8435 | 2.142
Chart: wt% CaO in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 5.16 | 5.76 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 3.9322 | 3.483 | 2.8317 | 2.7976 | 0 | 0 | 0 | 0 | 0
Calculated | 0 | 0 | 0 | 4.9122 | 5.3134 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 3.5231 | 3.1388 | 2.9448 | 2.7696 | 0 | 0 | 0 | 0 | 0

## Slide 9: Figure 9
Chart: Wt.% Cu in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0.73551 | 0.81243 | 0.79528 | 1.2946 | 0.57732 | 0.5233 | 0.71055 | 0.68114 | 0.95262 | 0.67948 | 0.50574 | 0.81376 | 0.92772 | 0.42926 | 0.55435 | 0.6559 | 1.2827 | 1.0277 | 1.3857 | 0.76773 | 0.72696 | 0.55459 | 1.0653 | 0.76683 | 0.80393
Calculated | 0.66274 | 0.74971 | 0.80895 | 1.0965 | 0.59709 | 0.48911 | 0.64547 | 0.73056 | 0.94864 | 0.62265 | 0.59821 | 0.88593 | 1.0383 | 0.47879 | 0.55544 | 0.68594 | 1.066 | 0.84657 | 1.2196 | 0.88239 | 0.61783 | 0.59768 | 0.88842 | 0.68588 | 0.67386
Chart: Fe/SiO2 in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 1.7157 | 1.4034 | 1.4266 | 1.3556 | 1.6013 | 1.4323 | 1.7242 | 1.4176 | 1.0583 | 1.6492 | 1.4094 | 1.286 | 1.1764 | 1.4175 | 1.7569 | 1.1168 | 1.338 | 1.5567 | 0.8305 | 0.84909 | 1.6202 | 1.3411 | 1.2339 | 1.3084 | 1.7778
Calculated | 1.8051 | 1.4828 | 1.4206 | 1.4356 | 1.7091 | 1.2562 | 1.5435 | 1.2063 | 0.96469 | 1.4989 | 1.5138 | 1.0436 | 0.99232 | 1.2443 | 1.718 | 1.0157 | 1.5074 | 1.7248 | 0.77476 | 0.89669 | 1.4663 | 1.4267 | 1.0668 | 1.4623 | 1.919
Chart: ppm Au and Ag in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Au, exp LA ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.35995 | 2.1753 | 4.3562 | 1.1215 | 0.53462 | 1.5301 | 0.45779 | 0.8206 | 4.2584 | 5.1525 | 0.54425 | 1.2394 | 6.6318
Au, Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 2.2156 | 9.0139 | 3.5393 | 1.5607 | 1.5852 | 3.1243 | 4.5159 | 1.6883 | 3.9561 | 3.4452 | 0.6355 | 1.0026 | 5.2749
Ag, exp LA ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 52.4858 | 42.0944 | 44.967 | 65.8556 | 62.1653 | 4.4677 | 22.8511 | 5.1907 | 45.8994 | 58.0456 | 54.243 | 32.9955 | 43.2223
Ag, Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 67.9146 | 48.4977 | 30.1642 | 57.9843 | 60.5918 | 8.5041 | 28.9877 | 10.0914 | 39.8424 | 37.5209 | 36.7747 | 30.1875 | 47.6849

## Slide 10: Figure 10
Chart: wt.% Cu in slag: Calculated - Experimental
| 65.669263430536049 | 74.891881740251321 | 75.763107737414089 | 77.51580341005878 | 65.407074182864193 | 59.67171043303906 | 60.527949682128629 | 71.224646596906297 | 64.50541329411277 | 49.552477977937585 | 55.300062987160949 | 60.767425681915689 | 67.581626001050068 | 48.757961763242719 | 48.964402070152659 | 57.825902248946136 | 76.656126324818501 | 73.310402196468161 | 77.058327610268563 | 74.412001706437707 | 58.016221366989278 | 57.730973450056766 | 72.442506471476705 | 70.027019887056099 | 55.296350446952083
%Cu in liquid slag | -0.072775 | -0.062715 | 0.013663 | -0.19808 | 0.019771 | -0.03419 | -0.065075 | 0.049426 | -0.0039814 | -0.056826 | 0.092472 | 0.072171 | 0.11062 | 0.049538 | 0.0010867 | 0.030041 | -0.21671 | -0.1811 | -0.1661 | 0.11466 | -0.10913 | 0.043089 | -0.1769 | -0.080952 | -0.13007
Chart: Fe/SiO2 in slag: Calculated - Experimental
| 0 | 0 | 0 | 0 | 0 | 8.75 | 9.2100000000000009 | 11.58 | 12.901721627057036 | 8.2569277671350712 | 0 | 10.91234642310838 | 12.27 | 7.8 | 0 | 9.14 | 0 | 0 | 19.707163148719228 | 19.706537918605587 | 9.3006753468549679 | 9.3616310745875655 | 12.171706180814814 | 0 | 0
Fe/SiO2 in liquid slag vs wt.% Al2O3 in slag | 0.089326 | 0.079386 | -0.0060391 | 0.080059 | 0.10777 | -0.17613 | -0.1807 | -0.21129 | -0.093592 | -0.15032 | 0.10439 | -0.24233 | -0.18412 | -0.17327 | -0.038874 | -0.10105 | 0.16942 | 0.1681 | -0.055743 | 0.047602 | -0.15396 | 0.085634 | -0.1671 | 0.15392 | 0.14121
Fe/SiO2 in liquid slag vs wt.% MgO in slag | 0.089326 | 0.079386 | -0.0060391 | 0.080059 | 0.10777 | -0.17613 | -0.1807 | -0.21129 | -0.093592 | -0.15032 | 0.10439 | -0.24233 | -0.18412 | -0.17327 | -0.038874 | -0.10105 | 0.16942 | 0.1681 | -0.055743 | 0.047602 | -0.15396 | 0.085634 | -0.1671 | 0.15392 | 0.14121

## Slide 11: Table S1. Experiments #1-8. EPMA data
# exp. | Exp. name | Temp (°C) | Substrate | logP(O2), atm | logP(S2), atm | logP(SO2), atm | Phase | Composition (wt%) |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  | Cu/Cu2O | Fe/FeO | S | O/SiO2 | MgO | Al2O3 | CaO | "Old" total
1 | RSM1 | 1200 | spinel | -7.95 | -2.17 | 0.86 | slag | 0.83 | 65.04 | 1.00 | 29.47 | 1.40 | 0.00 | 0.00 | 98.9
 |  |  |  |  |  |  | matte | 65.67 | 9.78 | 23.67 | 0.88 | 0.00 | 0.00 | 0.00 | 102.3
 |  |  |  |  |  |  | spinel | bdl | 99.32 | bdl | 0.38 | 0.28 | 0.00 | 0.00 | 100.2
2 | RSM3 | 1200 | spinel | -7.68 | -2.68 | 0.83 | slag | 0.91 | 61.93 | 0.28 | 34.31 | 2.85 | 0.00 | 0.00 | 99.7
 |  |  |  |  |  |  | matte | 74.89 | 3.46 | 21.03 | 0.57 | 0.00 | 0.00 | 0.00 | 102.6
 |  |  |  |  |  |  | spinel | bdl | 98.86 | bdl | 0.54 | 0.56 | 0.00 | 0.00 | 100.4
 |  |  |  |  |  |  | tridymite | bdl | 1.27 | bdl | 98.67 | 0.07 | 0.00 | 0.00 | 101.3
3 | RSM3 | 1200 | MgO | -7.68 | -2.68 | 0.83 | slag | 0.90 | 61.94 | 0.29 | 33.76 | 3.12 | 0.00 | 0.00 | 100.7
 |  |  |  |  |  |  | matte | 75.76 | 3.02 | 20.79 | 0.43 | 0.00 | 0.00 | 0.00 | 100.4
 |  |  |  |  |  |  | spinel | 0.09 | 98.43 | bdl | 0.71 | 0.77 | 0.00 | 0.00 | 97.6
 |  |  |  |  |  |  | oivine | 0.13 | 55.88 | bdl | 31.73 | 12.24 | 0.00 | 0.00 | 101.7
4 | RSM6 | 1250 | spinel | -7.52 | -2.20 | 0.86 | slag | 1.46 | 58.11 | 0.15 | 33.33 | 1.96 | 0.00 | 5.16 | 98.0
 |  |  |  |  |  |  | matte | 77.52 | 1.38 | 20.87 | 0.23 | 0.00 | 0.00 | 0.00 | 102.1
 |  |  |  |  |  |  | spinel | bdl | 98.86 | bdl | 0.33 | 0.77 | 0.00 | bdl | 101.9
5 | RSM6 | 1250 | MgO | -7.52 | -2.20 | 0.86 | slag | 0.65 | 59.68 | 0.82 | 28.98 | 4.14 | 0.00 | 5.76 | 100.7
 |  |  |  |  |  |  | matte | 65.41 | 10.51 | 22.74 | 0.87 | 0.00 | 0.00 | 0.00 | 100.5
 |  |  |  |  |  |  | spinel | bdl | 97.76 | bdl | 0.53 | 1.58 | 0.00 | bdl | 97.0
 |  |  |  |  |  |  | oivine | 0.08 | 43.28 | bdl | 34.45 | 21.66 | 0.00 | 0.52 | 100.8
6 | RSM8 | 1200 | Al2O3 | -8.00 | -2.09 | 0.83 | slag | 0.59 | 58.74 | 0.78 | 31.89 | 0.00 | 8.75 | 0.00 | 100.2
 |  |  |  |  |  |  | matte | 59.67 | 14.29 | 24.77 | 1.27 | 0.00 | 0.00 | 0.00 | 102.9
 |  |  |  |  |  |  | spinel | bdl | 84.09 | bdl | 0.35 | 0.00 | 15.54 | 0.00 | 98.2
7 | RSM10 | 1250 | Al2O3 | -7.55 | -2.11 | 0.84 | slag | 0.80 | 62.00 | 0.97 | 27.96 | 0.00 | 9.21 | 0.00 | 99.9
 |  |  |  |  |  |  | matte | 60.53 | 14.18 | 24.23 | 1.06 | 0.00 | 0.00 | 0.00 | 103.1
 |  |  |  |  |  |  | spinel | bdl | 76.96 | bdl | 0.43 | 0.00 | 22.58 | 0.00 | 98.5
8 | RSM12 | 1250 | Al2O3 | -7.28 | -2.65 | 0.81 | slag | 0.77 | 56.55 | 0.33 | 31.02 | 0.00 | 11.58 | 0.00 | 100.3
 |  |  |  |  |  |  | matte | 71.22 | 6.17 | 22.02 | 0.59 | 0.00 | 0.00 | 0.00 | 102.0
 |  |  |  |  |  |  | spinel | bdl | 65.61 | bdl | 0.14 | 0.00 | 34.17 | 0.00 | 99.6

## Slide 12: Table S2. Experiments #9-16. EPMA data

## Slide 13: Table S3. Experiments #9-16. LA-ICP-MS data
# exp. | Exp. name | Temp (°C) | Substrate | logP(O2), atm | logP(SO2), atm | Phase | Composition (ppm) |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  | Cu | Fe | S | Al | Mg | Si | Ni | Co | As | Bi | Pb | Zn | Au | Ag | Sb
9 | RSM13 new | 1250 | Al2O3 | -7.25 | 0.82 | slag | 9050 | 375682.88 | 1012.58 | 68282.45 | 433.92 | 165993.17 | 6570.88 | 1426.86 | 1066.12 | 16.25 | n/a | 2299.65 | 0.36 | 52.49 | 5215.19
 |  |  |  |  |  | matte | 645054 | 37444.23 | 201999.21 | n/a | n/a | n/a | 49308.00 | 765.67 | 1826.34 | 287.45 | n/a | 240.10 | 5931.80 | 8590.96 | 1971.77
 |  |  |  |  |  | spinel | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a
10 | RSM11 new | 1250 | Al2O3 | -7.55 | 0.84 | slag | 6455 | 468620.52 | 5835.32 | 43699.85 | 173.93 | 132864.35 | 4226.21 | 1531.15 | 1983.09 | 604.86 | n/a | 3673.47 | 2.18 | 42.09 | 3842.46
 |  |  |  |  |  | matte | 495525 | 131841.53 | 220716.14 | n/a | n/a | n/a | 84525.84 | 2467.47 | 3938.59 | 3294.55 | n/a | 783.07 | 4611.82 | 7145.00 | 2658.58
 |  |  |  |  |  | spinel | 37 | 632338.53 | 232.28 | 69050.33 | 44.39 | 1679.49 | 8274.14 | 1783.55 | 1.90 | 0.02 | n/a | 2926.72 | 0.01 | 0.02 | 3.53
11 | RSM2 new | 1200 | MgO | -7.95 | 0.86 | slag | 4805 | 476859.84 | 9719.04 | 85.70 | 13776.88 | 158204.46 | 3997.48 | 1956.90 | 909.89 | 144.04 | n/a | 7830.71 | 4.36 | 44.97 | 7247.94
 |  |  |  |  |  | matte | 553001 | 105666.47 | 220824.62 | n/a | n/a | n/a | 84317.41 | 2439.99 | 662.13 | 4558.53 | n/a | 1291.02 | 5782.42 | 7215.07 | 3234.47
 |  |  |  |  |  | spinel | 25 | 739318.21 | 258.50 | 111.00 | 4430.49 | 4734.33 | 9748.09 | 2142.80 | 23.81 | 0.10 | n/a | 3045.61 | 0.00 | 0.00 | 26.46
12 | RSM11 old (pure SO2) | 1250 | Al2O3 |  | 1.00 | slag | 7731 | 419211.02 | 1695.51 | 57753.67 | 410.83 | 152430.53 | 6202.46 | 2181.04 | 226.74 | 0.84 | n/a | 3421.46 | 1.12 | 65.86 | 5081.35
 |  |  |  |  |  | matte | 607674 | 44369.07 | 220936.08 | n/a | n/a | n/a | 90602.97 | 1425.32 | 490.45 | 10.28 | n/a | 309.05 | 8344.68 | 9273.98 | 2611.31
 |  |  |  |  |  | spinel | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a
13 | RSM13old (pure SO2) | 1250 | Al2O3 |  | 1.00 | slag | 8813 | 397384.38 | 1035.30 | 64939.06 | 297.87 | 152430.53 | 6312.02 | 1979.04 | 681.00 | 2.91 | n/a | 3667.14 | 0.53 | 62.17 | 5371.93
 |  |  |  |  |  | matte | 675816 | 23264.61 | 208300.38 | n/a | n/a | n/a | 61022.77 | 618.34 | 1003.89 | 11.82 | n/a | 209.21 | 5416.99 | 7831.00 | 21.10
 |  |  |  |  |  | spinel | 121 | 568780.60 | 145.77 | 76105.66 | 66.60 | 2026.04 | 22332.24 | 2412.69 | 1.63 | 0.02 | n/a | 3134.21 | bdl | 0.08 | 56.40
14 | RSM9 | 1200 | Al2O3 | -8.00 | 0.83 | slag | 4078 | 453032.26 | 4521.70 | 41281.55 | 145.45 | 149438.94 | 2582.29 | 1603.90 | 2950.11 | 123.15 | n/a | 4161.12 | 1.53 | 4.47 | 5187.19
 |  |  |  |  |  | matte | 487580 | 149567.24 | 242918.66 | n/a | n/a | n/a | 97746.58 | 3063.43 | 5861.37 | 6235.14 | n/a | 970.55 | 5251.99 | 948.69 | 4022.42
 |  |  |  |  |  | spinel | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a | n/a
15 | RSM2 pure SO2 | 1200 | MgO |  | 1.00 | slag | 5266 | 513715.32 | 5949.21 | 213.06 | 14775.26 | 136724.71 | 3440.99 | 2271.68 | 4812.17 | 13.04 | n/a | 7054.31 | 0.46 | 22.85 | 6141.86
 |  |  |  |  |  | matte | 489644 | 52520.11 | 241072.44 | n/a | n/a | n/a | 55634.93 | 1131.98 | 4809.57 | 209.62 | n/a | 692.13 | 3011.42 | 5461.39 | 1250.54
 |  |  |  |  |  | spinel | 228 | 753830.24 | 343.04 | 143.82 | 3315.31 | 5955.35 | 13116.70 | 2091.98 | 6.80 | 0.37 | n/a | 2571.09 | bdl | 1.29 | 184.96
 |  |  |  |  |  | olivine | 216 | 427473.49 | 242.79 | n/a | 66653.11 | 147242.00 | 14945.14 | 3841.48 | 0.18 | 0.03 | n/a | 4808.96 | bdl | 0.15 | 7.43
16 | RSM9 (pure SO2 | 1200 | Al2O3 |  | 1.00 | slag | 6231 | 405918.20 | 1633.83 | 48373.51 | 230.81 | 169959.34 | 3648.67 | 1569.18 | 488.80 | 8.53 | n/a | 4048.74 | 0.82 | 5.19 | 5002.72
 |  |  |  |  |  | matte | 578259 | 72377.84 | 231142.99 | n/a | n/a | n/a | 96471.39 | 1872.18 | 913.50 | 277.33 | n/a | 571.42 | 6180.99 | 1038.53 | 2739.06
 |  |  |  |  |  | spinel | 89 | 669259.47 | 198.32 | 49598.55 | 37.46 | 2464.67 | 11467.80 | 2126.13 | 0.92 | 0.03 | n/a | 2808.69 | 0.00 | bdl | 6.19

## Slide 14: Table S4. Experiments #17-20. EPMA data
# exp. | Exp. name | Temp (°C) | Substrate | logP(O2), atm | logP(S2), atm | logP(SO2), atm | Phase | Composition (wt%) |  |  |  |  |  |  | 
 |  |  |  |  |  |  |  | Cu/Cu2O | Fe/FeO | S | O/SiO2 | MgO | Al2O3 | CaO | "Old" total
17 | RSM14 new | 1270 | MgO |  |  | 0.80 | slag | 1.28 | 56.28 | 0.11 | 32.70 | 5.69 | 0.00 | 3.93 | 98.6
 |  |  |  |  |  |  | matte | 76.66 | 1.59 | 20.89 | 0.87 | 0.00 | 0.00 | 0.00 | 101.3
 |  |  |  |  |  |  | spinel | 0.02 | 97.88 | 0.01 | 0.45 | 1.67 | 0.00 | 0.02 | 99.0
 |  |  |  |  |  |  | olivine | 0.08 | 42.67 | 0.01 | 34.39 | 22.65 | 0.00 | 0.23 | 99.5
18 | RSM15 new | 1270 | MgO |  |  | 0.80 | slag | 1.03 | 60.35 | 0.38 | 30.14 | 4.63 | 0.00 | 3.48 | 98.4
 |  |  |  |  |  |  | matte | 73.31 | 3.91 | 21.62 | 1.16 | 0.00 | 0.00 | 0.00 | 101.7
 |  |  |  |  |  |  | spinel | 0.02 | 97.82 | 0.01 | 0.51 | 1.62 | 0.00 | 0.07 | 98.9
 |  |  |  |  |  |  | oivine | 0.13 | 44.04 | 0.01 | 34.42 | 21.17 | 0.00 | 0.28 | 99.3
19 | RSM17 | 1300 | Al2O3 |  |  | 0.80 | slag | 1.39 | 39.19 | 0.06 | 36.69 | 0.14 | 19.71 | 2.83 | 98.2
 |  |  |  |  |  |  | matte | 77.06 | 1.69 | 21.22 | 0.03 | 0.00 | 0.00 | 0.00 | 101.9
 |  |  |  |  |  |  | spinel | 0.12 | 53.99 | 0.00 | 0.07 | 0.23 | 45.57 | 0.02 | 98.9
20 | RSM6 | 1300 | Al2O3 |  |  | 0.80 | slag | 0.77 | 39.91 | 0.06 | 36.55 | 0.21 | 19.71 | 2.80 | 98.3
 |  |  |  |  |  |  | matte | 74.41 | 3.64 | 21.71 | 0.23 | 0.00 | 0.00 | 0.00 | 102.0
 |  |  |  |  |  |  | spinel | 0.05 | 78.56 | 0.00 | 0.23 | 0.08 | 21.07 | 0.01 | 100.2

## Slide 15: Table S5. Experiments #21-25. EPMA + LA-ICP-MS data
# exp. | Exp. name | Temp (°C) | Substrate | logP(O2), atm | logP(SO2), atm | Phase | Composition (wt%) |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 |  |  |  |  |  |  | Cu/Cu2O | Fe/FeO | S | O/Al2O3 | MgO | SiO2 | Ni | Co | As | Bi | Pb | Zn | Au | Ag | Sb
21 | RSM11 new | 1250 | Al2O3 |  | 0.80 | slag | 0.73 | 57.84 | 0.84 | 9.30 | 0.00 | 27.76 | 0.06 | 0.18 | 1.23E-02 | 3.28E-05 | 0.08 | 0.57 | 4.26E-04 | 4.59E-03 | 0.40
 |  |  |  |  |  | matte | 58.02 | 12.23 | 23.42 | 1.11 | 0.00 | 0.00 | 1.15 | 0.20 | 7.07E-03 | 4.95E-04 | 0.11 | 0.17 | 0.44 | 0.55 | 0.08
 |  |  |  |  |  | spinel | 0.04 | 73.54 | 0.00 | 21.72 | 0.00 | 0.35 | 0.23 | 0.24 | 1.51E-03 | 1.71E-06 | 0.03 | 0.88 | 0.00 | 0.00 | 0.00
22 | RSM9 new | 1250 | Al2O3 |  | 0.80 | slag | 0.55 | 54.49 | 0.63 | 9.36 | 0.00 | 31.59 | 0.04 | 0.16 | 0.05 | 0.01 | 0.14 | 0.54 | 5.15E-04 | 5.80E-03 | 0.33
 |  |  |  |  |  | matte | 57.73 | 12.59 | 23.86 | 0.77 | 0.00 | 0.00 | 1.17 | 0.21 | 1.49E-02 | 2.11E-01 | 0.22 | 0.18 | 0.41 | 0.52 | 0.09
 |  |  |  |  |  | spinel | 0.03 | 80.39 | 0.00 | 14.78 | 0.00 | 0.52 | 0.07 | 0.25 | 0.02 | 0.00 | 0.02 | 0.61 | 0.00 | 0.00 | 0.01
23 | RSM13 new | 1250 | Al2O3 |  | 0.80 | slag | 1.07 | 50.97 | 0.18 | 12.17 | 0.00 | 32.12 | 0.10 | 0.25 | 0.04 | 0.00 | 0.17 | 0.48 | 5.44E-05 | 5.42E-03 | 0.55
 |  |  |  |  |  | matte | 72.44 | 2.71 | 20.36 | 0.56 | 0.00 | 0.00 | 0.84 | 0.06 | 3.88E-03 | 3.33E-05 | 0.10 | 0.09 | 0.39 | 0.48 | 0.11
 |  |  |  |  |  | spinel | 0.05 | 62.95 | 0.00 | 31.70 | 0.00 | 0.33 | 0.37 | 0.46 | 0.01 | 0.00 | 0.02 | 1.44 | 0.00 | 0.00 | 0.01
24 | RSM4 new | 1200 | MgO |  | 0.80 | slag | 0.77 | 57.48 | 0.34 | 0.00 | 2.93 | 34.16 | 0.11 | 0.23 | 0.18 | 0.03 | 0.30 | 0.73 | 1.24E-04 | 3.30E-03 | 0.57
 |  |  |  |  |  | matte | 70.03 | 3.87 | 20.96 | 0.78 | 0.00 | 0.00 | 0.81 | 0.09 | 1.63E-02 | 2.63E-01 | 0.37 | 0.12 | 0.52 | 0.61 | 0.04
 |  |  |  |  |  | spinel | 0.07 | 91.60 | 0.00 | 0.00 | 3.27 | 0.37 | 0.41 | 0.25 | 0.04 | 0.00 | 0.04 | 0.38 | 0.00 | 0.00 | 0.01
 |  |  |  |  |  | olivine | 0.05 | 52.28 | 0.00 | 0.00 | 11.49 | 32.24 | 0.52 | 0.48 | 0.12 | 0.00 | 0.02 | 0.58 | 0.00 | 0.00 | 0.00
25 | RSM2 new | 1200 | MgO |  | 0.80 | slag | 0.80 | 63.17 | 1.45 | 0.00 | 2.04 | 27.63 | 0.06 | 0.18 | 0.55 | 0.03 | 0.28 | 0.80 | 6.63E-04 | 4.32E-03 | 0.61
 |  |  |  |  |  | matte | 55.30 | 13.26 | 22.93 | 1.44 | 0.00 | 0.00 | 1.07 | 0.21 | 0.10 | 0.72 | 0.67 | 0.23 | 0.50 | 0.74 | 0.19
 |  |  |  |  |  | spinel | 0.00 | 94.27 | 0.00 | 0.00 | 0.62 | 0.78 | 0.16 | 0.17 | 0.02 | 0.00 | 0.03 | 0.33 | 0.00 | 0.00 | 0.00
 |  |  |  |  |  | olivine | 0.03 | 53.83 | 0.00 | 0.00 | 10.71 | 32.01 | 0.23 | 0.33 | 0.11 | 0.00 | 0.02 | 0.63 | 0.00 | 0.00 | 0.00

## Slide 16: Figure S1. FactSage predictions for experiments
Chart: wt%S in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 23.6723 | 21.0302 | 20.7875 | 20.8743 | 22.7441 | 24.7701 | 24.2275 | 22.0186 | 20.1999 | 22.0716 | 22.0825 | 22.0936 | 20.83 | 24.2919 | 24.1072 | 23.1143 | 20.8862 | 21.6172 | 21.2214 | 21.7137 | 23.4163 | 23.8567 | 20.3594 | 20.9596 | 22.9254
Calculated | 22.8417 | 21.1495 | 20.9576 | 20.449 | 22.6151 | 23.98 | 23.5646 | 21.8602 | 21.9403 | 23.9515 | 23.4268 | 22.7282 | 21.6739 | 24.699 | 24.6036 | 23.4101 | 20.6158 | 21.2726 | 20.6233 | 21.1748 | 23.5842 | 23.5704 | 21.231 | 21.4791 | 23.4827
Chart: wt%Fe in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 9.7791 | 3.4562 | 3.0179 | 1.3784 | 10.5114 | 14.2925 | 14.1847 | 6.1655 | 2.6411 | 10.2379 | 6.5799 | 4.0688 | 2.338 | 10.8115 | 11.0523 | 5.7853 | 1.5862 | 3.915 | 1.6909 | 3.6444 | 12.2336 | 12.5865 | 2.714 | 3.8667 | 13.2616
Calculated | 10.6882 | 3.5076 | 2.8081 | 1.529 | 11.0407 | 15.4048 | 14.8899 | 6.4362 | 3.3329 | 10.8975 | 6.8745 | 4.3277 | 2.9189 | 11.0892 | 11.6171 | 5.6766 | 2.2672 | 4.8803 | 1.9486 | 3.9433 | 14.3953 | 14.4393 | 3.7551 | 4.8898 | 15.273
Chart: log10[P(O2), atm]
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | -7.95 | -7.68 | -7.68 | -7.52 | -7.52 | -8 | -7.55 | -7.28 | -7.2549 | -7.5547 | -7.9457 | -7.9967
Calculated | -7.9069 | -7.6469 | -7.5907 | -6.9603 | -7.4687 | -8.0684 | -7.6257 | -7.4463 | -7.2517 | -7.5045 | -7.7701 | -7.2305 | -7.1578 | -7.9432 | -7.8563 | -7.5916 | -6.9229 | -7.1227 | -6.8042 | -6.9769 | -7.6402 | -7.6463 | -7.3213 | -7.7551 | -8.0148
Chart: Mass slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Target | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9 | 0.9
Calculated | 0.9192 | 1.0047 | 0.92984 | 0.9453 | 0.97741 | 0.83269 | 0.84326 | 0.82075 | 0.85963 | 0.8541 | 0.94723 | 0.80053 | 0.81571 | 0.842 | 0.87521 | 0.81975 | 1.0063 | 1.0022 | 0.86602 | 0.90922 | 0.82809 | 0.93096 | 0.8183 | 0.93845 | 0.95592
Chart: Mass Spinel
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Target | 0.1 | 0.08 | 0.08 | 0.1 | 0.08 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.08 | 0.08 | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 | 0.08 | 0.08
Calculated | 0.061416 | 0.0096247 | 0.089337 | 0.070796 | 0.031326 | 0.17189 | 0.16726 | 0.19092 | 0.14494 | 0.16018 | 0.058116 | 0.22014 | 0.19447 | 0.18585 | 0.12068 | 0.19354 | 0 | 0 | 0.13604 | 0.096 | 0.13184 | 0.03631 | 0.16158 | 0 | 0
Chart: Mass Olivine
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Target | 0 | 0.02 | 0.02 | 0 | 0.02 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.02 | 0.02 | 0 | 0 | 0 | 0 | 0 | 0.02 | 0.02
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.013657 | 0 | 0 | 0 | 0.031474 | 0.013545 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.037996 | 0.0042378

## Slide 17
Chart: wt%Ag in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.34742 | 0.59528 | 0.36453 | 0 | 0 | 0.11118 | 0.067674 | 0 | 0 | 0 | 0 | 0 | 0.11037 | 0.21621 | 0.099555 | 0.37069 | 0.66954
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.27566 | 0.7043 | 0.50169 | 0.047963 | 0.10856 | 0.33107 | 0.21922 | 0.11121 | 0 | 0 | 0 | 0 | 0.15187 | 0.26994 | 0.13666 | 0.46285 | 0.79849
Chart: wt%Au in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.090838 | 0.16473 | 0.19348 | 0.078999 | 0.034571 | 0.09 | 0.13208 | 0.11301 | 0 | 0 | 0 | 0 | 0.17381 | 0.18058 | 0.089551 | 0.11853 | 0.22663
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.043885 | 0.12159 | 0.12946 | 0.045353 | 0.022716 | 0.11683 | 0.1658 | 0.077767 | 0 | 0 | 0 | 0 | 0.22176 | 0.20723 | 0.077621 | 0.12366 | 0.31547
Chart: Log10[wt%Ag in slag / wt% Ag in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -2.1694 | -2.1758 | -2.0822 | -1.996 | -2.0243 | -2.5143 | -2.3516 | -2.4347 | -2.077 | -1.9564 | -1.9449 | -2.2658 | -2.2315
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -2.0585 | -2.1165 | -2.2603 | -2.0536 | -2.0376 | -2.2363 | -2.2506 | -2.1488 | -2.141 | -2.1508 | -2.1159 | -2.3065 | -2.1908
LA-ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A
Chart: Log10[wt%Au in slag / wt% Au in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -4.4779 | -3.6906 | -3.2636 | -3.6983 | -4.1953 | -3.57 | -4.0516 | -3.8627 | -3.0189 | -2.8969 | -3.8575 | -3.6257 | -2.8802
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -3.6902 | -3.0754 | -3.3576 | -3.5562 | -3.7249 | -3.2623 | -3.06 | -3.5532 | -3.0528 | -3.0754 | -3.7906 | -3.7198 | -2.9822
Chart: ppm Ag in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Ag, exp LA ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 52.4858 | 42.0944 | 44.967 | 65.8556 | 62.1653 | 4.4677 | 22.8511 | 5.1907 | 45.8994 | 58.0456 | 54.243 | 32.9955 | 43.2223
Ag, Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 67.9146 | 48.4977 | 30.1642 | 57.9843 | 60.5918 | 8.5041 | 28.9877 | 10.0914 | 39.8424 | 37.5209 | 36.7747 | 30.1875 | 47.6849
Chart: ppm Au in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Au, exp LA ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.35995 | 2.1753 | 4.3562 | 1.1215 | 0.53462 | 1.5301 | 0.45779 | 0.8206 | 4.2584 | 5.1525 | 0.54425 | 1.2394 | 6.6318
Au, Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 2.2156 | 9.0139 | 3.5393 | 1.5607 | 1.5852 | 3.1243 | 4.5159 | 1.6883 | 3.9561 | 3.4452 | 0.6355 | 1.0026 | 5.2749
Figure S2. FactSage predictions for experiments

## Slide 18: Figure S3. FactSage predictions for experiments
Chart: Log10[wt%Ni in slag / wt% Ni in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -1.0692 | -1.4311 | -1.451 | -1.238 | -0.97057 | -1.6946 | -1.5535 | -1.5081 | #N/A | #N/A | #N/A | #N/A | -1.2952 | -1.4605 | -0.94305 | -0.85467 | -1.2758
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -1.1805 | -1.4498 | -1.2472 | -1.2314 | -1.0713 | -1.6014 | -1.3877 | -1.3679 | #N/A | #N/A | #N/A | #N/A | -1.4747 | -1.4976 | -1.1762 | -1.0484 | -1.3049
Chart: wt%Ni in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 7.7058 | 11.4042 | 11.2912 | 10.7292 | 5.8985 | 12.7832 | 12.3087 | 11.7552 | 0 | 0 | 0 | 0 | 1.1461 | 1.1743 | 0.83883 | 0.80535 | 1.072
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 7.3409 | 11.3135 | 10.9726 | 10.2171 | 5.6404 | 12.5699 | 11.9081 | 11.0788 | 0 | 0 | 0 | 0 | 1.1712 | 1.1859 | 0.84263 | 0.85364 | 1.0933
Chart: Log10[wt%Co in slag / wt% Co in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.40776 | -0.0043924 | 0.10782 | 0.24001 | 0.38981 | -0.26182 | -0.22629 | -0.062668 | #N/A | #N/A | #N/A | #N/A | -0.048511 | -0.1307 | 0.63816 | 0.42647 | -0.079443
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.50698 | 0.038119 | 0.03271 | 0.42275 | 0.57773 | -0.023425 | -0.17416 | 0.28007 | #N/A | #N/A | #N/A | #N/A | -0.058068 | -0.061465 | 0.46293 | 0.15443 | -0.25319
Chart: wt%Co in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.08845 | 0.25154 | 0.20912 | 0.12229 | 0.064238 | 0.26501 | 0.23551 | 0.16595 | 0 | 0 | 0 | 0 | 0.19747 | 0.21396 | 0.057782 | 0.086324 | 0.21372
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.075391 | 0.23725 | 0.22472 | 0.092947 | 0.046017 | 0.20825 | 0.21423 | 0.15718 | 0 | 0 | 0 | 0 | 0.20517 | 0.20762 | 0.082165 | 0.13248 | 0.25746
Chart: wt%S in slag
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 1 | 0.28 | 0.28629 | 0.15 | 0.82 | 0.78 | 0.97 | 0.33 | 0.12533 | 0.73764 | 0.6067 | #N/A | #N/A | #N/A | #N/A | #N/A | 0.10964 | 0.3847 | 0.061874 | 0.062913 | 0.8421 | 0.62927 | 0.17585 | 0.34288 | 1.4459
Calculated | 1.1058 | 0.31907 | 0.24274 | 0.15663 | 0.90335 | 0.84876 | 1.0627 | 0.35948 | 0.16485 | 0.76369 | 0.60057 | 0.23049 | 0.15951 | 0.59813 | 0.99524 | 0.29063 | 0.19574 | 0.46532 | 0.058025 | 0.1324 | 1.0033 | 0.9548 | 0.20593 | 0.44126 | 1.5605

## Slide 19
Chart: wt%Zn in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.090838 | 0.16473 | 0.19348 | 0.078999 | 0.034571 | 0.09 | 0.13208 | 0.11301 | 0 | 0 | 0 | 0 | 0.17381 | 0.18058 | 0.089551 | 0.11853 | 0.22663
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.043885 | 0.12159 | 0.12946 | 0.045353 | 0.022716 | 0.11683 | 0.1658 | 0.077767 | 0 | 0 | 0 | 0 | 0.22176 | 0.20723 | 0.077621 | 0.12366 | 0.31547
Chart: Log10[wt%Zn in slag / wt% Zn in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.5858 | 0.36341 | 0.47066 | 0.55923 | 0.77249 | 0.61555 | 0.6056 | 0.53017 | #N/A | #N/A | #N/A | #N/A | 0.51417 | 0.47966 | 0.72557 | 0.78977 | 0.54799
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.9415 | 0.55902 | 0.67945 | 0.8899 | 1.0185 | 0.48553 | 0.47076 | 0.74566 | #N/A | #N/A | #N/A | #N/A | 0.42819 | 0.422 | 0.88414 | 0.76483 | 0.34687
Chart: Log10[wt%Pb in slag / wt% Pb in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -0.10738 | -0.24851 | -0.041551 | #N/A | #N/A | 0.50053 | 0.49704 | #N/A | #N/A | #N/A | #N/A | #N/A | -0.11702 | -0.18466 | 0.23114 | -0.097652 | -0.38031
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.12633 | -0.48418 | -0.45877 | 0.0077506 | 0.1736 | -0.45054 | -0.66888 | -0.11495 | #N/A | #N/A | #N/A | #N/A | -0.52249 | -0.50836 | 0.020703 | -0.38325 | -0.77029
Chart: wt%Pb in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.34742 | 0.59528 | 0.36453 | 0 | 0 | 0.11118 | 0.067674 | 0 | 0 | 0 | 0 | 0 | 0.11037 | 0.21621 | 0.099555 | 0.37069 | 0.66954
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.27566 | 0.7043 | 0.50169 | 0.047963 | 0.10856 | 0.33107 | 0.21922 | 0.11121 | 0 | 0 | 0 | 0 | 0.15187 | 0.26994 | 0.13666 | 0.46285 | 0.79849
Chart: wt%Bi in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.028745 | 0.32946 | 0.45585 | 0.0010284 | 0.0011823 | 0.62351 | 0.020962 | 0.027733 | 0 | 0 | 0 | 0 | 0.00049526 | 0.21058 | 3.3258e-05 | 0.26307 | 0.7238
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.024416 | 0.33287 | 0.37959 | 0.00088538 | 0.0011162 | 0.5357 | 0.018432 | 0.022543 | 0 | 0 | 0 | 0 | 0.00045886 | 0.18918 | 2.8001e-05 | 0.21174 | 0.66463
Chart: Log10[wt%Bi in slag / wt% Bi in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
LA-ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -1.2478 | -0.73614 | -1.5004 | -1.088 | -0.60949 | -1.7044 | -1.2061 | -1.5122 | #N/A | #N/A | #N/A | #N/A | -1.179 | -1.3979 | -0.90748 | -1.0178 | -1.3413
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -0.55253 | -0.73023 | -0.58991 | -0.50494 | -0.43805 | -0.6461 | -0.62556 | -0.47734 | #N/A | #N/A | #N/A | #N/A | -0.74708 | -0.7613 | -0.40628 | -0.42304 | -0.83657
Figure S4. FactSage predictions for experiments

## Slide 20: Figure S5. FactSage predictions for experiments
Chart: wt%As in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.1952 | 0.44166 | 0.12969 | 0.028787 | 0.13033 | 0.58 | 0.67 | 0.06 | 0 | 0 | 0 | 0 | 0.0070657 | 0.014938 | 0.0038771 | 0.016333 | 0.10252
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.092691 | 0.12844 | 0.094113 | 0.017223 | 0.047493 | 0.16737 | 0.25368 | 0.042261 | 0 | 0 | 0 | 0 | 0.0016983 | 0.0043048 | 0.004757 | 0.021816 | 0.074844
Chart: Log10[wt%As in slag / wt% As in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | -0.016791 | -0.27394 | 0.15585 | 0.04962 | -0.06165 | -0.32281 | -0.32448 | 0.26324 | #N/A | #N/A | #N/A | #N/A | 0.24025 | 0.5087 | 0.97054 | 1.0302 | 0.73215
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.533 | 0.68034 | 0.35841 | 0.46976 | 0.67853 | 0.67173 | 0.50091 | 0.52898 | #N/A | #N/A | #N/A | #N/A | 1.0716 | 1.146 | 0.92578 | 0.8872 | 0.86942
LA-ICP-MS | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A
Chart: wt%Sb in matte
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Experiment | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.082675 | 0.089999 | 0.11237 | 0.043173 | 0.18894
Calculated | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.12924 | 0.10369 | 0.091643 | 0.10151 | 0.24318
Chart: Log10[wt%Sb in slag / wt% Sb in matte)
| RSM1 | RSM3 | RSM3 | RSM6 | RSM6 | RSM8 | RSM10 | RSM12 | RSM13 new | RSM11 new | RSM2 new | RSM11 old (pure SO2) | RSM13old (pure SO2) | RSM9 | RSM2 pure SO2 | RSM9 (pure SO2 | RSM14 new | RSM15 new | RSM17 | RSM6 | RSM11 new | RSM9 new | RSM13 new | RSM4 new | RSM2 new
Calculated | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.47228 | 0.46778 | 0.83679 | 0.68049 | 0.32771
EPMA | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | #N/A | 0.68892 | 0.56161 | 0.68849 | 1.1213 | 0.5076

## Slide 21: Figure S6. Case 1. Smelter

## Slide 22: Figure S7. Case 1. Converter

## Slide 23: Figure S8. Case 1. Anode refining

## Slide 24: Figure S9. Case 2. Smelter

## Slide 25: Figure S9. Case 2. Converter

## Slide 26: Figure S10. Case 2. Anode refining